|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src1566 / NDC92

Empirical formula 	C144H96B3F78Fe4Ga4O8

Formula weight 	3970.92

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Hexagonal

Space group 	R-3

Unit cell dimensions	a = 24.595(2) Å	a = 90°

b = 24.595(2) Å	b = 90°

c = 48.278(6) Å	g  = 120°

Volume	25293(4) Å3

Z	6

Density (calculated)	1.564 Mg / m3

Absorption coefficient	1.100 mm-1

F(000)	11814

Crystal	Block; Light Pink

Crystal size	0.14 ´ 0.10 ´ 0.06 mm3

q range for data collection	3.03 - 27.48°

Index ranges	-31 £ h £ 31, -31 £ k £ 29, -61 £ l £ 62

Reflections collected	74112

Independent reflections	12842 [Rint = 0.0980]

Completeness to q = 27.48°	99.6 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9369 and 0.8612

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	12842 / 3107 / 1273

Goodness-of-fit on F2	1.141

Final R indices [F2 > 2s(F2)]	R1 = 0.0974, wR2 = 0.2097

R indices (all data)	R1 = 0.1306, wR2 = 0.2270

Largest diff. peak and hole	0.954 and -0.766 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

There was disordered in the various ionic species.

The SQUEEZE program was used to remove a highly disordered species, which might have been a [cp*Fe(CO)3]+ ion.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

F1	3532(2)	7420(2)	611(1)	47(1)	1

F2	4091(2)	7200(2)	1087(1)	46(1)	1

Ga1	3616(1)	7602(1)	1000(1)	28(1)	1

Ga2	3333	6667	400(1)	30(1)	1

C1	4766(3)	8992(2)	986(1)	32(1)	1

C2	4836(3)	9239(3)	1258(1)	37(1)	1

C3	4460(3)	9528(3)	1276(1)	39(1)	1

C4	4177(3)	9479(3)	1020(1)	39(1)	1

C5	4366(3)	9144(3)	836(1)	35(1)	1

C6	5148(3)	8732(3)	860(2)	47(2)	1

C7	5264(3)	9240(4)	1474(2)	55(2)	1

C8	4408(4)	9863(3)	1529(2)	64(2)	1

C9	3775(4)	9761(4)	937(2)	57(2)	1

C10	4235(3)	9059(3)	534(1)	47(2)	1

C11	3093(3)	8347(3)	1136(1)	34(1)	1

C12	3814(3)	8259(3)	1503(1)	31(1)	1

O11	2573(2)	8210(2)	1120(1)	47(1)	1

O12	3788(2)	8092(2)	1732(1)	41(1)	1

Fe1	3886(1)	8576(1)	1179(1)	27(1)	1

C101	3425(8)	6545(8)	-491(2)	53(4)	0.33

C102	2854(7)	6230(7)	-343(3)	52(4)	0.33

C103	2757(6)	6686(7)	-215(2)	41(3)	0.33

C104	3251(7)	7278(7)	-278(2)	38(3)	0.33

C105	3676(7)	7198(7)	-455(2)	48(4)	0.33

C106	3734(11)	6261(12)	-663(3)	67(7)	0.33

C107	2426(10)	5529(8)	-325(4)	64(6)	0.33

C108	2192(8)	6564(12)	-32(4)	72(8)	0.33

C109	3346(10)	7921(8)	-187(4)	48(5)	0.33

C110	4273(8)	7713(11)	-571(3)	69(6)	0.33

C111	4257(6)	7462(7)	65(3)	43(4)	0.33

C112	3795(10)	6208(9)	0(3)	55(5)	0.33

O111	4628(7)	7947(7)	143(4)	75(5)	0.33

O112	3990(10)	5853(8)	5(3)	65(5)	0.33

Fe2	3596(1)	6774(2)	-61(1)	33(1)	0.33

B1	1756(3)	8297(3)	-674(1)	43(1)	1

C21	2020(2)	9057(3)	-643(1)	37(1)	1

C22	2330(3)	9491(3)	-860(1)	43(1)	1

C23	2591(3)	10110(3)	-843(1)	43(1)	1

C24	2523(3)	10381(3)	-604(1)	43(1)	1

C25	2191(3)	9984(3)	-388(1)	45(2)	1

C26	1948(3)	9353(3)	-410(1)	42(1)	1

C27	2889(10)	10510(11)	-1093(4)	60(6)	0.32(5)

C28	2110(11)	10258(11)	-127(4)	65(6)	0.32(5)

F21	3330(13)	10399(17)	-1195(8)	87(9)	0.32(5)

F22	2491(19)	10410(30)	-1294(7)	93(12)	0.32(5)

F23	3200(20)	11108(11)	-1037(8)	82(10)	0.32(5)

F24	2250(30)	10853(13)	-155(9)	107(12)	0.32(5)

F25	1546(13)	9960(20)	-37(8)	101(10)	0.32(5)

F26	2480(20)	10270(30)	75(6)	105(10)	0.32(5)

C127	2957(7)	10516(6)	-1083(3)	54(3)	0.68(5)

C128	2068(8)	10238(6)	-129(2)	64(4)	0.68(5)

F121	3269(8)	10292(8)	-1221(3)	96(5)	0.68(5)

F122	2576(9)	10553(12)	-1267(4)	76(4)	0.68(5)

F123	3370(10)	11102(6)	-1016(5)	79(5)	0.68(5)

F124	2436(9)	10863(6)	-110(4)	78(4)	0.68(5)

F125	1495(7)	10097(13)	-97(5)	132(8)	0.68(5)

F126	2224(16)	10024(10)	95(3)	118(7)	0.68(5)

C31	1190(5)	8113(3)	-894(3)	38(3)	0.534(10)

C32	1146(5)	8018(5)	-1177(3)	41(3)	0.534(10)

C33	624(6)	7868(8)	-1326(2)	58(4)	0.534(10)

C34	84(6)	7767(9)	-1195(3)	45(4)	0.534(10)

C35	87(6)	7873(9)	-911(3)	47(4)	0.534(10)

C36	626(6)	8028(9)	-776(3)	42(4)	0.534(10)

C37	615(7)	7833(8)	-1636(3)	87(5)	0.534(10)

C38	-472(6)	7830(7)	-770(3)	58(3)	0.534(10)

F31	857(8)	8415(8)	-1750(3)	132(6)	0.534(10)

F32	1010(7)	7672(11)	-1735(3)	136(6)	0.534(10)

F33	73(6)	7535(7)	-1752(3)	110(5)	0.534(10)

F34	-884(8)	7824(9)	-956(3)	90(5)	0.534(10)

F35	-346(5)	8283(5)	-598(2)	82(3)	0.534(10)

F36	-804(7)	7309(6)	-627(3)	85(4)	0.534(10)

C131	1095(6)	8043(3)	-850(3)	37(4)	0.466(10)

C132	992(6)	7895(5)	-1130(3)	73(6)	0.466(10)

C133	531(7)	7686(8)	-1301(3)	67(5)	0.466(10)

C134	-19(8)	7609(10)	-1199(4)	61(5)	0.466(10)

C135	-7(7)	7720(11)	-916(4)	55(5)	0.466(10)

C136	501(7)	7927(9)	-752(4)	38(4)	0.466(10)

C137	576(8)	7533(7)	-1594(3)	82(5)	0.466(10)

C138	-626(7)	7585(8)	-803(4)	75(5)	0.466(10)

F131	878(7)	8036(6)	-1746(2)	73(4)	0.466(10)

F132	875(9)	7216(7)	-1633(2)	121(5)	0.466(10)

F133	41(7)	7172(10)	-1700(4)	166(10)	0.466(10)

F134	-769(13)	8019(11)	-870(6)	141(9)	0.466(10)

F135	-1070(6)	7068(8)	-897(4)	137(7)	0.466(10)

F136	-627(11)	7536(13)	-533(3)	131(8)	0.466(10)

C41	1617(8)	7967(7)	-366(3)	33(3)	0.450(15)

C42	1976(8)	8175(7)	-116(3)	42(4)	0.450(15)

C43	1847(8)	7892(8)	127(3)	44(4)	0.450(15)

C44	1298(7)	7330(7)	161(4)	40(4)	0.450(15)

C45	914(7)	7073(7)	-66(3)	44(4)	0.450(15)

C46	1077(9)	7374(8)	-310(4)	40(4)	0.450(15)

C47	2247(7)	8131(8)	381(3)	52(4)	0.450(15)

C48	340(7)	6449(7)	-25(3)	56(4)	0.450(15)

F41	2682(11)	8728(7)	365(6)	71(5)	0.450(15)

F42	2556(6)	7824(6)	434(3)	59(3)	0.450(15)

F43	1923(8)	8080(11)	604(3)	82(4)	0.450(15)

F44	-31(11)	6237(12)	-243(4)	99(7)	0.450(15)

F45	0(9)	6430(9)	175(4)	161(10)	0.450(15)

F46	475(10)	5990(8)	16(8)	151(10)	0.450(15)

C141	1607(7)	7892(7)	-401(2)	46(4)	0.550(15)

C142	2010(7)	8142(6)	-174(3)	41(4)	0.550(15)

C143	1918(7)	7841(7)	68(3)	46(4)	0.550(15)

C144	1411(7)	7248(7)	98(3)	55(5)	0.550(15)

C145	1005(7)	6970(6)	-122(3)	66(5)	0.550(15)

C146	1110(8)	7283(7)	-362(3)	56(6)	0.550(15)

C147	2378(7)	8129(8)	298(3)	60(4)	0.550(15)

C148	451(7)	6326(7)	-94(3)	112(6)	0.550(15)

F141	2656(11)	8748(7)	302(5)	92(6)	0.550(15)

F142	2839(8)	8002(9)	274(4)	135(7)	0.550(15)

F143	2131(8)	7952(9)	540(3)	116(7)	0.550(15)

F144	-82(8)	6307(12)	-159(4)	139(8)	0.550(15)

F145	372(11)	6107(11)	155(4)	195(12)	0.550(15)

F146	509(7)	5945(6)	-271(4)	158(7)	0.550(15)

C51	2368(7)	8267(7)	-778(2)	36(4)	0.344(8)

C52	3014(7)	8672(7)	-792(3)	30(4)	0.344(8)

C53	3463(6)	8595(7)	-887(4)	42(5)	0.344(8)

C54	3288(7)	8018(6)	-999(4)	44(4)	0.344(8)

C55	2664(7)	7554(6)	-984(4)	51(4)	0.344(8)

C56	2229(8)	7664(7)	-866(4)	48(5)	0.344(8)

C57	4118(7)	9129(8)	-891(4)	64(6)	0.344(8)

C58	2482(8)	6911(7)	-1081(4)	72(5)	0.344(8)

F51	4146(13)	9654(10)	-983(8)	93(8)	0.344(8)

F52	4468(9)	9040(11)	-1071(6)	106(7)	0.344(8)

F53	4375(11)	9240(13)	-651(5)	143(11)	0.344(8)

F54	2251(11)	6472(7)	-887(4)	136(8)	0.344(8)

F55	2925(7)	6916(9)	-1202(6)	225(14)	0.344(8)

F56	2049(11)	6708(11)	-1280(5)	124(10)	0.344(8)

C151	2263(4)	8182(4)	-855(2)	41(3)	0.656(8)

C152	2914(5)	8591(5)	-859(2)	47(3)	0.656(8)

C153	3350(4)	8551(5)	-999(2)	46(3)	0.656(8)

C154	3166(5)	8031(4)	-1166(2)	51(3)	0.656(8)

C155	2538(5)	7577(4)	-1175(2)	49(2)	0.656(8)

C156	2140(5)	7650(5)	-1018(2)	47(3)	0.656(8)

C157	4022(5)	9049(5)	-981(3)	64(3)	0.656(8)

C158	2322(5)	7020(5)	-1356(2)	63(3)	0.656(8)

F151	4091(9)	9607(6)	-922(5)	118(6)	0.656(8)

F152	4312(5)	9119(6)	-1221(3)	109(4)	0.656(8)

F153	4343(5)	8960(5)	-794(3)	108(4)	0.656(8)

F154	2153(5)	7128(4)	-1605(2)	99(3)	0.656(8)

F155	2714(4)	6836(5)	-1396(2)	84(3)	0.656(8)

F156	1807(5)	6517(5)	-1260(3)	99(4)	0.656(8)

Table 3. Bond lengths [Å] and angles [°].

F1-Ga1	1.918(4)

F1-Ga2	1.951(4)

F2-Ga1	1.919(4)

F2-Ga1i	1.935(4)

Ga1-F2ii	1.935(4)

Ga1-Fe1	2.3073(10)

Ga2-F1ii	1.951(4)

Ga2-F1i	1.951(4)

Ga2-Fe2ii	2.296(3)

Ga2-Fe2i	2.296(3)

Ga2-Fe2	2.296(3)

C1-C5	1.414(8)

C1-C2	1.422(8)

C1-C6	1.502(8)

C1-Fe1	2.095(5)

C2-C3	1.424(9)

C2-C7	1.482(9)

C2-Fe1	2.109(6)

C3-C4	1.391(9)

C3-C8	1.516(9)

C3-Fe1	2.095(6)

C4-C5	1.436(8)

C4-C9	1.519(9)

C4-Fe1	2.109(6)

C5-C10	1.489(9)

C5-Fe1	2.105(6)

C6-H6A	0.9800

C6-H6B	0.9800

C6-H6C	0.9800

C7-H7A	0.9800

C7-H7B	0.9800

C7-H7C	0.9800

C8-H8A	0.9800

C8-H8B	0.9800

C8-H8C	0.9800

C9-H9A	0.9800

C9-H9B	0.9800

C9-H9C	0.9800

C10-H10A	0.9800

C10-H10B	0.9800

C10-H10C	0.9800

C11-O11	1.152(7)

C11-Fe1	1.752(6)

C12-O12	1.168(7)

C12-Fe1	1.718(6)

C101-C105	1.414(17)

C101-C102	1.413(17)

C101-C106	1.509(16)

C101-Fe2	2.136(9)

C102-C103	1.403(16)

C102-C107	1.508(17)

C102-Fe2	2.127(10)

C103-C104	1.387(16)

C103-C108	1.543(17)

C103-Fe2	2.099(10)

C104-C105	1.437(16)

C104-C109	1.541(16)

C104-Fe2	2.098(10)

C105-C110	1.489(17)

C105-Fe2	2.127(10)

C106-H10D	0.9800

C106-H10E	0.9800

C106-H10F	0.9800

C107-H10G	0.9800

C107-H10H	0.9800

C107-H10I	0.9800

C108-H10J	0.9800

C108-H10K	0.9800

C108-H10L	0.9800

C109-H10M	0.9800

C109-H10N	0.9800

C109-H10O	0.9800

C110-H11A	0.9800

C110-H11B	0.9800

C110-H11C	0.9800

C111-O111	1.145(15)

C111-Fe2	1.767(12)

C112-O112	1.190(14)

C112-Fe2	1.717(12)

B1-C141	1.584(11)

B1-C31	1.622(11)

B1-C51	1.624(12)

B1-C21	1.648(7)

B1-C41	1.650(11)

B1-C131	1.652(11)

B1-C151	1.659(10)

C21-C26	1.402(8)

C21-C22	1.416(8)

C22-C23	1.328(8)

C22-H22	0.9500

C23-C24	1.385(8)

C23-C27	1.494(13)

C23-C127	1.499(11)

C24-C25	1.384(8)

C24-H24	0.9500

C25-C26	1.360(7)

C25-C28	1.486(13)

C25-C128	1.492(11)

C26-H26	0.9500

C27-F23	1.303(14)

C27-F22	1.311(14)

C27-F21	1.339(14)

C28-F25	1.278(15)

C28-F26	1.327(15)

C28-F24	1.333(14)

C127-F123	1.323(11)

C127-F121	1.325(10)

C127-F122	1.326(12)

C128-F125	1.281(12)

C128-F126	1.341(12)

C128-F124	1.342(11)

C31-C32	1.380(12)

C31-C36	1.415(12)

C32-C33	1.352(12)

C32-H32	0.9500

C33-C34	1.377(12)

C33-C37	1.501(12)

C34-C35	1.394(12)

C34-H34	0.9500

C35-C36	1.350(11)

C35-C38	1.491(12)

C36-H36	0.9500

C37-F33	1.283(13)

C37-F32	1.308(14)

C37-F31	1.360(14)

C38-F35	1.297(13)

C38-F36	1.320(13)

C38-F34	1.346(12)

C131-C132	1.393(12)

C131-C136	1.423(12)

C132-C133	1.284(12)

C132-H132	0.9500

C133-C134	1.361(13)

C133-C137	1.480(13)

C134-C135	1.389(13)

C134-H134	0.9500

C135-C136	1.346(12)

C135-C138	1.489(13)

C136-H136	0.9500

C137-F133	1.271(13)

C137-F131	1.306(13)

C137-F132	1.324(14)

C138-F135	1.274(14)

C138-F136	1.310(14)

C138-F134	1.320(14)

C41-C46	1.425(12)

C41-C42	1.430(12)

C42-C43	1.319(12)

C42-H42	0.9500

C43-C44	1.376(13)

C43-C47	1.495(12)

C44-C45	1.380(13)

C44-H44	0.9500

C45-C46	1.338(12)

C45-C48	1.491(12)

C46-H46	0.9500

C47-F43	1.306(14)

C47-F41	1.317(13)

C47-F42	1.338(13)

C48-F45	1.264(13)

C48-F44	1.317(14)

C48-F46	1.341(14)

C141-C146	1.393(12)

C141-C142	1.398(12)

C142-C143	1.339(11)

C142-H142	0.9500

C143-C144	1.373(12)

C143-C147	1.488(12)

C144-C145	1.379(12)

C144-H144	0.9500

C145-C146	1.345(12)

C145-C148	1.493(12)

C146-H146	0.9500

C147-F143	1.293(13)

C147-F141	1.321(13)

C147-F142	1.322(13)

C148-F145	1.292(13)

C148-F144	1.325(14)

C148-F146	1.329(15)

C51-C52	1.392(13)

C51-C56	1.410(13)

C52-C53	1.294(12)

C52-H52	0.9500

C53-C54	1.372(13)

C53-C57	1.485(13)

C54-C55	1.383(13)

C54-H54	0.9500

C55-C56	1.354(13)

C55-C58	1.488(13)

C56-H56	0.9500

C57-F53	1.280(14)

C57-F52	1.317(15)

C57-F51	1.334(14)

C58-F55	1.229(14)

C58-F54	1.326(14)

C58-F56	1.331(15)

C151-C152	1.403(10)

C151-C156	1.422(11)

C152-C153	1.310(10)

C152-H152	0.9500

C153-C154	1.384(11)

C153-C157	1.489(11)

C154-C155	1.381(11)

C154-H154	0.9500

C155-C156	1.318(11)

C155-C158	1.484(11)

C156-H156	0.9500

C157-F153	1.287(12)

C157-F152	1.325(12)

C157-F151	1.330(12)

C158-F155	1.267(11)

C158-F156	1.337(13)

C158-F154	1.342(11)

Ga1-F1-Ga2	133.0(2)

Ga1-F2-Ga1i	133.5(2)

F1-Ga1-F2	96.53(16)

F1-Ga1-F2ii	93.33(17)

F2-Ga1-F2ii	96.4(2)

F1-Ga1-Fe1	123.41(12)

F2-Ga1-Fe1	121.35(12)

F2ii-Ga1-Fe1	119.18(12)

F1-Ga2-F1ii	95.10(16)

F1-Ga2-F1i	95.10(16)

F1ii-Ga2-F1i	95.10(16)

F1-Ga2-Fe2ii	110.21(13)

F1ii-Ga2-Fe2ii	118.39(14)

F1i-Ga2-Fe2ii	134.58(13)

F1-Ga2-Fe2i	134.58(13)

F1ii-Ga2-Fe2i	110.21(13)

F1i-Ga2-Fe2i	118.39(14)

Fe2ii-Ga2-Fe2i	24.45(10)

F1-Ga2-Fe2	118.39(14)

F1ii-Ga2-Fe2	134.58(13)

F1i-Ga2-Fe2	110.21(13)

Fe2ii-Ga2-Fe2	24.45(10)

Fe2i-Ga2-Fe2	24.45(10)

C5-C1-C2	108.0(5)

C5-C1-C6	125.0(6)

C2-C1-C6	125.9(6)

C5-C1-Fe1	70.8(3)

C2-C1-Fe1	70.8(3)

C6-C1-Fe1	133.2(4)

C1-C2-C3	107.4(5)

C1-C2-C7	125.8(6)

C3-C2-C7	126.6(6)

C1-C2-Fe1	69.7(3)

C3-C2-Fe1	69.7(3)

C7-C2-Fe1	129.8(4)

C4-C3-C2	108.9(5)

C4-C3-C8	126.0(7)

C2-C3-C8	125.0(6)

C4-C3-Fe1	71.2(3)

C2-C3-Fe1	70.7(3)

C8-C3-Fe1	126.5(4)

C3-C4-C5	107.9(5)

C3-C4-C9	127.3(6)

C5-C4-C9	124.7(6)

C3-C4-Fe1	70.2(3)

C5-C4-Fe1	70.0(3)

C9-C4-Fe1	128.4(5)

C1-C5-C4	107.7(5)

C1-C5-C10	126.4(6)

C4-C5-C10	125.3(6)

C1-C5-Fe1	69.9(3)

C4-C5-Fe1	70.2(3)

C10-C5-Fe1	131.9(4)

C1-C6-H6A	109.5

C1-C6-H6B	109.5

H6A-C6-H6B	109.5

C1-C6-H6C	109.5

H6A-C6-H6C	109.5

H6B-C6-H6C	109.5

C2-C7-H7A	109.5

C2-C7-H7B	109.5

H7A-C7-H7B	109.5

C2-C7-H7C	109.5

H7A-C7-H7C	109.5

H7B-C7-H7C	109.5

C3-C8-H8A	109.5

C3-C8-H8B	109.5

H8A-C8-H8B	109.5

C3-C8-H8C	109.5

H8A-C8-H8C	109.5

H8B-C8-H8C	109.5

C4-C9-H9A	109.5

C4-C9-H9B	109.5

H9A-C9-H9B	109.5

C4-C9-H9C	109.5

H9A-C9-H9C	109.5

H9B-C9-H9C	109.5

C5-C10-H10A	109.5

C5-C10-H10B	109.5

H10A-C10-H10B	109.5

C5-C10-H10C	109.5

H10A-C10-H10C	109.5

H10B-C10-H10C	109.5

O11-C11-Fe1	176.5(6)

O12-C12-Fe1	174.5(5)

C12-Fe1-C11	96.7(3)

C12-Fe1-C1	118.4(3)

C11-Fe1-C1	144.7(3)

C12-Fe1-C3	99.4(2)

C11-Fe1-C3	113.9(3)

C1-Fe1-C3	66.4(2)

C12-Fe1-C5	156.0(3)

C11-Fe1-C5	106.5(3)

C1-Fe1-C5	39.3(2)

C3-Fe1-C5	65.9(2)

C12-Fe1-C4	135.5(3)

C11-Fe1-C4	91.8(3)

C1-Fe1-C4	66.4(2)

C3-Fe1-C4	38.6(2)

C5-Fe1-C4	39.8(2)

C12-Fe1-C2	90.6(2)

C11-Fe1-C2	153.5(3)

C1-Fe1-C2	39.5(2)

C3-Fe1-C2	39.6(2)

C5-Fe1-C2	66.0(2)

C4-Fe1-C2	65.8(2)

C12-Fe1-Ga1	87.66(18)

C11-Fe1-Ga1	85.67(19)

C1-Fe1-Ga1	91.84(15)

C3-Fe1-Ga1	157.95(18)

C5-Fe1-Ga1	99.82(17)

C4-Fe1-Ga1	136.63(18)

C2-Fe1-Ga1	120.21(18)

C105-C101-C102	108.1(11)

C105-C101-C106	124.0(16)

C102-C101-C106	128.0(16)

C105-C101-Fe2	70.3(5)

C102-C101-Fe2	70.3(5)

C106-C101-Fe2	125.2(4)

C103-C102-C101	107.7(12)

C103-C102-C107	126.1(15)

C101-C102-C107	126.2(16)

C103-C102-Fe2	69.6(5)

C101-C102-Fe2	71.0(5)

C107-C102-Fe2	125.0(4)

C104-C103-C102	109.5(12)

C104-C103-C108	124.1(15)

C102-C103-C108	126.4(15)

C104-C103-Fe2	70.6(5)

C102-C103-Fe2	71.7(5)

C108-C103-Fe2	124.0(4)

C103-C104-C105	107.6(11)

C103-C104-C109	128.2(14)

C105-C104-C109	124.3(14)

C103-C104-Fe2	70.8(5)

C105-C104-Fe2	71.2(5)

C109-C104-Fe2	124.4(5)

C101-C105-C104	107.2(11)

C101-C105-C110	127.1(15)

C104-C105-C110	125.7(14)

C101-C105-Fe2	71.0(5)

C104-C105-Fe2	69.0(5)

C110-C105-Fe2	124.3(5)

C101-C106-H10D	109.5

C101-C106-H10E	109.5

H10D-C106-H10E	109.5

C101-C106-H10F	109.5

H10D-C106-H10F	109.5

H10E-C106-H10F	109.5

C102-C107-H10G	109.5

C102-C107-H10H	109.5

H10G-C107-H10H	109.5

C102-C107-H10I	109.5

H10G-C107-H10I	109.5

H10H-C107-H10I	109.5

C103-C108-H10J	109.5

C103-C108-H10K	109.5

H10J-C108-H10K	109.5

C103-C108-H10L	109.5

H10J-C108-H10L	109.5

H10K-C108-H10L	109.5

C104-C109-H10M	109.5

C104-C109-H10N	109.5

H10M-C109-H10N	109.5

C104-C109-H10O	109.5

H10M-C109-H10O	109.5

H10N-C109-H10O	109.5

C105-C110-H11A	109.5

C105-C110-H11B	109.5

H11A-C110-H11B	109.5

C105-C110-H11C	109.5

H11A-C110-H11C	109.5

H11B-C110-H11C	109.5

O111-C111-Fe2	169.6(19)

O112-C112-Fe2	169.7(18)

C112-Fe2-C111	102.5(9)

C112-Fe2-C104	158.2(6)

C111-Fe2-C104	93.3(7)

C112-Fe2-C103	129.9(8)

C111-Fe2-C103	127.4(7)

C104-Fe2-C103	38.6(5)

C112-Fe2-C102	95.8(7)

C111-Fe2-C102	155.7(7)

C104-Fe2-C102	65.2(5)

C103-Fe2-C102	38.8(5)

C112-Fe2-C105	123.8(6)

C111-Fe2-C105	91.3(6)

C104-Fe2-C105	39.8(4)

C103-Fe2-C105	65.2(5)

C102-Fe2-C105	65.1(5)

C112-Fe2-C101	92.9(6)

C111-Fe2-C101	123.5(7)

C104-Fe2-C101	65.6(5)

C103-Fe2-C101	64.9(5)

C102-Fe2-C101	38.7(5)

C105-Fe2-C101	38.7(5)

C112-Fe2-Ga2	85.3(5)

C111-Fe2-Ga2	81.2(5)

C104-Fe2-Ga2	112.3(4)

C103-Fe2-Ga2	97.2(4)

C102-Fe2-Ga2	116.4(5)

C105-Fe2-Ga2	150.9(4)

C101-Fe2-Ga2	154.8(5)

C141-B1-C31	118.2(8)

C141-B1-C51	98.8(4)

C31-B1-C51	118.2(7)

C141-B1-C21	118.3(6)

C31-B1-C21	100.0(3)

C51-B1-C21	103.4(7)

C141-B1-C41	8.3(8)

C31-B1-C41	121.0(8)

C51-B1-C41	102.8(4)

C21-B1-C41	110.0(6)

C141-B1-C131	108.4(8)

C31-B1-C131	10.4(9)

C51-B1-C131	125.7(8)

C21-B1-C131	103.4(3)

C41-B1-C131	110.8(8)

C141-B1-C151	106.7(3)

C31-B1-C151	102.8(7)

C51-B1-C151	15.5(5)

C21-B1-C151	109.8(5)

C41-B1-C151	112.2(3)

C131-B1-C151	110.2(7)

C26-C21-C22	111.3(5)

C26-C21-B1	125.6(5)

C22-C21-B1	123.0(5)

C23-C22-C21	126.2(6)

C23-C22-H22	116.9

C21-C22-H22	116.9

C22-C23-C24	119.8(6)

C22-C23-C27	120.2(11)

C24-C23-C27	119.5(11)

C22-C23-C127	120.1(8)

C24-C23-C127	120.1(7)

C27-C23-C127	6.4(12)

C25-C24-C23	117.5(6)

C25-C24-H24	121.3

C23-C24-H24	121.3

C26-C25-C24	120.9(6)

C26-C25-C28	120.0(11)

C24-C25-C28	119.0(11)

C26-C25-C128	118.5(8)

C24-C25-C128	120.6(8)

C28-C25-C128	3.5(14)

C25-C26-C21	124.0(6)

C25-C26-H26	118.0

C21-C26-H26	118.0

F23-C27-F22	109.5(19)

F23-C27-F21	103.5(17)

F22-C27-F21	107(2)

F23-C27-C23	113.1(19)

F22-C27-C23	113(2)

F21-C27-C23	110.0(17)

F25-C28-F26	107.2(19)

F25-C28-F24	106(2)

F26-C28-F24	104.8(18)

F25-C28-C25	112.1(19)

F26-C28-C25	112.7(18)

F24-C28-C25	113(2)

F123-C127-F121	106.7(11)

F123-C127-F122	105.9(11)

F121-C127-F122	105.7(11)

F123-C127-C23	114.3(12)

F121-C127-C23	112.9(10)

F122-C127-C23	110.7(12)

F125-C128-F126	106.7(13)

F125-C128-F124	108.9(12)

F126-C128-F124	103.3(11)

F125-C128-C25	114.4(12)

F126-C128-C25	110.7(12)

F124-C128-C25	112.1(12)

C32-C31-C36	112.6(10)

C32-C31-B1	132.6(11)

C36-C31-B1	114.8(10)

C33-C32-C31	123.9(10)

C33-C32-H32	118.1

C31-C32-H32	118.1

C32-C33-C34	120.2(10)

C32-C33-C37	122.2(11)

C34-C33-C37	117.5(11)

C33-C34-C35	120.2(11)

C33-C34-H34	119.9

C35-C34-H34	119.9

C36-C35-C34	116.2(10)

C36-C35-C38	122.7(11)

C34-C35-C38	121.1(10)

C35-C36-C31	126.8(11)

C35-C36-H36	116.6

C31-C36-H36	116.6

F33-C37-F32	112.7(14)

F33-C37-F31	102.1(13)

F32-C37-F31	99.9(15)

F33-C37-C33	116.6(13)

F32-C37-C33	112.8(12)

F31-C37-C33	110.9(12)

F35-C38-F36	105.4(12)

F35-C38-F34	107.0(12)

F36-C38-F34	104.0(12)

F35-C38-C35	114.5(11)

F36-C38-C35	114.0(12)

F34-C38-C35	111.1(12)

C132-C131-C136	103.6(10)

C132-C131-B1	127.9(12)

C136-C131-B1	128.5(12)

C133-C132-C131	137.6(12)

C133-C132-H132	111.2

C131-C132-H132	111.2

C132-C133-C134	116.1(12)

C132-C133-C137	123.4(13)

C134-C133-C137	120.6(12)

C133-C134-C135	114.1(13)

C133-C134-H134	122.9

C135-C134-H134	122.9

C136-C135-C134	125.2(12)

C136-C135-C138	121.5(13)

C134-C135-C138	113.3(12)

C135-C136-C131	123.1(13)

C135-C136-H136	118.4

C131-C136-H136	118.4

F133-C137-F131	109.5(15)

F133-C137-F132	102.6(15)

F131-C137-F132	104.8(13)

F133-C137-C133	112.2(13)

F131-C137-C133	112.1(12)

F132-C137-C133	115.0(13)

F135-C138-F136	107.4(16)

F135-C138-F134	106.2(16)

F136-C138-F134	109.3(17)

F135-C138-C135	111.3(13)

F136-C138-C135	109.7(14)

F134-C138-C135	112.7(16)

C46-C41-C42	107.4(10)

C46-C41-B1	122.2(12)

C42-C41-B1	130.4(12)

C43-C42-C41	128.3(12)

C43-C42-H42	115.9

C41-C42-H42	115.9

C42-C43-C44	119.4(12)

C42-C43-C47	125.7(13)

C44-C43-C47	114.9(12)

C43-C44-C45	117.9(13)

C43-C44-H44	121.0

C45-C44-H44	121.0

C46-C45-C44	120.0(12)

C46-C45-C48	123.7(13)

C44-C45-C48	116.3(12)

C45-C46-C41	126.9(12)

C45-C46-H46	116.6

C41-C46-H46	116.6

F43-C47-F41	105.7(15)

F43-C47-F42	106.3(12)

F41-C47-F42	105.4(14)

F43-C47-C43	112.7(12)

F41-C47-C43	113.6(14)

F42-C47-C43	112.4(12)

F45-C48-F44	106.4(15)

F45-C48-F46	107.2(17)

F44-C48-F46	101.4(16)

F45-C48-C45	114.1(13)

F44-C48-C45	114.2(15)

F46-C48-C45	112.4(13)

C146-C141-C142	114.6(10)

C146-C141-B1	126.3(11)

C142-C141-B1	119.1(10)

C143-C142-C141	123.5(10)

C143-C142-H142	118.2

C141-C142-H142	118.2

C142-C143-C144	119.5(11)

C142-C143-C147	120.5(11)

C144-C143-C147	119.9(11)

C143-C144-C145	119.6(11)

C143-C144-H144	120.2

C145-C144-H144	120.2

C146-C145-C144	119.7(11)

C146-C145-C148	119.8(11)

C144-C145-C148	120.5(11)

C145-C146-C141	123.0(11)

C145-C146-H146	118.5

C141-C146-H146	118.5

F143-C147-F141	105.0(14)

F143-C147-F142	108.3(14)

F141-C147-F142	105.3(15)

F143-C147-C143	113.4(12)

F141-C147-C143	113.2(13)

F142-C147-C143	111.1(11)

F145-C148-F144	105.5(15)

F145-C148-F146	110.6(16)

F144-C148-F146	105.9(14)

F145-C148-C145	113.1(13)

F144-C148-C145	112.3(14)

F146-C148-C145	109.1(12)

C52-C51-C56	109.1(10)

C52-C51-B1	137.3(11)

C56-C51-B1	113.5(11)

C53-C52-C51	131.6(12)

C53-C52-H52	114.2

C51-C52-H52	114.2

C52-C53-C54	116.3(12)

C52-C53-C57	120.2(13)

C54-C53-C57	123.4(13)

C53-C54-C55	118.5(12)

C53-C54-H54	120.7

C55-C54-H54	120.7

C56-C55-C54	121.2(12)

C56-C55-C58	119.9(12)

C54-C55-C58	118.8(12)

C55-C56-C51	122.6(12)

C55-C56-H56	118.7

C51-C56-H56	118.7

F53-C57-F52	109.6(18)

F53-C57-F51	108.5(18)

F52-C57-F51	102.6(17)

F53-C57-C53	112.3(14)

F52-C57-C53	111.8(15)

F51-C57-C53	111.6(16)

F55-C58-F54	111.1(18)

F55-C58-F56	101.7(17)

F54-C58-F56	105.6(15)

F55-C58-C55	110.1(13)

F54-C58-C55	114.9(13)

F56-C58-C55	112.6(16)

C152-C151-C156	107.0(8)

C152-C151-B1	124.8(8)

C156-C151-B1	128.1(8)

C153-C152-C151	129.6(10)

C153-C152-H152	115.2

C151-C152-H152	115.2

C152-C153-C154	117.8(9)

C152-C153-C157	121.5(10)

C154-C153-C157	120.6(9)

C155-C154-C153	118.8(9)

C155-C154-H154	120.6

C153-C154-H154	120.6

C156-C155-C154	118.6(8)

C156-C155-C158	121.2(9)

C154-C155-C158	120.2(9)

C155-C156-C151	127.7(9)

C155-C156-H156	116.1

C151-C156-H156	116.1

F153-C157-F152	107.5(11)

F153-C157-F151	104.6(13)

F152-C157-F151	105.8(12)

F153-C157-C153	115.0(9)

F152-C157-C153	111.2(10)

F151-C157-C153	112.1(11)

F155-C158-F156	105.1(11)

F155-C158-F154	107.6(9)

F156-C158-F154	104.6(11)

F155-C158-C155	115.8(9)

F156-C158-C155	112.6(9)

F154-C158-C155	110.5(9)

Symmetry transformations used to generate equivalent atoms:

(i) -x+y,-x+1,z    (ii) -y+1,x-y+1,z

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

F1	54(2) 	47(2)	40(2) 	-4(2)	0(2) 	25(2)

F2	53(2) 	41(2)	47(2) 	-4(2)	-4(2) 	25(2)

Ga1	29(1) 	26(1)	29(1) 	-1(1)	1(1) 	14(1)

Ga2	32(1) 	32(1)	26(1) 	0	0 	16(1)

C1	31(3) 	21(3)	39(3) 	4(2)	9(2) 	9(2)

C2	29(3) 	30(3)	35(3) 	1(2)	3(2) 	2(2)

C3	42(3) 	26(3)	36(3) 	2(2)	11(2) 	7(2)

C4	43(3) 	30(3)	45(3) 	5(2)	6(3) 	19(3)

C5	31(3) 	30(3)	39(3) 	2(2)	4(2) 	12(2)

C6	38(3) 	40(4)	63(4) 	13(3)	16(3) 	20(3)

C7	42(4) 	53(4)	49(4) 	8(3)	-10(3) 	7(3)

C8	76(5) 	38(4)	54(4) 	-14(3)	20(4) 	11(4)

C9	56(5) 	46(4)	79(5) 	14(4)	9(4) 	33(4)

C10	53(4) 	41(4)	35(3) 	4(3)	3(3) 	14(3)

C11	32(3) 	35(3)	34(3) 	-1(2)	1(2) 	14(2)

C12	27(3) 	27(3)	36(3) 	-1(2)	3(2) 	13(2)

O11	34(2) 	60(3)	47(3) 	-1(2)	-4(2) 	24(2)

O12	40(2) 	47(3)	33(2) 	6(2)	2(2) 	20(2)

Fe1	28(1) 	24(1)	29(1) 	1(1)	2(1) 	12(1)

C101	70(10) 	84(10)	32(5) 	-11(7)	-17(8) 	59(7)

C102	62(8) 	59(7)	45(9) 	-19(7)	-26(5) 	40(6)

C103	42(6) 	48(7)	37(8) 	3(7)	-7(5) 	27(6)

C104	48(8) 	52(7)	22(7) 	6(6)	4(6) 	31(6)

C105	62(9) 	80(9)	32(6) 	13(6)	10(7) 	57(8)

C106	120(20) 	92(17)	24(8) 	4(10)	2(11) 	83(17)

C107	84(14) 	57(8)	60(15) 	-31(9)	-47(11) 	43(8)

C108	38(10) 	51(15)	120(30) 	-1(14)	18(11) 	17(11)

C109	58(14) 	46(8)	47(12) 	13(9)	8(10) 	31(9)

C110	84(14) 	106(14)	46(13) 	42(11)	38(11) 	68(11)

C111	36(8) 	45(8)	51(9) 	-3(7)	1(5) 	23(6)

C112	88(15) 	64(10)	41(9) 	-15(9)	-20(10) 	59(11)

O111	35(9) 	56(9)	93(14) 	1(9)	4(9) 	-6(7)

O112	116(15) 	90(12)	37(8) 	-9(8)	-9(9) 	86(12)

Fe2	34(1) 	38(2)	29(1) 	1(1)	-2(1) 	19(2)

B1	35(3) 	34(3)	57(4) 	-3(3)	2(3) 	15(3)

C21	37(3) 	34(3)	42(3) 	0(2)	-4(3) 	20(3)

C22	48(4) 	50(3)	38(3) 	-3(3)	-2(3) 	30(3)

C23	48(4) 	42(3)	45(3) 	8(3)	4(3) 	27(3)

C24	50(4) 	33(3)	45(3) 	0(3)	1(3) 	20(3)

C25	57(4) 	40(3)	37(3) 	-5(3)	-5(3) 	24(3)

C26	42(4) 	33(3)	47(4) 	4(3)	2(3) 	17(3)

C27	69(14) 	66(9)	48(9) 	17(9)	12(8) 	34(12)

C28	96(13) 	57(11)	49(10) 	-4(9)	10(9) 	44(14)

F21	53(12) 	67(14)	116(19) 	10(13)	42(11) 	10(11)

F22	101(17) 	110(20)	54(13) 	33(13)	-3(12) 	40(15)

F23	100(20) 	59(8)	64(14) 	26(8)	38(14) 	25(10)

F24	200(30) 	63(11)	66(18) 	-3(11)	37(19) 	70(14)

F25	109(13) 	109(18)	57(14) 	-13(13)	32(10) 	33(13)

F26	150(20) 	120(30)	51(11) 	-33(15)	-26(14) 	70(20)

C127	73(8) 	52(6)	56(6) 	11(5)	26(5) 	45(6)

C128	89(8) 	50(6)	53(6) 	-5(6)	11(7) 	35(7)

F121	166(14) 	94(8)	84(8) 	47(6)	76(8) 	107(10)

F122	97(8) 	87(9)	54(6) 	35(6)	20(6) 	53(7)

F123	73(8) 	49(4)	104(9) 	21(4)	29(6) 	22(4)

F124	113(8) 	52(5)	62(7) 	-22(4)	-1(6) 	36(5)

F125	90(7) 	146(14)	136(15) 	-80(12)	26(7) 	41(7)

F126	226(19) 	84(10)	39(4) 	-5(5)	-6(8) 	73(12)

C31	32(5) 	41(7)	43(6) 	-4(5)	10(5) 	20(5)

C32	21(4) 	46(5)	39(4) 	-11(4)	14(3) 	5(4)

C33	39(6) 	55(10)	51(5) 	-21(6)	-7(5) 	2(7)

C34	22(5) 	34(10)	55(6) 	5(6)	-7(5) 	-5(7)

C35	36(5) 	53(9)	48(6) 	14(6)	0(5) 	19(6)

C36	17(5) 	52(9)	39(7) 	4(7)	11(5) 	4(6)

C37	74(9) 	107(12)	51(7) 	-31(9)	-10(7) 	22(10)

C38	32(6) 	75(9)	59(8) 	13(6)	-4(5) 	22(7)

F31	141(12) 	137(11)	56(7) 	1(8)	10(7) 	25(9)

F32	130(10) 	219(18)	65(9) 	-48(11)	0(8) 	91(13)

F33	94(8) 	124(12)	73(8) 	-28(9)	-48(7) 	25(8)

F34	59(7) 	143(13)	84(8) 	26(7)	-4(6) 	63(9)

F35	69(6) 	105(8)	93(8) 	-8(6)	10(5) 	59(6)

F36	76(9) 	99(8)	88(10) 	39(7)	35(8) 	50(7)

C131	26(5) 	27(7)	34(6) 	12(5)	18(5) 	-4(5)

C132	56(8) 	63(10)	34(7) 	-6(7)	20(6) 	-18(8)

C133	57(8) 	37(9)	40(6) 	-6(6)	8(5) 	-28(7)

C134	52(8) 	21(10)	58(7) 	-6(7)	0(6) 	-21(8)

C135	42(6) 	52(11)	54(7) 	4(8)	0(6) 	12(7)

C136	31(6) 	40(9)	38(7) 	27(6)	21(5) 	13(7)

C137	83(10) 	64(10)	40(7) 	-9(7)	3(7) 	-9(8)

C138	44(8) 	92(11)	74(9) 	15(10)	3(8) 	23(8)

F131	105(10) 	68(8)	34(5) 	10(6)	13(6) 	34(7)

F132	249(16) 	81(9)	31(6) 	-15(6)	-5(8) 	81(11)

F133	91(8) 	173(18)	83(12) 	-95(13)	13(7) 	-46(9)

F134	132(18) 	156(14)	180(20) 	38(15)	41(16) 	105(14)

F135	54(7) 	137(11)	171(15) 	-43(11)	15(8) 	10(7)

F136	86(13) 	240(20)	70(8) 	12(10)	19(7) 	82(14)

C41	28(8) 	21(6)	60(6) 	-7(5)	-6(5) 	21(5)

C42	37(8) 	26(7)	64(7) 	-14(6)	-15(7) 	15(6)

C43	35(7) 	48(7)	56(7) 	-8(6)	-12(6) 	27(5)

C44	33(7) 	44(7)	56(9) 	-8(6)	-5(6) 	29(5)

C45	36(6) 	35(6)	61(8) 	-2(5)	-4(5) 	17(5)

C46	37(7) 	24(6)	61(8) 	-10(6)	-12(6) 	16(5)

C47	43(8) 	58(8)	63(9) 	-3(9)	-17(7) 	30(6)

C48	35(8) 	52(7)	72(9) 	-1(7)	-10(6) 	15(5)

F41	77(9) 	56(6)	70(14) 	-13(6)	-43(7) 	26(6)

F42	67(8) 	75(7)	55(7) 	-4(6)	-22(6) 	52(6)

F43	81(9) 	133(12)	55(8) 	-1(7)	-9(6) 	71(8)

F44	82(11) 	64(10)	65(9) 	12(8)	-27(7) 	-27(7)

F45	118(14) 	116(13)	124(12) 	-43(11)	74(11) 	-35(9)

F46	92(12) 	43(7)	290(30) 	57(16)	-26(17) 	12(7)

C141	33(8) 	37(6)	48(6) 	-5(5)	-8(5) 	4(5)

C142	30(7) 	41(7)	41(6) 	-2(5)	4(5) 	9(5)

C143	43(6) 	49(7)	42(6) 	2(5)	-6(5) 	21(5)

C144	46(8) 	62(8)	45(7) 	13(6)	-1(6) 	17(6)

C145	41(7) 	56(7)	70(9) 	25(6)	-15(6) 	1(6)

C146	51(9) 	40(8)	40(7) 	-3(5)	-14(6) 	-4(6)

C147	61(8) 	68(7)	50(7) 	3(7)	-15(6) 	30(6)

C148	79(9) 	77(10)	98(10) 	59(7)	-51(9) 	-24(7)

F141	101(11) 	74(6)	59(10) 	-5(5)	-46(7) 	13(6)

F142	97(10) 	197(15)	142(14) 	-106(12)	-93(9) 	98(11)

F143	113(13) 	120(12)	48(7) 	2(7)	-21(7) 	8(10)

F144	57(7) 	131(15)	121(16) 	64(11)	-39(9) 	-33(7)

F145	127(16) 	148(17)	130(11) 	111(10)	-80(10) 	-67(10)

F146	153(12) 	43(6)	206(17) 	20(8)	-93(11) 	-5(7)

C51	28(6) 	22(8)	55(10) 	-18(8)	-14(7) 	10(6)

C52	32(6) 	17(7)	26(8) 	-17(7)	-9(7) 	0(6)

C53	31(6) 	26(6)	66(13) 	16(7)	0(7) 	12(5)

C54	42(7) 	40(7)	57(11) 	12(8)	14(9) 	27(6)

C55	52(8) 	31(6)	62(11) 	-9(7)	10(8) 	15(6)

C56	41(8) 	31(7)	51(11) 	-22(9)	13(9) 	3(6)

C57	28(8) 	46(9)	108(14) 	25(10)	0(9) 	11(7)

C58	71(11) 	48(8)	96(13) 	-29(8)	4(9) 	29(8)

F51	22(9) 	44(9)	200(20) 	60(11)	32(11) 	6(7)

F52	42(9) 	97(13)	190(20) 	36(16)	37(13) 	45(9)

F53	84(14) 	120(20)	136(16) 	16(13)	-51(12) 	-18(13)

F54	220(20) 	44(8)	134(14) 	-12(8)	-74(12) 	53(11)

F55	97(13) 	117(15)	400(30) 	-168(19)	67(16) 	8(12)

F56	172(19) 	74(16)	77(14) 	-28(11)	-37(14) 	25(16)

C151	28(4) 	26(5)	58(6) 	-10(5)	-1(5) 	5(4)

C152	27(4) 	39(6)	68(8) 	12(5)	-4(5) 	10(4)

C153	29(4) 	44(5)	65(8) 	22(5)	4(4) 	18(4)

C154	49(5) 	46(5)	66(8) 	17(5)	13(5) 	30(4)

C155	62(6) 	49(5)	44(6) 	-5(4)	1(5) 	33(4)

C156	45(5) 	34(5)	50(7) 	-13(5)	1(5) 	12(4)

C157	32(5) 	46(6)	114(9) 	19(6)	8(5) 	19(5)

C158	59(7) 	79(8)	55(6) 	-22(6)	-1(5) 	39(5)

F151	61(9) 	44(6)	230(17) 	13(8)	47(9) 	12(6)

F152	47(6) 	102(8)	137(9) 	21(7)	39(6) 	7(5)

F153	49(5) 	70(7)	165(11) 	25(7)	-40(7) 	0(5)

F154	156(9) 	107(7)	71(5) 	-37(4)	-43(5) 	93(7)

F155	93(6) 	99(7)	90(6) 	-47(5)	-28(5) 	69(6)

F156	101(7) 	47(5)	134(8) 	-37(5)	23(6) 	26(5)

Table 5. Hydrogen coordinates [´ 104] and isotropic displacement parameters [Å2 ´ 103].

Atom 	x	y	z	Ueq	S.o.f.

H6A	4898	8421	719	70	1

H6B	5266	8532	1005	70	1

H6C	5527	9073	776	70	1

H7A	5671	9628	1461	83	1

H7B	5324	8878	1447	83	1

H7C	5082	9214	1657	83	1

H8A	4511	9704	1695	95	1

H8B	3978	9787	1544	95	1

H8C	4700	10315	1511	95	1

H9A	3500	9724	1091	86	1

H9B	3519	9535	776	86	1

H9C	4046	10205	890	86	1

H10A	4562	9423	434	71	1

H10B	3826	9020	496	71	1

H10C	4231	8678	471	71	1

H10D	4116	6597	-748	100	0.33

H10E	3444	5995	-807	100	0.33

H10F	3843	6007	-543	100	0.33

H10G	2604	5318	-434	96	0.33

H10H	2012	5417	-399	96	0.33

H10I	2385	5395	-132	96	0.33

H10J	2257	6964	41	108	0.33

H10K	2155	6288	122	108	0.33

H10L	1807	6363	-143	108	0.33

H10M	3021	7858	-53	73	0.33

H10N	3316	8145	-349	73	0.33

H10O	3760	8168	-102	73	0.33

H11A	4453	7536	-700	104	0.33

H11B	4571	7930	-420	104	0.33

H11C	4190	8011	-670	104	0.33

H22	2353	9323	-1034	52	1

H24	2697	10823	-589	51	1

H26	1717	9098	-257	50	1

H32	1503	8061	-1272	49	0.534(10)

H34	-292	7624	-1299	54	0.534(10)

H36	627	8087	-581	51	0.534(10)

H132	1366	7968	-1220	87	0.466(10)

H134	-379	7490	-1310	74	0.466(10)

H136	461	7999	-562	46	0.466(10)

H42	2355	8566	-126	51	0.450(15)

H44	1186	7126	336	48	0.450(15)

H46	803	7169	-461	48	0.450(15)

H142	2369	8548	-192	50	0.550(15)

H144	1341	7030	268	66	0.550(15)

H146	831	7080	-512	67	0.550(15)

H52	3149	9079	-719	36	0.344(8)

H54	3589	7940	-1086	52	0.344(8)

H56	1814	7323	-843	57	0.344(8)

H152	3061	8949	-743	57	0.656(8)

H154	3465	7988	-1274	61	0.656(8)

H156	1722	7307	-1013	56	0.656(8)