|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01sot119

Empirical formula 	C6H11Cl0.50N1.50

Formula weight 	121.89

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Cmc21

Unit cell dimensions	a = 15.094(2) Å	 = 90°

b = 9.0070(12) Å	 = 90°

c = 10.3253(16) Å	  = 90°

Volume	1403.7(4) Å3

Z	8

Density (calculated)	1.154 Mg / m3

Absorption coefficient	0.253 mm1

F(000)	528

Crystal	plate; colourless

Crystal size	0.24  0.20  0.04 mm3

 range for data collection	2.63  27.49°

Index ranges	19  h  19, 10  k  11, 13  l  11

Reflections collected	3927

Independent reflections	1465 [Rint = 0.0851]

Completeness to  = 27.49°	97.6 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9899 and 0.9417

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1465 / 1 / 90

Goodness-of-fit on F2	1.056

Final R indices [F2 > 2(F2)]	R1 = 0.0617, wR2 = 0.1393

R indices (all data)	R1 = 0.0900, wR2 = 0.1558

Absolute structure parameter	0.14(13)

Extinction coefficient	0.004(3)

Largest diff. peak and hole	0.521 and 0.416 e Å3

Diffractometer: Enraf Nonius KappaCCD area detector ( scans and  scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Cl1	5000	7885(1)	9719(1)	36(1)	1

C1	7577(3)	8251(4)	5461(4)	44(1)	1

C2	7095(3)	9388(3)	4946(4)	40(1)	1

N1	6405(2)	9657(3)	5737(3)	41(1)	1

C4	6427(3)	8691(4)	6772(4)	47(1)	1

C3	7149(3)	7822(4)	6619(4)	50(1)	1

C5	0	6951(5)	8257(7)	70(2)	1

C6	776(4)	9277(5)	8013(8)	96(2)	1

C7	366(7)	8782(8)	9957(6)	51(2)	0.50

N2	0	8576(4)	8579(4)	47(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1C2	1.364(5)

C1C3	1.413(6)

C1H1	0.9500

C2N1	1.346(5)

C2H2	0.9500

N1C4	1.378(5)

N1H1N	0.92(5)

C4C3	1.351(6)

C4H4	0.9500

C3H3	0.9500

C5N2	1.501(6)

C5H5A	0.9800

C5H5B	0.9800

C5H5C	0.9800

C6N2	1.453(6)

C6H6A	0.9800

C6H6B	0.9800

C6H6C	0.9800

C7N2	1.537(8)

C7H7A	0.9800

C7H7B	0.9800

C7H7C	0.9800

N2C6i	1.453(6)

N2C7i	1.537(8)

C2C1C3	107.0(4)

C2C1H1	126.5

C3C1H1	126.5

N1C2C1	108.1(3)

N1C2H2	125.9

C1C2H2	125.9

C2N1C4	109.8(3)

C2N1H1N	120(3)

C4N1H1N	130(3)

C3C4N1	107.1(4)

C3C4H4	126.4

N1C4H4	126.4

C4C3C1	108.0(4)

C4C3H3	126.0

C1C3H3	126.0

N2C5H5A	109.5

N2C5H5B	109.5

H5AC5H5B	109.5

N2C5H5C	109.5

H5AC5H5C	109.5

H5BC5H5C	109.5

N2C6H6A	109.5

N2C6H6B	109.5

H6AC6H6B	109.5

N2C6H6C	109.5

H6AC6H6C	109.5

H6BC6H6C	109.5

N2C7H7A	109.5

N2C7H7B	109.5

H7AC7H7B	109.5

N2C7H7C	109.5

H7AC7H7C	109.5

H7BC7H7C	109.5

C6iN2C6	107.3(6)

C6iN2C5	109.5(3)

C6N2C5	109.5(3)

C6iN2C7i	91.7(5)

C6N2C7i	127.6(5)

C5N2C7i	108.9(5)

C6iN2C7	127.6(5)

C6N2C7	91.7(5)

C5N2C7	108.9(5)

C7iN2C7	42.2(7)

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Cl1	45(1) 	25(1)	39(1) 	1(1)	0 	0

C1	44(2) 	37(2)	51(2) 	5(2)	1(2) 	9(2)

C2	44(2) 	28(2)	48(3) 	1(2)	4(2) 	0(1)

N1	47(2) 	27(2)	48(2) 	2(1)	1(2) 	6(1)

C4	60(3) 	42(2)	38(2) 	2(2)	5(2) 	2(2)

C3	63(3) 	42(2)	44(2) 	13(2)	3(2) 	10(2)

C5	142(7) 	17(2)	51(4) 	2(2)	0 	0

C6	48(3) 	53(3)	186(8) 	28(4)	3(4) 	5(2)

C7	92(7) 	32(3)	28(4) 	3(3)	6(3) 	5(3)

N2	91(4) 	21(2)	30(2) 	2(2)	0 	0