|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2010src0035 / MABJT/32

Empirical formula 	C5H16B5NO10

Formula weight 	304.24

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 9.4446(4) Å	 = 90°

b = 13.9129(7) Å	 = 92.517(3)°

c = 10.3330(3) Å	  = 90°

Volume	1356.46(10) Å3

Z	4

Density (calculated)	1.490 Mg / m3

Absorption coefficient	0.131 mm1

F(000)	632

Crystal	Cut Block; Colourless

Crystal size	0.42  0.38  0.18 mm3

 range for data collection	3.53  27.48°

Index ranges	12  h  12, 18  k  16, 13  l  13

Reflections collected	15990

Independent reflections	3110 [Rint = 0.0500]

Completeness to  = 27.48°	99.8 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9768 and 0.9469

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3110 / 13 / 215

Goodness-of-fit on F2	1.027

Final R indices [F2 > 2(F2)]	R1 = 0.0447, wR2 = 0.1078

R indices (all data)	R1 = 0.0665, wR2 = 0.1204

Largest diff. peak and hole	0.264 and 0.270 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

The cyclopentane ring was disordered over two sites (76:24) resulting in the use of some mild distance and thermal restraints.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

B1	7796(2)	1246(1)	1286(2)	17(1)	1

B2	5289(2)	762(1)	1198(2)	18(1)	1

B3	6054(2)	1902(1)	337(2)	20(1)	1

B4	10391(2)	996(1)	1350(2)	18(1)	1

B5	9430(2)	2147(1)	2774(2)	19(1)	1

O1	6662(1)	587(1)	1590(1)	18(1)	1

O2	4958(1)	1477(1)	303(1)	20(1)	1

O3	7417(1)	1802(1)	105(1)	19(1)	1

O4	9065(1)	681(1)	1010(1)	18(1)	1

O5	10592(1)	1730(1)	2231(1)	22(1)	1

O6	8092(1)	1901(1)	2381(1)	19(1)	1

O7	4267(1)	201(1)	1669(1)	25(1)	1

O8	5668(1)	2407(1)	1421(1)	25(1)	1

O9	11553(1)	601(1)	840(1)	24(1)	1

O10	9738(1)	2815(1)	3705(1)	25(1)	1

C1	2586(4)	1578(4)	6626(5)	22(1)	0.741(3)

C2	1304(5)	996(3)	6056(5)	34(1)	0.741(3)

C3	1887(5)	373(3)	4970(3)	46(1)	0.741(3)

C4	3274(3)	816(2)	4673(2)	46(1)	0.741(3)

C5	3887(5)	1165(5)	5984(7)	33(1)	0.741(3)

N1	2727(9)	1443(9)	8069(5)	24(1)	0.741(3)

C21	2852(16)	1548(14)	6450(16)	22(1)	0.259(3)

C22	1399(17)	1209(12)	5883(17)	34(1)	0.259(3)

C23	1765(14)	234(11)	5324(12)	46(1)	0.259(3)

C24	3278(9)	126(6)	5270(7)	46(1)	0.259(3)

C25	3987(17)	1026(16)	5810(20)	33(1)	0.259(3)

N21	2880(30)	1430(30)	7880(16)	24(1)	0.259(3)

Table 3. Bond lengths [Å] and angles [°].

B1O1	1.455(2)

B1O6	1.4701(19)

B1O4	1.4715(19)

B1O3	1.4763(19)

B2O7	1.349(2)

B2O1	1.3639(19)

B2O2	1.384(2)

B3O3	1.354(2)

B3O8	1.358(2)

B3O2	1.385(2)

B4O9	1.355(2)

B4O4	1.3581(19)

B4O5	1.374(2)

B5O6	1.354(2)

B5O10	1.359(2)

B5O5	1.383(2)

O7H7	0.8400

O8H8	0.8400

O9H9	0.8400

O10H10	0.8400

C1N1	1.504(5)

C1C5	1.533(4)

C1C2	1.551(5)

C1H1	1.0000

C2C3	1.539(5)

C2H2A	0.9900

C2H2B	0.9900

C3C4	1.492(5)

C3H3A	0.9900

C3H3B	0.9900

C4C5	1.529(6)

C4H4A	0.9900

C4H4B	0.9900

C5H5A	0.9900

C5H5B	0.9900

N1H1A	0.9100

N1H1B	0.9100

N1H1C	0.9100

C21C25	1.472(13)

C21N21	1.486(14)

C21C22	1.543(14)

C21H21	1.0000

C22C23	1.520(15)

C22H22A	0.9900

C22H22B	0.9900

C23C24	1.441(13)

C23H23A	0.9900

C23H23B	0.9900

C24C25	1.517(15)

C24H24A	0.9900

C24H24B	0.9900

C25H25A	0.9900

C25H25B	0.9900

N21H21A	0.9100

N21H21B	0.9100

N21H21C	0.9100

O1B1O6	109.93(11)

O1B1O4	108.62(13)

O6B1O4	110.58(11)

O1B1O3	110.76(11)

O6B1O3	110.05(13)

O4B1O3	106.84(11)

O7B2O1	118.37(14)

O7B2O2	120.87(13)

O1B2O2	120.72(14)

O3B3O8	123.23(14)

O3B3O2	120.95(14)

O8B3O2	115.81(13)

O9B4O4	121.41(14)

O9B4O5	117.94(13)

O4B4O5	120.65(14)

O6B5O10	123.59(14)

O6B5O5	121.22(14)

O10B5O5	115.18(13)

B2O1B1	121.53(13)

B2O2B3	118.32(12)

B3O3B1	121.70(12)

B4O4B1	121.79(12)

B4O5B5	119.47(12)

B5O6B1	122.06(12)

B2O7H7	109.5

B3O8H8	109.5

B4O9H9	109.5

B5O10H10	109.5

N1C1C5	110.2(5)

N1C1C2	110.2(5)

C5C1C2	105.5(3)

N1C1H1	110.3

C5C1H1	110.3

C2C1H1	110.3

C3C2C1	105.8(3)

C3C2H2A	110.6

C1C2H2A	110.6

C3C2H2B	110.6

C1C2H2B	110.6

H2AC2H2B	108.7

C4C3C2	105.2(3)

C4C3H3A	110.7

C2C3H3A	110.7

C4C3H3B	110.7

C2C3H3B	110.7

H3AC3H3B	108.8

C3C4C5	104.5(3)

C3C4H4A	110.8

C5C4H4A	110.8

C3C4H4B	110.8

C5C4H4B	110.8

H4AC4H4B	108.9

C4C5C1	102.9(4)

C4C5H5A	111.2

C1C5H5A	111.2

C4C5H5B	111.2

C1C5H5B	111.2

H5AC5H5B	109.1

C25C21N21	114.2(16)

C25C21C22	109.5(12)

N21C21C22	108.5(15)

C25C21H21	108.2

N21C21H21	108.2

C22C21H21	108.2

C23C22C21	101.7(11)

C23C22H22A	111.4

C21C22H22A	111.4

C23C22H22B	111.4

C21C22H22B	111.4

H22AC22H22B	109.3

C24C23C22	110.5(11)

C24C23H23A	109.6

C22C23H23A	109.6

C24C23H23B	109.6

C22C23H23B	109.6

H23AC23H23B	108.1

C23C24C25	108.8(10)

C23C24H24A	109.9

C25C24H24A	109.9

C23C24H24B	109.9

C25C24H24B	109.9

H24AC24H24B	108.3

C21C25C24	104.7(11)

C21C25H25A	110.8

C24C25H25A	110.8

C21C25H25B	110.8

C24C25H25B	110.8

H25AC25H25B	108.9

C21N21H21A	109.5

C21N21H21B	109.5

H21AN21H21B	109.5

C21N21H21C	109.5

H21AN21H21C	109.5

H21BN21H21C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

B1	13(1) 	23(1)	16(1) 	1(1)	1(1) 	1(1)

B2	16(1) 	21(1)	18(1) 	2(1)	0(1) 	0(1)

B3	17(1) 	24(1)	19(1) 	3(1)	1(1) 	2(1)

B4	14(1) 	21(1)	18(1) 	0(1)	1(1) 	0(1)

B5	17(1) 	23(1)	17(1) 	1(1)	1(1) 	1(1)

O1	12(1) 	21(1)	20(1) 	1(1)	1(1) 	0(1)

O2	13(1) 	27(1)	21(1) 	3(1)	0(1) 	2(1)

O3	14(1) 	25(1)	18(1) 	3(1)	1(1) 	0(1)

O4	12(1) 	22(1)	21(1) 	4(1)	1(1) 	0(1)

O5	13(1) 	27(1)	25(1) 	8(1)	1(1) 	2(1)

O6	14(1) 	25(1)	18(1) 	3(1)	1(1) 	1(1)

O7	13(1) 	29(1)	34(1) 	8(1)	1(1) 	1(1)

O8	17(1) 	35(1)	23(1) 	8(1)	0(1) 	2(1)

O9	13(1) 	30(1)	28(1) 	10(1)	2(1) 	1(1)

O10	17(1) 	33(1)	25(1) 	11(1)	2(1) 	3(1)

C1	18(2) 	25(1)	24(2) 	5(1)	12(1) 	7(1)

C2	33(1) 	41(3)	26(2) 	0(2)	4(1) 	1(2)

C3	64(2) 	44(2)	31(2) 	2(2)	7(2) 	2(1)

C4	62(2) 	47(2)	31(1) 	0(1)	14(1) 	20(1)

C5	35(1) 	29(2)	37(2) 	5(1)	19(1) 	12(1)

N1	19(2) 	28(1)	24(2) 	2(2)	1(1) 	3(2)

C21	18(2) 	25(1)	24(2) 	5(1)	12(1) 	7(1)

C22	33(1) 	41(3)	26(2) 	0(2)	4(1) 	1(2)

C23	64(2) 	44(2)	31(2) 	2(2)	7(2) 	2(1)

C24	62(2) 	47(2)	31(1) 	0(1)	14(1) 	20(1)

C25	35(1) 	29(2)	37(2) 	5(1)	19(1) 	12(1)

N21	19(2) 	28(1)	24(2) 	2(2)	1(1) 	3(2)

Table 5. Hydrogen coordinates [ 104] and isotropic displacement parameters [Å2  103].

Atom 	x	y	z	Ueq	S.o.f.

H7	3469	396	1389	38	1

H8	6396	2619	1763	38	1

H9	11300	194	275	36	1

H10	8993	2970	4068	37	1

H1	2472	2275	6409	27	0.741(3)

H2A	899	587	6731	40	0.741(3)

H2B	555	1434	5704	40	0.741(3)

H3A	2019	299	5263	55	0.741(3)

H3B	1232	380	4195	55	0.741(3)

H4A	3138	1360	4062	56	0.741(3)

H4B	3908	337	4291	56	0.741(3)

H5A	4618	1666	5875	40	0.741(3)

H5B	4307	627	6497	40	0.741(3)

H1A	2827	807	8255	36	0.741(3)

H1B	1938	1673	8438	36	0.741(3)

H1C	3501	1769	8389	36	0.741(3)

H21	2953	2248	6253	27	0.259(3)

H22A	700	1149	6565	40	0.259(3)

H22B	1023	1652	5201	40	0.259(3)

H23A	1382	281	5870	55	0.259(3)

H23B	1322	171	4442	55	0.259(3)

H24A	3540	28	4362	56	0.259(3)

H24B	3597	441	5783	56	0.259(3)

H25A	4766	860	6448	40	0.259(3)

H25B	4376	1418	5114	40	0.259(3)

H21A	2874	795	8081	36	0.259(3)

H21B	2095	1716	8197	36	0.259(3)

H21C	3670	1712	8238	36	0.259(3)

Table 6. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O7H7...O9i	0.84	1.89	2.7241(15)	169.2

O8H8...O6ii	0.84	1.98	2.8194(15)	178.2

O9H9...O4iii	0.84	1.82	2.6603(15)	174.1

O10H10...O3iv	0.84	1.90	2.7311(14)	171.0

N1H1A...O1v	0.91	2.00	2.902(12)	168.9

N1H1B...O10vi	0.91	2.22	3.103(8)	162.0

N1H1C...O8vii	0.91	2.23	3.108(10)	161.7

N1H1C...O2vii	0.91	2.39	3.056(8)	129.8

N21H21A...O1v	0.91	2.00	2.89(4)	166.8

N21H21B...O10vi	0.91	2.40	3.29(2)	166.0

N21H21C...O8vii	0.91	2.14	3.03(3)	165.5

N21H21C...O2vii	0.91	2.43	3.12(2)	132.2

Symmetry transformations used to generate equivalent atoms:

(i) x1,y,z    (ii) x,y+1/2,z1/2    (iii) x+2,y,z

(iv)  x,y+1/2,z+1/2    (v) x+1,y,z+1    (vi) x1,y+1/2,z+1/2

(vii) x,y,z+1