|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005slh0413    (CAG 142)

Empirical formula 	C29H34CdN2O4P2S4

Formula weight 	777.16

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 10.7073(4) Å	a = 90°

b = 16.3214(4) Å	b = 91.799(2)°

c = 19.5513(6) Å	g  = 90°

Volume	3415.06(19) Å3

Z	4

Density (calculated)	1.512 Mg / m3

Absorption coefficient	1.013 mm-1

F(000)	1584

Crystal	fragment; colourless

Crystal size	0.20 ´ 0.20 ´ 0.07 mm3

q range for data collection	3.14 - 27.49°

Index ranges	-13 £ h £ 12, -21 £ k £ 18, -25 £ l £ 21

Reflections collected	22124

Independent reflections	7757 [Rint = 0.0319]

Completeness to q = 27.49°	99.1 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9324 and 0.8230

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7757 / 0 / 384

Goodness-of-fit on F2	1.022

Final R indices [F2 > 2s(F2)]	R1 = 0.0311, wR2 = 0.0663

R indices (all data)	R1 = 0.0461, wR2 = 0.0727

Extinction coefficient	0.00096(19)

Largest diff. peak and hole	0.645 and -0.850 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33-37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421-426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	59(3)	6208(2)	-334(2)	45(1)	1

C2	3135(2)	7172(1)	539(1)	22(1)	1

C3	3965(2)	7240(2)	1094(1)	31(1)	1

C4	5100(2)	7648(2)	1039(2)	34(1)	1

C5	5396(2)	7992(2)	416(2)	32(1)	1

C6	4570(2)	7940(2)	-140(1)	30(1)	1

C7	3450(2)	7530(1)	-83(1)	24(1)	1

C8	7402(3)	8449(2)	848(2)	63(1)	1

C9	605(2)	6302(2)	4429(1)	36(1)	1

C10	3593(2)	5533(1)	3431(1)	21(1)	1

C11	4293(2)	5576(2)	2845(1)	29(1)	1

C12	5506(2)	5301(2)	2844(1)	31(1)	1

C13	6046(2)	4962(1)	3436(1)	22(1)	1

C14	5357(2)	4898(1)	4021(1)	24(1)	1

C15	4134(2)	5183(2)	4014(1)	24(1)	1

C16	7863(2)	4395(2)	3990(2)	37(1)	1

C17	-1880(2)	6681(1)	3100(1)	25(1)	1

C18	-2568(2)	7113(1)	3566(1)	24(1)	1

C19	-2587(2)	7961(1)	3544(1)	19(1)	1

C20	-1912(2)	8334(1)	3037(1)	24(1)	1

C21	-1236(2)	7861(1)	2594(1)	24(1)	1

C22	-3316(2)	8463(1)	4040(1)	20(1)	1

C23	-4540(2)	8788(1)	3715(1)	22(1)	1

C24	-5230(2)	9324(1)	4221(1)	21(1)	1

C25	-6396(2)	9724(1)	3927(1)	18(1)	1

C26	-7299(2)	9297(1)	3545(1)	23(1)	1

C27	-8337(2)	9704(1)	3280(1)	23(1)	1

C29	-7683(2)	10908(2)	3754(1)	28(1)	1

C30	-6613(2)	10550(2)	4024(1)	26(1)	1

N1	-1215(2)	7041(1)	2620(1)	20(1)	1

N2	-8548(2)	10503(1)	3381(1)	21(1)	1

O1	1283(2)	6518(1)	-149(1)	29(1)	1

O2	6489(2)	8406(1)	298(1)	44(1)	1

O3	1807(2)	6006(1)	4211(1)	28(1)	1

O4	7259(2)	4720(1)	3388(1)	29(1)	1

P1	1667(1)	6654(1)	639(1)	20(1)	1

P2	2025(1)	5925(1)	3407(1)	21(1)	1

S1	416(1)	7384(1)	1076(1)	23(1)	1

S2	1903(1)	5604(1)	1143(1)	26(1)	1

S3	794(1)	5117(1)	3005(1)	21(1)	1

S4	1975(1)	7002(1)	2933(1)	28(1)	1

Cd1	293(1)	6246(1)	2052(1)	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1-O1	1.440(3)

C1-H1A	0.9800

C1-H1B	0.9800

C1-H1C	0.9800

C2-C3	1.386(3)

C2-C7	1.399(3)

C2-P1	1.800(2)

C3-C4	1.393(4)

C3-H3	0.9500

C4-C5	1.387(4)

C4-H4	0.9500

C5-O2	1.378(3)

C5-C6	1.382(4)

C6-C7	1.381(3)

C6-H6	0.9500

C7-H7	0.9500

C8-O2	1.432(4)

C8-H8A	0.9800

C8-H8B	0.9800

C8-H8C	0.9800

C9-O3	1.451(3)

C9-H9A	0.9800

C9-H9B	0.9800

C9-H9C	0.9800

C10-C15	1.384(3)

C10-C11	1.392(3)

C10-P2	1.796(2)

C11-C12	1.374(3)

C11-H11	0.9500

C12-C13	1.392(3)

C12-H12	0.9500

C13-O4	1.364(3)

C13-C14	1.383(3)

C14-C15	1.390(3)

C14-H14	0.9500

C15-H15	0.9500

C16-O4	1.427(3)

C16-H16A	0.9800

C16-H16B	0.9800

C16-H16C	0.9800

C17-N1	1.332(3)

C17-C18	1.383(3)

C17-H17	0.9500

C18-C19	1.384(3)

C18-H18	0.9500

C19-C20	1.387(3)

C19-C22	1.507(3)

C20-C21	1.382(3)

C20-H20	0.9500

C21-N1	1.339(3)

C21-H21	0.9500

C22-C23	1.534(3)

C22-H22A	0.9900

C22-H22B	0.9900

C23-C24	1.529(3)

C23-H23A	0.9900

C23-H23B	0.9900

C24-C25	1.507(3)

C24-H24A	0.9900

C24-H24B	0.9900

C25-C30	1.383(3)

C25-C26	1.390(3)

C26-C27	1.381(3)

C26-H26	0.9500

C27-N2	1.339(3)

C27-H27	0.9500

C29-N2	1.336(3)

C29-C30	1.377(3)

C29-H29	0.9500

C30-H30	0.9500

N1-Cd1	2.3744(18)

N2-Cd1i	2.3623(19)

O1-P1	1.5987(17)

O3-P2	1.6023(18)

P1-S2	1.9902(8)

P1-S1	2.0042(8)

P2-S4	1.9880(9)

P2-S3	2.0067(8)

S1-Cd1	2.6692(6)

S2-Cd1	2.7241(6)

S3-Cd1	2.6632(6)

S4-Cd1	2.7454(6)

Cd1-N2ii	2.3623(19)

O1-C1-H1A	109.5

O1-C1-H1B	109.5

H1A-C1-H1B	109.5

O1-C1-H1C	109.5

H1A-C1-H1C	109.5

H1B-C1-H1C	109.5

C3-C2-C7	118.8(2)

C3-C2-P1	119.47(19)

C7-C2-P1	121.75(18)

C2-C3-C4	121.1(3)

C2-C3-H3	119.4

C4-C3-H3	119.4

C5-C4-C3	119.0(3)

C5-C4-H4	120.5

C3-C4-H4	120.5

O2-C5-C6	115.1(3)

O2-C5-C4	124.4(3)

C6-C5-C4	120.5(2)

C7-C6-C5	120.1(2)

C7-C6-H6	119.9

C5-C6-H6	119.9

C6-C7-C2	120.4(2)

C6-C7-H7	119.8

C2-C7-H7	119.8

O2-C8-H8A	109.5

O2-C8-H8B	109.5

H8A-C8-H8B	109.5

O2-C8-H8C	109.5

H8A-C8-H8C	109.5

H8B-C8-H8C	109.5

O3-C9-H9A	109.5

O3-C9-H9B	109.5

H9A-C9-H9B	109.5

O3-C9-H9C	109.5

H9A-C9-H9C	109.5

H9B-C9-H9C	109.5

C15-C10-C11	118.4(2)

C15-C10-P2	122.35(18)

C11-C10-P2	119.20(18)

C12-C11-C10	121.1(2)

C12-C11-H11	119.4

C10-C11-H11	119.4

C11-C12-C13	119.8(2)

C11-C12-H12	120.1

C13-C12-H12	120.1

O4-C13-C14	124.7(2)

O4-C13-C12	115.4(2)

C14-C13-C12	119.9(2)

C13-C14-C15	119.5(2)

C13-C14-H14	120.2

C15-C14-H14	120.2

C10-C15-C14	121.1(2)

C10-C15-H15	119.5

C14-C15-H15	119.5

O4-C16-H16A	109.5

O4-C16-H16B	109.5

H16A-C16-H16B	109.5

O4-C16-H16C	109.5

H16A-C16-H16C	109.5

H16B-C16-H16C	109.5

N1-C17-C18	123.1(2)

N1-C17-H17	118.4

C18-C17-H17	118.4

C17-C18-C19	119.8(2)

C17-C18-H18	120.1

C19-C18-H18	120.1

C18-C19-C20	117.0(2)

C18-C19-C22	122.1(2)

C20-C19-C22	120.9(2)

C21-C20-C19	119.8(2)

C21-C20-H20	120.1

C19-C20-H20	120.1

N1-C21-C20	122.9(2)

N1-C21-H21	118.6

C20-C21-H21	118.6

C19-C22-C23	111.98(18)

C19-C22-H22A	109.2

C23-C22-H22A	109.2

C19-C22-H22B	109.2

C23-C22-H22B	109.2

H22A-C22-H22B	107.9

C24-C23-C22	110.66(19)

C24-C23-H23A	109.5

C22-C23-H23A	109.5

C24-C23-H23B	109.5

C22-C23-H23B	109.5

H23A-C23-H23B	108.1

C25-C24-C23	114.32(19)

C25-C24-H24A	108.7

C23-C24-H24A	108.7

C25-C24-H24B	108.7

C23-C24-H24B	108.7

H24A-C24-H24B	107.6

C30-C25-C26	116.5(2)

C30-C25-C24	120.7(2)

C26-C25-C24	122.8(2)

C27-C26-C25	119.8(2)

C27-C26-H26	120.1

C25-C26-H26	120.1

N2-C27-C26	123.5(2)

N2-C27-H27	118.3

C26-C27-H27	118.3

N2-C29-C30	123.6(2)

N2-C29-H29	118.2

C30-C29-H29	118.2

C29-C30-C25	120.1(2)

C29-C30-H30	119.9

C25-C30-H30	119.9

C17-N1-C21	117.3(2)

C17-N1-Cd1	118.33(14)

C21-N1-Cd1	122.63(15)

C29-N2-C27	116.4(2)

C29-N2-Cd1i	117.95(15)

C27-N2-Cd1i	125.63(15)

C1-O1-P1	119.74(17)

C5-O2-C8	117.5(3)

C9-O3-P2	118.27(16)

C13-O4-C16	117.27(19)

O1-P1-C2	99.14(10)

O1-P1-S2	112.47(7)

C2-P1-S2	111.16(8)

O1-P1-S1	109.78(7)

C2-P1-S1	111.44(8)

S2-P1-S1	112.16(4)

O3-P2-C10	99.71(10)

O3-P2-S4	112.42(7)

C10-P2-S4	109.76(8)

O3-P2-S3	108.96(7)

C10-P2-S3	112.25(8)

S4-P2-S3	113.01(4)

P1-S1-Cd1	86.54(3)

P1-S2-Cd1	85.31(3)

P2-S3-Cd1	86.26(3)

P2-S4-Cd1	84.39(3)

N2ii-Cd1-N1	84.63(6)

N2ii-Cd1-S3	92.04(5)

N1-Cd1-S3	100.14(5)

N2ii-Cd1-S1	99.02(5)

N1-Cd1-S1	90.18(5)

S3-Cd1-S1	165.557(19)

N2ii-Cd1-S2	94.47(5)

N1-Cd1-S2	165.70(5)

S3-Cd1-S2	94.157(19)

S1-Cd1-S2	75.837(18)

N2ii-Cd1-S4	162.12(5)

N1-Cd1-S4	84.46(5)

S3-Cd1-S4	76.024(19)

S1-Cd1-S4	95.13(2)

S2-Cd1-S4	99.57(2)

Symmetry transformations used to generate equivalent atoms:

(i) -x-1,y+1/2,-z+1/2    (ii) -x-1,y-1/2,-z+1/2

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	35(2) 	61(2)	37(2) 	-9(1)	-10(1) 	-14(2)

C2	19(1) 	20(1)	27(1) 	-1(1)	3(1) 	4(1)

C3	27(1) 	32(1)	33(2) 	4(1)	-1(1) 	-1(1)

C4	23(1) 	33(1)	47(2) 	-1(1)	-8(1) 	2(1)

C5	19(1) 	19(1)	58(2) 	-6(1)	9(1) 	3(1)

C6	28(1) 	22(1)	40(2) 	-1(1)	14(1) 	2(1)

C7	25(1) 	21(1)	28(1) 	-1(1)	6(1) 	6(1)

C8	22(2) 	37(2)	130(4) 	9(2)	-17(2) 	-1(1)

C9	26(1) 	52(2)	30(2) 	-17(1)	5(1) 	8(1)

C10	20(1) 	21(1)	21(1) 	-2(1)	-1(1) 	1(1)

C11	27(1) 	41(2)	18(1) 	4(1)	-2(1) 	4(1)

C12	28(1) 	44(2)	22(1) 	4(1)	7(1) 	5(1)

C13	20(1) 	20(1)	26(1) 	0(1)	1(1) 	0(1)

C14	25(1) 	25(1)	22(1) 	5(1)	-3(1) 	1(1)

C15	24(1) 	29(1)	20(1) 	1(1)	4(1) 	-1(1)

C16	24(1) 	38(2)	48(2) 	18(1)	-3(1) 	6(1)

C17	24(1) 	16(1)	36(2) 	1(1)	6(1) 	1(1)

C18	20(1) 	19(1)	35(1) 	5(1)	10(1) 	2(1)

C19	14(1) 	19(1)	22(1) 	2(1)	0(1) 	3(1)

C20	29(1) 	15(1)	26(1) 	1(1)	5(1) 	2(1)

C21	28(1) 	19(1)	24(1) 	3(1)	6(1) 	0(1)

C22	19(1) 	19(1)	22(1) 	1(1)	2(1) 	2(1)

C23	21(1) 	23(1)	22(1) 	-1(1)	1(1) 	5(1)

C24	21(1) 	20(1)	22(1) 	-1(1)	1(1) 	3(1)

C25	20(1) 	19(1)	16(1) 	0(1)	4(1) 	2(1)

C26	22(1) 	18(1)	30(1) 	0(1)	1(1) 	1(1)

C27	21(1) 	19(1)	29(1) 	0(1)	0(1) 	-3(1)

C29	31(1) 	19(1)	34(2) 	-4(1)	-7(1) 	7(1)

C30	27(1) 	22(1)	28(1) 	-7(1)	-6(1) 	2(1)

N1	17(1) 	19(1)	25(1) 	-1(1)	3(1) 	1(1)

N2	19(1) 	20(1)	23(1) 	0(1)	0(1) 	1(1)

O1	26(1) 	39(1)	22(1) 	-4(1)	-1(1) 	-3(1)

O2	21(1) 	32(1)	79(2) 	-10(1)	11(1) 	-5(1)

O3	23(1) 	40(1)	21(1) 	-9(1)	0(1) 	5(1)

O4	20(1) 	33(1)	35(1) 	8(1)	4(1) 	5(1)

P1	19(1) 	21(1)	21(1) 	0(1)	2(1) 	1(1)

P2	20(1) 	23(1)	19(1) 	-5(1)	-2(1) 	3(1)

S1	21(1) 	21(1)	26(1) 	4(1)	6(1) 	4(1)

S2	28(1) 	19(1)	31(1) 	1(1)	6(1) 	4(1)

S3	23(1) 	20(1)	22(1) 	-1(1)	-2(1) 	0(1)

S4	28(1) 	19(1)	36(1) 	-2(1)	-8(1) 	0(1)

Cd1	16(1) 	18(1)	20(1) 	0(1)	1(1) 	0(1)