|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2007src0607  (JBBI-011-MacHPF6)

Empirical formula 	C13H19F6N2OP

Formula weight 	364.27

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P212121

Unit cell dimensions	a = 11.7560(4) Å	a = 90°

b = 15.6189(3) Å	b = 90°

c = 18.4464(6) Å	g  = 90°

Volume	3387.05(17) Å3

Z	8

Density (calculated)	1.429 Mg / m3

Absorption coefficient	0.225 mm-1

F(000)	1504

Crystal	shard; colourless

Crystal size	0.20 ´ 0.14 ´ 0.02 mm3

q range for data collection	3.10 - 27.12°

Index ranges	-15 £ h £ 14, -18 £ k £ 19, -20 £ l £ 23

Reflections collected	44871

Independent reflections	7443 [Rint = 0.0883]

Completeness to q = 27.12°	99.5 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9955 and 0.9564

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7443 / 0 / 437

Goodness-of-fit on F2	1.011

Final R indices [F2 > 2s(F2)]	R1 = 0.0549, wR2 = 0.1265

R indices (all data)	R1 = 0.1229, wR2 = 0.1542

Absolute structure parameter	-0.12(13)

Largest diff. peak and hole	0.242 and -0.307 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: PLATON  (A.L. Spek, J. Appl. Crystallogr. 2003, 36, 7).

Special details:

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C16	1648(4)	7097(3)	-3865(3)	90(2)	1

C19	-855(3)	7491(2)	-3217(2)	66(1)	1

C1	5397(3)	6072(2)	-2538(2)	51(1)	1

C2	6383(3)	6435(2)	-2104(2)	57(1)	1

C3	6706(4)	7378(3)	-1060(2)	86(1)	1

C4	4749(3)	7072(2)	-1633(2)	56(1)	1

C5	4374(4)	7995(2)	-1571(2)	78(1)	1

C6	4165(3)	6498(3)	-1077(2)	75(1)	1

C7	5643(3)	5919(2)	-3336(2)	65(1)	1

C8	4615(3)	5647(2)	-3779(2)	67(1)	1

C9	4481(4)	5966(3)	-4472(2)	83(1)	1

C10	3579(5)	5732(5)	-4900(3)	109(2)	1

C11	2808(5)	5173(4)	-4639(4)	102(2)	1

C12	2891(4)	4844(3)	-3950(4)	99(2)	1

C13	3820(4)	5079(3)	-3516(3)	82(1)	1

C14	331(3)	6115(2)	-2220(2)	48(1)	1

C15	1316(3)	6414(2)	-2680(2)	56(1)	1

C17	-309(3)	6639(2)	-3392(2)	52(1)	1

C18	-689(4)	6278(3)	-4113(2)	81(1)	1

C20	520(3)	5327(2)	-1754(2)	61(1)	1

C21	-496(3)	5148(2)	-1286(2)	56(1)	1

C22	-1300(4)	4550(2)	-1483(2)	73(1)	1

C23	-2300(4)	4458(3)	-1068(3)	97(2)	1

C24	-2471(5)	4951(3)	-470(3)	99(2)	1

C25	-1658(5)	5537(4)	-260(3)	99(2)	1

C26	-696(4)	5636(3)	-672(2)	78(1)	1

N1	4531(2)	6749(2)	-2395(2)	50(1)	1

N2	5986(2)	6966(2)	-1606(2)	55(1)	1

N3	-567(2)	5997(2)	-2794(2)	48(1)	1

N4	931(2)	6664(2)	-3325(2)	56(1)	1

O1	7392(2)	6245(2)	-2198(2)	83(1)	1

O2	2299(2)	6421(2)	-2452(2)	81(1)	1

F1	4703(3)	7056(2)	1185(2)	126(1)	1

F2	4925(2)	5763(2)	1709(2)	107(1)	1

F3	6109(3)	6839(2)	1986(1)	98(1)	1

F4	6700(2)	5717(2)	1355(2)	109(1)	1

F5	6536(3)	6996(2)	825(2)	142(1)	1

F6	5328(3)	5941(2)	538(2)	116(1)	1

F7	-4722(2)	2987(1)	-1333(2)	94(1)	1

F8	-5328(3)	4130(2)	-695(1)	112(1)	1

F9	-6471(3)	2987(2)	-824(2)	110(1)	1

F10	-6884(3)	4203(2)	-1406(2)	116(1)	1

F11	-6252(2)	3054(2)	-2019(1)	90(1)	1

F12	-5134(3)	4205(2)	-1892(2)	101(1)	1

P1	5701(1)	6401(1)	1254(1)	64(1)	1

P2	-5809(1)	3604(1)	-1349(1)	63(1)	1

Table 3. Bond lengths [Å] and angles [°].

C16-N4	1.469(4)

C19-C17	1.513(4)

C1-N1	1.491(4)

C1-C7	1.518(5)

C1-C2	1.519(5)

C2-O1	1.235(4)

C2-N2	1.324(4)

C3-N2	1.465(5)

C4-N2	1.465(4)

C4-C5	1.512(5)

C4-N1	1.516(5)

C4-C6	1.525(5)

C7-C8	1.519(5)

C8-C13	1.378(6)

C8-C9	1.381(6)

C9-C10	1.372(7)

C10-C11	1.347(8)

C11-C12	1.376(8)

C12-C13	1.403(6)

C14-N3	1.506(4)

C14-C15	1.510(5)

C14-C20	1.517(5)

C15-O2	1.230(4)

C15-N4	1.331(5)

C17-N4	1.464(4)

C17-C18	1.513(5)

C17-N3	1.522(4)

C20-C21	1.500(5)

C21-C22	1.378(5)

C21-C26	1.386(5)

C22-C23	1.411(6)

C23-C24	1.359(7)

C24-C25	1.379(7)

C25-C26	1.371(6)

F1-P1	1.563(3)

F2-P1	1.591(3)

F3-P1	1.588(3)

F4-P1	1.598(3)

F5-P1	1.566(3)

F6-P1	1.566(3)

F7-P2	1.601(2)

F8-P2	1.564(3)

F9-P2	1.573(3)

F10-P2	1.575(3)

F11-P2	1.593(2)

F12-P2	1.585(3)

N1-C1-C7	114.4(3)

N1-C1-C2	99.4(3)

C7-C1-C2	115.1(3)

O1-C2-N2	125.9(3)

O1-C2-C1	124.8(3)

N2-C2-C1	109.3(3)

N2-C4-C5	113.2(3)

N2-C4-N1	99.3(3)

C5-C4-N1	109.8(3)

N2-C4-C6	111.0(3)

C5-C4-C6	112.3(3)

N1-C4-C6	110.6(3)

C1-C7-C8	114.5(3)

C13-C8-C9	118.7(4)

C13-C8-C7	122.0(4)

C9-C8-C7	119.3(4)

C10-C9-C8	121.7(5)

C11-C10-C9	119.1(5)

C10-C11-C12	121.7(5)

C11-C12-C13	119.0(5)

C8-C13-C12	119.7(5)

N3-C14-C15	100.4(3)

N3-C14-C20	113.7(3)

C15-C14-C20	117.2(3)

O2-C15-N4	128.5(3)

O2-C15-C14	122.0(4)

N4-C15-C14	109.5(3)

N4-C17-C18	112.3(3)

N4-C17-C19	112.4(3)

C18-C17-C19	113.0(3)

N4-C17-N3	98.9(3)

C18-C17-N3	109.5(3)

C19-C17-N3	109.8(3)

C21-C20-C14	111.1(3)

C22-C21-C26	118.2(4)

C22-C21-C20	121.4(3)

C26-C21-C20	120.3(4)

C21-C22-C23	119.8(4)

C24-C23-C22	120.3(5)

C23-C24-C25	120.2(5)

C26-C25-C24	119.4(5)

C25-C26-C21	122.1(5)

C1-N1-C4	106.6(2)

C2-N2-C4	113.4(3)

C2-N2-C3	123.3(3)

C4-N2-C3	123.2(3)

C14-N3-C17	106.8(2)

C15-N4-C17	113.9(3)

C15-N4-C16	123.1(3)

C17-N4-C16	121.7(3)

F1-P1-F6	91.21(17)

F1-P1-F5	92.3(2)

F6-P1-F5	91.27(19)

F1-P1-F3	90.79(16)

F6-P1-F3	177.95(17)

F5-P1-F3	89.09(18)

F1-P1-F2	91.28(17)

F6-P1-F2	89.87(17)

F5-P1-F2	176.2(2)

F3-P1-F2	89.64(16)

F1-P1-F4	177.64(19)

F6-P1-F4	89.89(16)

F5-P1-F4	89.7(2)

F3-P1-F4	88.09(15)

F2-P1-F4	86.64(16)

F8-P2-F9	91.46(17)

F8-P2-F10	91.72(17)

F9-P2-F10	90.45(18)

F8-P2-F12	89.77(16)

F9-P2-F12	178.44(17)

F10-P2-F12	90.47(18)

F8-P2-F11	177.83(17)

F9-P2-F11	89.14(15)

F10-P2-F11	90.36(16)

F12-P2-F11	89.59(15)

F8-P2-F7	90.74(16)

F9-P2-F7	90.80(16)

F10-P2-F7	177.21(17)

F12-P2-F7	88.22(15)

F11-P2-F7	87.17(14)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C16	84(3) 	80(3)	104(4) 	21(2)	52(3) 	-3(2)

C19	55(2) 	61(2)	81(3) 	8(2)	-6(2) 	9(2)

C1	45(2) 	50(2)	59(2) 	3(2)	2(2) 	6(2)

C2	42(2) 	62(2)	67(2) 	14(2)	2(2) 	4(2)

C3	74(3) 	106(3)	80(3) 	-6(3)	-19(3) 	-9(2)

C4	41(2) 	75(2)	53(2) 	-1(2)	3(2) 	-1(2)

C5	73(3) 	78(2)	84(3) 	-6(2)	12(2) 	18(2)

C6	62(2) 	102(3)	60(2) 	10(2)	12(2) 	-11(2)

C7	63(2) 	63(2)	70(2) 	-5(2)	10(2) 	6(2)

C8	70(3) 	61(2)	70(3) 	-10(2)	3(2) 	16(2)

C9	90(3) 	93(3)	66(3) 	-7(2)	4(3) 	11(3)

C10	105(4) 	146(5)	76(3) 	-8(3)	-6(3) 	27(4)

C11	105(4) 	101(4)	101(5) 	-31(3)	-41(4) 	25(3)

C12	82(3) 	70(3)	145(5) 	-17(3)	-16(3) 	2(2)

C13	85(3) 	61(2)	99(4) 	-4(2)	-18(3) 	3(2)

C14	32(2) 	64(2)	48(2) 	-4(2)	1(2) 	2(1)

C15	38(2) 	57(2)	73(2) 	-6(2)	12(2) 	1(2)

C17	49(2) 	56(2)	52(2) 	2(2)	4(2) 	1(1)

C18	107(3) 	79(3)	57(2) 	1(2)	-14(2) 	-6(3)

C20	47(2) 	74(2)	62(2) 	5(2)	4(2) 	10(2)

C21	57(2) 	60(2)	51(2) 	11(2)	6(2) 	11(2)

C22	73(3) 	61(2)	86(3) 	2(2)	17(2) 	2(2)

C23	77(3) 	76(3)	137(5) 	18(3)	30(3) 	-10(2)

C24	93(4) 	100(4)	105(4) 	32(3)	47(3) 	15(3)

C25	115(4) 	114(4)	66(3) 	9(3)	33(3) 	17(3)

C26	79(3) 	96(3)	57(2) 	3(2)	4(2) 	11(2)

N1	29(2) 	63(2)	59(2) 	5(1)	6(1) 	0(1)

N2	39(2) 	69(2)	58(2) 	3(2)	-4(2) 	-2(1)

N3	38(2) 	53(2)	54(2) 	-2(1)	-1(1) 	-1(1)

N4	48(2) 	57(2)	63(2) 	1(1)	18(2) 	-2(1)

O1	38(1) 	118(2)	93(2) 	23(2)	6(1) 	22(1)

O2	30(1) 	99(2)	115(2) 	-9(2)	1(1) 	-6(1)

F1	118(2) 	90(2)	170(3) 	-3(2)	-36(2) 	43(2)

F2	106(2) 	98(2)	117(2) 	29(2)	17(2) 	-22(2)

F3	125(2) 	86(2)	81(2) 	-24(1)	-11(2) 	7(2)

F4	100(2) 	111(2)	115(2) 	-24(2)	-10(2) 	38(2)

F5	157(3) 	153(3)	116(2) 	34(2)	27(2) 	-56(2)

F6	170(3) 	105(2)	73(2) 	-16(2)	-34(2) 	5(2)

F7	78(2) 	76(1)	129(2) 	1(2)	-5(2) 	13(1)

F8	151(3) 	110(2)	77(2) 	-30(2)	-32(2) 	-1(2)

F9	127(2) 	112(2)	90(2) 	15(2)	37(2) 	-17(2)

F10	114(2) 	119(2)	116(2) 	-21(2)	-11(2) 	50(2)

F11	89(2) 	101(2)	80(2) 	-36(1)	2(1) 	-13(1)

F12	136(2) 	78(1)	90(2) 	15(1)	9(2) 	-22(2)

P1	78(1) 	56(1)	57(1) 	3(1)	6(1) 	-1(1)

P2	76(1) 	57(1)	56(1) 	-4(1)	1(1) 	2(1)