|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2007src1588    (Motherwell – LJ)

Empirical formula 	C17H21NO4

Formula weight 	303.35

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	C2221

Unit cell dimensions	a = 7.4019(2) Å	 = 90°

b = 15.8155(3) Å	 = 90°

c = 26.8034(4) Å	  = 90°

Volume	3137.73(11) Å3

Z	8

Density (calculated)	1.284 Mg / m3

Absorption coefficient	0.091 mm1

F(000)	1296

Crystal	block; colourless

Crystal size	0.40  0.35  0.20 mm3

 range for data collection	2.99  27.50°

Index ranges	9  h  9, 20  k  20, 34  l  34

Reflections collected	28149

Independent reflections	3609 [Rint = 0.0493]

Completeness to  = 27.50°	99.2 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9820 and 0.9644

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3609 / 0 / 201

Goodness-of-fit on F2	1.039

Final R indices [F2 > 2(F2)]	R1 = 0.0339, wR2 = 0.0763

R indices (all data)	R1 = 0.0375, wR2 = 0.0784

Absolute structure parameter	0.2(7)

Largest diff. peak and hole	0.146 and 0.153 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: PLATON  (A.L. Spek, J. Appl. Crystallogr. 2003, 36, 7).

Special details:

C3 = S, C7 = R, C9 = R.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	681(2)	3000(1)	24(1)	24(1)	1

C2	787(2)	4089(1)	412(1)	28(1)	1

C3	224(2)	3592(1)	815(1)	20(1)	1

C4	1851(2)	4046(1)	1051(1)	21(1)	1

C5	3255(2)	4312(1)	663(1)	29(1)	1

C6	1222(2)	4802(1)	1364(1)	33(1)	1

C7	1542(2)	2112(1)	737(1)	20(1)	1

C8	756(2)	1269(1)	606(1)	26(1)	1

C9	416(2)	1644(1)	1116(1)	22(1)	1

C10	1299(2)	1270(1)	1566(1)	28(1)	1

C11	2312(2)	1736(1)	2358(1)	28(1)	1

C12	2745(2)	2479(1)	2677(1)	22(1)	1

C13	2439(2)	3304(1)	2516(1)	23(1)	1

C14	2882(2)	3978(1)	2825(1)	28(1)	1

C15	3620(2)	3821(1)	3293(1)	30(1)	1

C16	3917(2)	3001(1)	3456(1)	27(1)	1

C17	3483(2)	2326(1)	3148(1)	25(1)	1

N1	745(2)	2851(1)	522(1)	20(1)	1

O1	1191(1)	2552(1)	315(1)	33(1)	1

O2	88(1)	3774(1)	59(1)	29(1)	1

O3	1699(1)	1960(1)	1905(1)	25(1)	1

O4	2486(2)	1013(1)	2487(1)	58(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1	1.2120(16)

C1N1	1.3548(16)

C1O2	1.3675(16)

C2O2	1.4527(16)

C2C3	1.5312(17)

C3N1	1.4632(14)

C3C4	1.5380(16)

C4C5	1.5286(18)

C4C6	1.5332(17)

C7N1	1.4313(15)

C7C8	1.4969(16)

C7C9	1.5074(16)

C8C9	1.5099(16)

C9C10	1.4943(18)

C10O3	1.4506(15)

C11O4	1.2026(15)

C11O3	1.3429(15)

C11C12	1.4876(17)

C12C13	1.3923(16)

C12C17	1.3972(17)

C13C14	1.3904(18)

C14C15	1.3894(18)

C15C16	1.387(2)

C16C17	1.3874(19)

O1C1N1	128.68(13)

O1C1O2	122.05(12)

N1C1O2	109.28(11)

O2C2C3	105.24(10)

N1C3C2	99.23(9)

N1C3C4	112.86(10)

C2C3C4	115.61(10)

C5C4C6	111.36(11)

C5C4C3	112.43(10)

C6C4C3	110.56(11)

N1C7C8	118.17(10)

N1C7C9	116.45(10)

C8C7C9	60.34(8)

C7C8C9	60.18(8)

C10C9C7	119.71(12)

C10C9C8	120.16(11)

C7C9C8	59.48(8)

O3C10C9	107.32(10)

O4C11O3	123.20(13)

O4C11C12	124.22(12)

O3C11C12	112.57(10)

C13C12C17	120.43(12)

C13C12C11	121.74(11)

C17C12C11	117.83(11)

C14C13C12	119.67(12)

C15C14C13	119.60(13)

C16C15C14	120.94(13)

C15C16C17	119.67(12)

C16C17C12	119.69(12)

C1N1C7	123.68(10)

C1N1C3	112.39(10)

C7N1C3	123.00(9)

C1O2C2	108.30(9)

C11O3C10	115.87(10)

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	26(1) 	23(1)	24(1) 	2(1)	4(1) 	4(1)

C2	29(1) 	25(1)	29(1) 	2(1)	4(1) 	3(1)

C3	23(1) 	16(1)	23(1) 	1(1)	2(1) 	1(1)

C4	28(1) 	19(1)	18(1) 	1(1)	1(1) 	3(1)

C5	31(1) 	30(1)	25(1) 	4(1)	2(1) 	10(1)

C6	43(1) 	24(1)	32(1) 	9(1)	2(1) 	1(1)

C7	21(1) 	17(1)	22(1) 	1(1)	1(1) 	2(1)

C8	34(1) 	19(1)	25(1) 	4(1)	2(1) 	4(1)

C9	24(1) 	19(1)	23(1) 	1(1)	3(1) 	3(1)

C10	39(1) 	18(1)	26(1) 	1(1)	1(1) 	1(1)

C11	36(1) 	22(1)	26(1) 	4(1)	2(1) 	1(1)

C12	21(1) 	22(1)	21(1) 	3(1)	3(1) 	1(1)

C13	25(1) 	25(1)	21(1) 	3(1)	2(1) 	1(1)

C14	36(1) 	22(1)	27(1) 	2(1)	1(1) 	1(1)

C15	31(1) 	34(1)	24(1) 	4(1)	1(1) 	3(1)

C16	23(1) 	38(1)	19(1) 	2(1)	0(1) 	2(1)

C17	23(1) 	28(1)	24(1) 	7(1)	4(1) 	0(1)

N1	26(1) 	16(1)	19(1) 	2(1)	0(1) 	1(1)

O1	46(1) 	34(1)	21(1) 	6(1)	1(1) 	1(1)

O2	36(1) 	26(1)	24(1) 	1(1)	7(1) 	1(1)

O3	34(1) 	19(1)	22(1) 	1(1)	2(1) 	1(1)

O4	112(1) 	20(1)	43(1) 	7(1)	30(1) 	1(1)