|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	04mbh0608

Empirical formula 	C10H28N2O9

Formula weight 	320.34

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P1

Unit cell dimensions	a = 6.1179(14) Å	 = 90.92(3)°

b = 8.672(2) Å	 = 91.41(3)°

c = 15.182(8) Å	  = 99.79(2)°

Volume	793.3(5) Å3

Z	2

Density (calculated)	1.341 Mg / m3

Absorption coefficient	0.117 mm1

F(000)	348

Crystal	lath; colourless

Crystal size	0.70  0.20  0.10 mm3

 range for data collection	3.38  27.48°

Index ranges	7  h  7, 11  k  11, 19  l  19

Reflections collected	12962

Independent reflections	3575 [Rint = 0.0349]

Completeness to  = 27.48°	98.6 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9884 and 0.9226

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3575 / 9 / 222

Goodness-of-fit on F2	1.032

Final R indices [F2 > 2(F2)]	R1 = 0.0436, wR2 = 0.1017

R indices (all data)	R1 = 0.0635, wR2 = 0.1122

Largest diff. peak and hole	0.262 and 0.375 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	6475(3)	191(2)	6542(1)	28(1)	1

C2	5684(2)	1762(2)	6614(1)	18(1)	1

C3	3745(2)	1629(2)	7237(1)	18(1)	1

C4	2891(2)	3176(2)	7327(1)	16(1)	1

O1A	6183(2)	537(2)	5824(1)	45(1)	1

O1B	7404(2)	281(1)	7210(1)	38(1)	1

O2	5067(2)	2271(1)	5779(1)	24(1)	1

O3	2052(2)	415(1)	6934(1)	24(1)	1

O4A	957(2)	3222(1)	7105(1)	25(1)	1

O4B	4271(2)	4329(1)	7662(1)	19(1)	1

C21	144(3)	7844(2)	5230(1)	28(1)	1

C23	835(2)	6859(2)	6686(1)	18(1)	1

C24	57(2)	6582(2)	7600(1)	20(1)	1

C26	796(3)	5505(2)	9018(1)	27(1)	1

C27	2768(3)	5962(2)	5904(1)	29(1)	1

C28	3272(3)	7791(2)	8487(1)	28(1)	1

N22	893(2)	7279(1)	6067(1)	19(1)	1

N25	1750(2)	6323(1)	8227(1)	18(1)	1

O1W	8204(2)	838(2)	8916(1)	40(1)	1

O2W	5882(2)	3231(2)	9245(1)	34(1)	1

O3W	2057(2)	8297(2)	10041(1)	40(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1A	1.244(2)

C1O1B	1.259(2)

C1C2	1.525(2)

C2O2	1.413(2)

C2C3	1.525(2)

C2H2	1.0000

C3O3	1.4082(18)

C3C4	1.526(2)

C3H3	1.0000

C4O4A	1.2293(18)

C4O4B	1.2831(18)

O2H2O	0.8400

O3H3O	0.8400

C21N22	1.486(2)

C21H21A	0.9800

C21H21B	0.9800

C21H21C	0.9800

C23N22	1.4924(19)

C23C24	1.511(2)

C23H23A	0.9900

C23H23B	0.9900

C24N25	1.490(2)

C24H24A	0.9900

C24H24B	0.9900

C26N25	1.486(2)

C26H26A	0.9800

C26H26B	0.9800

C26H26C	0.9800

C27N22	1.487(2)

C27H27A	0.9800

C27H27B	0.9800

C27H27C	0.9800

C28N25	1.485(2)

C28H28A	0.9800

C28H28B	0.9800

C28H28C	0.9800

N22H22	0.9300

N25H25	0.9300

O1WH1W	0.871(17)

O1WH2W	0.845(16)

O2WH21W	0.850(16)

O2WH22W	0.855(16)

O3WH31W	0.854(16)

O3WH32W	0.863(16)

O1AC1O1B	124.07(16)

O1AC1C2	118.02(17)

O1BC1C2	117.90(16)

O2C2C1	111.28(13)

O2C2C3	110.59(12)

C1C2C3	109.59(12)

O2C2H2	108.4

C1C2H2	108.4

C3C2H2	108.4

O3C3C2	109.24(12)

O3C3C4	111.29(12)

C2C3C4	111.45(12)

O3C3H3	108.2

C2C3H3	108.2

C4C3H3	108.2

O4AC4O4B	125.14(14)

O4AC4C3	118.92(13)

O4BC4C3	115.91(12)

C2O2H2O	109.5

C3O3H3O	109.5

N22C21H21A	109.5

N22C21H21B	109.5

H21AC21H21B	109.5

N22C21H21C	109.5

H21AC21H21C	109.5

H21BC21H21C	109.5

N22C23C24	111.10(12)

N22C23H23A	109.4

C24C23H23A	109.4

N22C23H23B	109.4

C24C23H23B	109.4

H23AC23H23B	108.0

N25C24C23	110.25(12)

N25C24H24A	109.6

C23C24H24A	109.6

N25C24H24B	109.6

C23C24H24B	109.6

H24AC24H24B	108.1

N25C26H26A	109.5

N25C26H26B	109.5

H26AC26H26B	109.5

N25C26H26C	109.5

H26AC26H26C	109.5

H26BC26H26C	109.5

N22C27H27A	109.5

N22C27H27B	109.5

H27AC27H27B	109.5

N22C27H27C	109.5

H27AC27H27C	109.5

H27BC27H27C	109.5

N25C28H28A	109.5

N25C28H28B	109.5

H28AC28H28B	109.5

N25C28H28C	109.5

H28AC28H28C	109.5

H28BC28H28C	109.5

C21N22C27	111.43(13)

C21N22C23	109.67(12)

C27N22C23	112.39(12)

C21N22H22	107.7

C27N22H22	107.7

C23N22H22	107.7

C28N25C26	110.56(13)

C28N25C24	113.00(13)

C26N25C24	110.22(12)

C28N25H25	107.6

C26N25H25	107.6

C24N25H25	107.6

H1WO1WH2W	103(2)

H21WO2WH22W	103.8(19)

H31WO3WH32W	103(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	16(1) 	17(1)	52(1) 	8(1)	15(1) 	5(1)

C2	14(1) 	15(1)	26(1) 	3(1)	2(1) 	4(1)

C3	15(1) 	14(1)	24(1) 	2(1)	0(1) 	2(1)

C4	16(1) 	16(1)	18(1) 	2(1)	2(1) 	3(1)

O1A	59(1) 	22(1)	58(1) 	6(1)	28(1) 	13(1)

O1B	22(1) 	24(1)	70(1) 	18(1)	4(1) 	10(1)

O2	31(1) 	17(1)	24(1) 	1(1)	5(1) 	7(1)

O3	14(1) 	14(1)	43(1) 	3(1)	2(1) 	1(1)

O4A	17(1) 	19(1)	40(1) 	2(1)	3(1) 	6(1)

O4B	20(1) 	15(1)	23(1) 	1(1)	0(1) 	2(1)

C21	25(1) 	31(1)	28(1) 	13(1)	2(1) 	5(1)

C23	17(1) 	17(1)	21(1) 	2(1)	2(1) 	7(1)

C24	19(1) 	20(1)	23(1) 	1(1)	4(1) 	6(1)

C26	29(1) 	32(1)	20(1) 	6(1)	7(1) 	0(1)

C27	24(1) 	26(1)	34(1) 	9(1)	6(1) 	4(1)

C28	32(1) 	20(1)	28(1) 	3(1)	1(1) 	3(1)

N22	18(1) 	14(1)	26(1) 	6(1)	3(1) 	5(1)

N25	20(1) 	16(1)	18(1) 	0(1)	3(1) 	2(1)

O1W	31(1) 	44(1)	46(1) 	20(1)	8(1) 	7(1)

O2W	28(1) 	42(1)	29(1) 	9(1)	7(1) 	2(1)

O3W	32(1) 	37(1)	47(1) 	16(1)	7(1) 	2(1)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O2H2O...O1A	0.84	2.16	2.6402(18)	116.0

O3H3O...O4A	0.84	2.18	2.6427(16)	114.3

N25H25...O4B	0.93	1.74	2.6514(18)	167.1

N25H25...O4A	0.93	2.50	3.120(2)	124.1

O1WH1W...O1B	0.871(17)	1.888(17)	2.753(3)	172(3)

O1WH2W...O2W	0.845(16)	1.910(17)	2.753(2)	176(3)

O2WH22W...O4B	0.855(16)	1.966(16)	2.816(2)	172(2)

O2H2O...O1Ai	0.84	2.10	2.858(2)	150.6

O3H3O...O1Bii	0.84	2.15	2.8475(17)	140.5

N22H22...O1Biii	0.93	2.14	3.049(2)	165.8

N22H22...O1Aiii	0.93	2.14	2.840(2)	130.7

O3WH31W...O1Wiii	0.854(16)	1.944(17)	2.795(2)	174(3)

O2WH21W...O3Wiv	0.850(16)	1.895(16)	2.743(2)	175(2)

O3WH32W...O1Wv	0.863(16)	1.937(17)	2.794(2)	172(3)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z+1    (ii) x1,y,z    (iii) x1,y+1,z    (iv)  x,y+1,z+2

(v) x+1,y+1,z+2