|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	04skc0001c2c

Empirical formula 	C7H10N2O6

Formula weight 	218.17

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 25.065(5) Å	 = 90°

b = 4.9767(10) Å	 = 129.42(3)°

c = 19.142(4) Å	  = 90°

Volume	1844.7(6) Å3

Z	8

Density (calculated)	1.571 Mg / m3

Absorption coefficient	0.139 mm1

F(000)	912

Crystal	block; colourless

Crystal size	0.09  0.08  0.06 mm3

 range for data collection	4.21  27.48°

Index ranges	32  h  30, 5  k  6, 21  l  24

Reflections collected	6173

Independent reflections	2017 [Rint = 0.1934]

Completeness to  = 27.48°	94.6 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9917 and 0.9876

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2017 / 52 / 163

Goodness-of-fit on F2	1.030

Final R indices [F2 > 2(F2)]	R1 = 0.0993, wR2 = 0.1418

R indices (all data)	R1 = 0.2794, wR2 = 0.1972

Extinction coefficient	0.0028(9)

Largest diff. peak and hole	0.288 and 0.344 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	749(3)	634(11)	1412(4)	31(1)	1

C2	1122(3)	506(10)	2358(4)	31(2)	1

C3	1902(3)	409(11)	2886(4)	32(2)	1

C4	2268(3)	1955(11)	3761(4)	33(2)	1

O1A	324(2)	1006(7)	766(2)	36(1)	1

O1B	861(2)	2930(7)	1314(2)	35(1)	1

O2	908(2)	3151(7)	2358(3)	36(1)	1

O3	2069(2)	1557(7)	2363(3)	37(1)	1

O4A	2604(2)	3956(7)	3889(2)	39(1)	1

O4B	2187(2)	986(7)	4314(2)	37(1)	1

C25B	1054(8)	5700(40)	4006(10)	30(3)	0.519(11)

C24B	721(6)	4260(30)	4195(12)	33(3)	0.519(11)

N23B	904(6)	5110(20)	4991(9)	34(4)	0.519(11)

C22B	1350(7)	7090(30)	5300(9)	28(3)	0.519(11)

N21B	1456(9)	7510(40)	4709(11)	30(3)	0.519(11)

C25A	1272(11)	6180(50)	4151(13)	30(3)	0.481(11)

C24A	750(8)	4540(30)	3854(11)	33(3)	0.481(11)

N23A	628(8)	4560(30)	4451(12)	36(5)	0.481(11)

C22A	1078(11)	6160(30)	5117(12)	28(3)	0.481(11)

N21A	1460(10)	7300(40)	4942(13)	30(3)	0.481(11)

Table 3. Bond lengths [Å] and angles [°].

C1O1B	1.219(6)

C1O1A	1.287(6)

C1C2	1.525(7)

C2O2	1.422(5)

C2C3	1.529(7)

C2H2	1.0000

C3O3	1.426(6)

C3C4	1.513(8)

C3H3	1.0000

C4O4A	1.225(6)

C4O4B	1.291(7)

O1AH1	0.8400

O2H2O	0.8400

O3H3O	0.8400

O4BH4	0.8400

C25BC24B	1.314(15)

C25BN21B	1.383(13)

C25BH25B	0.9500

C24BN23B	1.352(16)

C24BH24B	0.9500

N23BC22B	1.315(14)

N23BH23B	0.8800

C22BN21B	1.331(14)

C22BH22B	0.9500

N21BH21B	0.8800

C25AC24A	1.325(14)

C25AN21A	1.386(14)

C25AH25A	0.9500

C24AN23A	1.357(15)

C24AH24A	0.9500

N23AC22A	1.309(16)

N23AH23A	0.8800

C22AN21A	1.325(15)

C22AH22A	0.9500

N21AH21A	0.8800

O1BC1O1A	125.3(5)

O1BC1C2	120.2(5)

O1AC1C2	114.4(5)

O2C2C1	113.4(4)

O2C2C3	110.7(4)

C1C2C3	109.6(5)

O2C2H2	107.6

C1C2H2	107.6

C3C2H2	107.6

O3C3C4	109.4(4)

O3C3C2	110.2(5)

C4C3C2	109.7(5)

O3C3H3	109.2

C4C3H3	109.2

C2C3H3	109.2

O4AC4O4B	125.9(5)

O4AC4C3	119.4(6)

O4BC4C3	114.7(5)

C1O1AH1	109.5

C2O2H2O	109.5

C3O3H3O	109.5

C4O4BH4	109.5

C24BC25BN21B	106.7(11)

C24BC25BH25B	126.6

N21BC25BH25B	126.6

C25BC24BN23B	108.4(11)

C25BC24BH24B	125.8

N23BC24BH24B	125.8

C22BN23BC24B	109.0(12)

C22BN23BH23B	125.5

C24BN23BH23B	125.5

N23BC22BN21B	108.0(13)

N23BC22BH22B	126.0

N21BC22BH22B	126.0

C22BN21BC25B	107.9(12)

C22BN21BH21B	126.1

C25BN21BH21B	126.1

C24AC25AN21A	105.9(13)

C24AC25AH25A	127.0

N21AC25AH25A	127.0

C25AC24AN23A	108.8(14)

C25AC24AH24A	125.6

N23AC24AH24A	125.6

C22AN23AC24A	108.1(13)

C22AN23AH23A	125.9

C24AN23AH23A	125.9

N23AC22AN21A	109.0(12)

N23AC22AH22A	125.5

N21AC22AH22A	125.5

C22AN21AC25A	107.9(12)

C22AN21AH21A	126.1

C25AN21AH21A	126.1

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	31(4) 	36(3)	37(4) 	6(3)	26(3) 	1(3)

C2	28(4) 	32(3)	32(4) 	2(3)	19(3) 	3(3)

C3	30(4) 	38(3)	36(4) 	2(3)	25(3) 	1(3)

C4	27(4) 	40(3)	25(4) 	4(3)	14(3) 	2(3)

O1A	39(3) 	37(2)	36(3) 	4(2)	25(2) 	7(2)

O1B	42(3) 	30(2)	32(2) 	2(2)	23(2) 	5(2)

O2	44(3) 	41(2)	30(3) 	3(2)	26(2) 	7(2)

O3	43(3) 	45(2)	39(3) 	9(2)	33(2) 	11(2)

O4A	40(3) 	46(2)	35(3) 	7(2)	26(2) 	15(2)

O4B	36(3) 	51(2)	26(2) 	2(2)	21(2) 	4(2)

C25B	13(11) 	51(8)	26(6) 	7(4)	12(7) 	17(6)

C24B	26(5) 	49(6)	42(10) 	7(7)	31(6) 	12(4)

N23B	34(9) 	42(8)	34(8) 	0(7)	26(8) 	14(6)

C22B	32(10) 	34(9)	28(6) 	2(5)	24(7) 	1(5)

N21B	32(3) 	35(4)	32(8) 	0(5)	24(5) 	8(3)

C25A	13(11) 	51(8)	26(6) 	7(4)	12(7) 	17(6)

C24A	26(5) 	49(6)	42(10) 	7(7)	31(6) 	12(4)

N23A	35(9) 	34(7)	46(12) 	2(8)	29(9) 	4(6)

C22A	32(10) 	34(9)	28(6) 	2(5)	24(7) 	1(5)

N21A	32(3) 	35(4)	32(8) 	0(5)	24(5) 	8(3)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O3H3O...O4A	0.84	2.10	2.605(5)	118.5

O2H2O...O1Bi	0.84	1.92	2.741(5)	164.6

N21AH21A...O4Bi	0.88	2.88	3.304(15)	111.7

O3H3O...O3ii	0.84	2.37	3.114(5)	148.2

O4BH4...O4Biii	0.84	1.72	2.528(7)	160.5

O4BH4...O4Aiii	0.84	2.61	3.133(5)	121.9

N23BH23B...O1Biv	0.88	2.00	2.819(13)	154.0

N21BH21B...O4Av	0.88	2.31	2.796(15)	114.8

N21AH21A...O4Av	0.88	1.84	2.706(16)	168.2

N23AH23A...O1Avi	0.88	1.92	2.781(13)	167.3

O1AH1...O1Avii	0.84	1.69	2.490(7)	157.9

Symmetry transformations used to generate equivalent atoms:

(i) x,y+1,z    (ii) x+1/2,y+1/2,z+1/2    (iii) x+1/2,y+1/2,z+1

(iv)  x,y,z+1/2    (v) x+1/2,y+3/2,z+1    (vi) x,y,z+1/2

(vii) x,y,z