|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0013

Empirical formula 	C12H20N2O4

Formula weight 	256.30

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 8.8691(7) Å	 = 90°

b = 13.2988(17) Å	 = 109.500(7)°

c = 12.1250(14) Å	  = 90°

Volume	1348.1(3) Å3

Z	4

Density (calculated)	1.263 Mg / m3

Absorption coefficient	0.095 mm1

F(000)	552

Crystal	shard; colourless

Crystal size	0.10  0.07  0.01 mm3

 range for data collection	2.93  27.48°

Index ranges	11  h  11, 17  k  17, 15  l  15

Reflections collected	17980

Independent reflections	3079 [Rint = 0.1667]

Completeness to  = 27.48°	99.5 %

Max. and min. transmission	0.9991 and 0.9906

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3079 / 0 / 168

Goodness-of-fit on F2	1.094

Final R indices [F2 > 2(F2)]	R1 = 0.1082, wR2 = 0.1252

R indices (all data)	R1 = 0.2045, wR2 = 0.1494

Largest diff. peak and hole	0.296 and 0.260 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	643(4)	987(3)	2304(3)	20(1)	1

C2	622(4)	1297(3)	1182(3)	25(1)	1

C3	1684(4)	437(3)	544(3)	24(1)	1

C4	2975(4)	769(3)	580(3)	25(1)	1

C5	4023(4)	95(3)	1231(3)	23(1)	1

C6	5480(4)	237(3)	2257(3)	22(1)	1

C7	5060(4)	740(3)	3248(3)	21(1)	1

C8	6502(4)	1069(3)	4268(3)	20(1)	1

O1A	1420(3)	1769(2)	2917(2)	27(1)	1

O1B	940(3)	128(2)	2607(2)	32(1)	1

O8A	6254(3)	1282(2)	5220(2)	23(1)	1

O8B	7824(3)	1125(2)	4133(2)	30(1)	1

C22	11964(4)	1209(3)	4824(3)	21(1)	1

C24	13193(4)	2233(3)	6275(3)	21(1)	1

C25	11638(4)	2199(3)	6169(3)	23(1)	1

C26	14565(4)	2785(3)	7119(3)	29(1)	1

N21	10887(4)	1556(2)	5261(2)	24(1)	1

N23	13380(3)	1604(2)	5422(2)	21(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1B	1.202(4)

C1O1A	1.328(4)

C1C2	1.503(5)

C2C3	1.518(5)

C2H2A	0.9900

C2H2B	0.9900

C3C4	1.523(4)

C3H3B	0.9900

C3H3A	0.9900

C4C5	1.522(5)

C4H4A	0.9900

C4H4B	0.9900

C5C6	1.529(4)

C5H5B	0.9900

C5H5A	0.9900

C6C7	1.526(5)

C6H6B	0.9900

C6H6A	0.9900

C7C8	1.517(4)

C7H7B	0.9900

C7H7A	0.9900

C8O8B	1.239(4)

C8O8A	1.276(4)

O1AH1	0.8400

C22N21	1.320(4)

C22N23	1.331(4)

C22H22	0.9500

C24C25	1.343(5)

C24N23	1.382(4)

C24C26	1.495(5)

C25N21	1.378(4)

C25H25	0.9500

C26H26A	0.9800

C26H26B	0.9800

C26H26C	0.9800

N21H21	0.8800

N23H23	0.8800

O1BC1O1A	123.5(3)

O1BC1C2	123.9(3)

O1AC1C2	112.5(3)

C1C2C3	113.8(3)

C1C2H2A	108.8

C3C2H2A	108.8

C1C2H2B	108.8

C3C2H2B	108.8

H2AC2H2B	107.7

C2C3C4	113.0(3)

C2C3H3B	109.0

C4C3H3B	109.0

C2C3H3A	109.0

C4C3H3A	109.0

H3BC3H3A	107.8

C5C4C3	113.0(3)

C5C4H4A	109.0

C3C4H4A	109.0

C5C4H4B	109.0

C3C4H4B	109.0

H4AC4H4B	107.8

C4C5C6	114.1(3)

C4C5H5B	108.7

C6C5H5B	108.7

C4C5H5A	108.7

C6C5H5A	108.7

H5BC5H5A	107.6

C7C6C5	113.9(3)

C7C6H6B	108.8

C5C6H6B	108.8

C7C6H6A	108.8

C5C6H6A	108.8

H6BC6H6A	107.7

C8C7C6	114.1(3)

C8C7H7B	108.7

C6C7H7B	108.7

C8C7H7A	108.7

C6C7H7A	108.7

H7BC7H7A	107.6

O8BC8O8A	124.2(3)

O8BC8C7	119.1(3)

O8AC8C7	116.6(3)

C1O1AH1	109.5

N21C22N23	108.7(3)

N21C22H22	125.6

N23C22H22	125.6

C25C24N23	106.5(3)

C25C24C26	131.1(3)

N23C24C26	122.4(3)

C24C25N21	107.7(3)

C24C25H25	126.1

N21C25H25	126.1

C24C26H26A	109.5

C24C26H26B	109.5

H26AC26H26B	109.5

C24C26H26C	109.5

H26AC26H26C	109.5

H26BC26H26C	109.5

C22N21C25	108.4(3)

C22N21H21	125.8

C25N21H21	125.8

C22N23C24	108.6(3)

C22N23H23	125.7

C24N23H23	125.7

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	18(2) 	25(2)	18(2) 	1(2)	6(2) 	2(2)

C2	27(2) 	24(2)	20(2) 	5(2)	4(2) 	4(2)

C3	25(2) 	28(2)	17(2) 	2(2)	5(2) 	1(2)

C4	25(2) 	25(2)	20(2) 	2(2)	1(2) 	2(2)

C5	24(2) 	26(2)	19(2) 	2(2)	7(2) 	1(2)

C6	22(2) 	26(2)	17(2) 	3(2)	5(2) 	2(2)

C7	17(2) 	23(2)	21(2) 	2(2)	3(2) 	1(2)

C8	20(2) 	21(2)	19(2) 	2(2)	6(2) 	2(2)

O1A	24(2) 	24(2)	24(2) 	2(1)	3(1) 	0(1)

O1B	34(2) 	23(2)	28(2) 	6(1)	5(1) 	0(1)

O8A	18(1) 	34(2)	16(1) 	1(1)	4(1) 	0(1)

O8B	16(1) 	49(2)	26(2) 	7(1)	7(1) 	8(1)

C22	22(2) 	22(2)	15(2) 	3(2)	0(2) 	0(2)

C24	20(2) 	24(2)	17(2) 	0(2)	3(2) 	0(2)

C25	24(2) 	25(2)	21(2) 	5(2)	9(2) 	0(2)

C26	25(2) 	31(2)	27(2) 	7(2)	3(2) 	2(2)

N21	17(2) 	31(2)	23(2) 	1(2)	5(1) 	1(1)

N23	17(2) 	27(2)	20(2) 	1(1)	6(1) 	1(1)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N21H21...O8B	0.88	1.80	2.664(4)	164.8

O1AH1...O8Ai	0.84	1.75	2.582(3)	170.8

N23H23...O8Aii	0.88	1.80	2.676(4)	173.0

Symmetry transformations used to generate equivalent atoms:

(i) x1,y,z1    (ii) x+1,y,z