|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 2. Crystal data and structure refinement details.

Identification code 	s92

Empirical formula 	C20H28N2O6

Formula weight 	392.44

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 5.5528(6) Å	 = 90°

b = 16.0180(18) Å	 = 103.378(9)°

c = 11.7768(19) Å	  = 90°

Volume	1019.1(2) Å3

Z	2

Density (calculated)	1.279 Mg / m3

Absorption coefficient	0.095 mm1

F(000)	420

Crystal	plate; colourless

Crystal size	0.50  0.15  0.02 mm3

 range for data collection	3.99  27.48°

Index ranges	5  h  6, 19  k  19, 14  l  15

Reflections collected	7917

Independent reflections	2248 [Rint = 0.0499]

Completeness to  = 25.00°	99.5 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9981 and 0.9543

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2248 / 1 / 256

Goodness-of-fit on F2	1.048

Final R indices [F2 > 2(F2)]	R1 = 0.0398, wR2 = 0.0860

R indices (all data)	R1 = 0.0520, wR2 = 0.0922

Absolute structure parameter	10(10)

Extinction coefficient	0.042(5)

Largest diff. peak and hole	0.213 and 0.280 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 3. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	4356(5)	1824(2)	86(2)	22(1)	1

C2	2905(5)	1032(2)	205(2)	21(1)	1

C3	3130(5)	834(2)	1495(2)	21(1)	1

C4	1924(5)	5(2)	1626(2)	23(1)	1

O1A	3231(4)	2436(1)	461(2)	31(1)	1

O1B	6628(4)	1808(1)	559(2)	30(1)	1

O2	407(4)	1058(1)	408(2)	26(1)	1

O3	1964(4)	1483(1)	2003(2)	26(1)	1

O4A	104(4)	1(1)	2082(2)	35(1)	1

O4B	2827(4)	646(1)	1253(2)	27(1)	1

C11	352(5)	1106(2)	7733(2)	21(1)	1

C12	593(5)	258(2)	7547(2)	24(1)	1

C13	1964(5)	24(2)	6768(3)	27(1)	1

C14	3091(5)	540(2)	6173(2)	30(1)	1

C15	2878(5)	1387(2)	6356(3)	31(1)	1

C16	1524(5)	1670(2)	7136(2)	26(1)	1

C17	1180(5)	1440(2)	8545(2)	22(1)	1

C18	2777(5)	799(2)	8984(2)	24(1)	1

N19	482(4)	1834(1)	9600(2)	22(1)	1

C21	3842(5)	2695(2)	6317(2)	22(1)	1

C22	3136(6)	2269(2)	5262(3)	29(1)	1

C23	4582(6)	1629(2)	4982(3)	31(1)	1

C24	6750(6)	1407(2)	5763(3)	30(1)	1

C25	7462(5)	1812(2)	6812(3)	30(1)	1

C26	6013(5)	2458(2)	7093(3)	27(1)	1

C27	2266(5)	3422(2)	6530(2)	22(1)	1

C28	2770(6)	4208(2)	5891(3)	28(1)	1

N29	2686(4)	3631(1)	7792(2)	22(1)	1

Table 4. Bond lengths [Å] and angles [°].

C1O1B	1.256(3)

C1O1A	1.257(3)

C1C2	1.526(4)

C2O2	1.409(3)

C2C3	1.529(4)

C2H2	1.0000

C3O3	1.428(3)

C3C4	1.524(4)

C3H3	1.0000

C4O4A	1.250(3)

C4O4B	1.266(3)

O2H2O	0.8400

O3H3O	0.8400

C11C12	1.387(4)

C11C16	1.394(4)

C11C17	1.517(4)

C12C13	1.396(4)

C12H12	0.9500

C13C14	1.379(4)

C13H13	0.9500

C14C15	1.383(4)

C14H14	0.9500

C15C16	1.391(4)

C15H15	0.9500

C16H16	0.9500

C17N19	1.504(3)

C17C18	1.522(4)

C17H17	1.0000

C18H18A	0.9800

C18H18B	0.9800

C18H18C	0.9800

N19H19A	0.9100

N19H19B	0.9100

N19H19C	0.9100

C21C26	1.386(4)

C21C22	1.391(4)

C21C27	1.512(4)

C22C23	1.389(4)

C22H22	0.9500

C23C24	1.381(4)

C23H23	0.9500

C24C25	1.370(4)

C24H24	0.9500

C25C26	1.397(4)

C25H25	0.9500

C26H26	0.9500

C27N29	1.489(4)

C27C28	1.525(4)

C27H27	1.0000

C28H28A	0.9800

C28H28B	0.9800

C28H28C	0.9800

N29H29A	0.9100

N29H29B	0.9100

N29H29C	0.9100

O1BC1O1A	124.9(3)

O1BC1C2	116.1(2)

O1AC1C2	119.0(2)

O2C2C1	114.0(2)

O2C2C3	111.1(2)

C1C2C3	109.9(2)

O2C2H2	107.2

C1C2H2	107.2

C3C2H2	107.2

O3C3C4	110.3(2)

O3C3C2	108.9(2)

C4C3C2	110.3(2)

O3C3H3	109.1

C4C3H3	109.1

C2C3H3	109.1

O4AC4O4B	125.3(3)

O4AC4C3	117.2(2)

O4BC4C3	117.5(2)

C2O2H2O	109.5

C3O3H3O	109.5

C12C11C16	118.8(2)

C12C11C17	122.2(2)

C16C11C17	119.0(2)

C11C12C13	120.5(3)

C11C12H12	119.7

C13C12H12	119.7

C14C13C12	120.1(3)

C14C13H13	119.9

C12C13H13	119.9

C13C14C15	119.9(3)

C13C14H14	120.0

C15C14H14	120.0

C14C15C16	120.1(3)

C14C15H15	120.0

C16C15H15	120.0

C15C16C11	120.5(3)

C15C16H16	119.7

C11C16H16	119.7

N19C17C11	110.0(2)

N19C17C18	107.3(2)

C11C17C18	115.6(2)

N19C17H17	107.9

C11C17H17	107.9

C18C17H17	107.9

C17C18H18A	109.5

C17C18H18B	109.5

H18AC18H18B	109.5

C17C18H18C	109.5

H18AC18H18C	109.5

H18BC18H18C	109.5

C17N19H19A	109.5

C17N19H19B	109.5

H19AN19H19B	109.5

C17N19H19C	109.5

H19AN19H19C	109.5

H19BN19H19C	109.5

C26C21C22	118.5(3)

C26C21C27	123.3(2)

C22C21C27	118.1(3)

C23C22C21	121.0(3)

C23C22H22	119.5

C21C22H22	119.5

C24C23C22	119.6(3)

C24C23H23	120.2

C22C23H23	120.2

C25C24C23	120.3(3)

C25C24H24	119.9

C23C24H24	119.9

C24C25C26	120.1(3)

C24C25H25	119.9

C26C25H25	119.9

C21C26C25	120.5(3)

C21C26H26	119.8

C25C26H26	119.8

N29C27C21	112.1(2)

N29C27C28	107.6(2)

C21C27C28	112.0(2)

N29C27H27	108.4

C21C27H27	108.4

C28C27H27	108.4

C27C28H28A	109.5

C27C28H28B	109.5

H28AC28H28B	109.5

C27C28H28C	109.5

H28AC28H28C	109.5

H28BC28H28C	109.5

C27N29H29A	109.5

C27N29H29B	109.5

H29AN29H29B	109.5

C27N29H29C	109.5

H29AN29H29C	109.5

H29BN29H29C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 5. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	28(2) 	17(1)	27(1) 	2(1)	16(1) 	1(1)

C2	19(1) 	18(1)	25(1) 	0(1)	6(1) 	1(1)

C3	24(1) 	19(1)	21(1) 	1(1)	4(1) 	2(1)

C4	29(2) 	19(1)	20(1) 	3(1)	3(1) 	2(1)

O1A	43(1) 	21(1)	35(1) 	9(1)	22(1) 	9(1)

O1B	23(1) 	25(1)	46(1) 	2(1)	13(1) 	5(1)

O2	22(1) 	31(1)	24(1) 	2(1)	5(1) 	2(1)

O3	34(1) 	21(1)	27(1) 	5(1)	13(1) 	4(1)

O4A	42(1) 	28(1)	42(1) 	2(1)	21(1) 	8(1)

O4B	30(1) 	19(1)	31(1) 	2(1)	3(1) 	1(1)

C11	17(1) 	25(1)	20(1) 	2(1)	2(1) 	1(1)

C12	24(1) 	23(1)	24(1) 	0(1)	6(1) 	4(1)

C13	25(1) 	27(1)	28(2) 	3(1)	6(1) 	2(1)

C14	27(2) 	38(2)	26(2) 	2(1)	10(1) 	2(1)

C15	31(2) 	36(2)	29(2) 	9(1)	11(1) 	5(1)

C16	24(1) 	23(1)	30(2) 	5(1)	5(1) 	1(1)

C17	19(1) 	20(1)	25(1) 	1(1)	3(1) 	1(1)

C18	20(1) 	22(1)	29(2) 	0(1)	6(1) 	2(1)

N19	22(1) 	20(1)	24(1) 	0(1)	6(1) 	1(1)

C21	26(1) 	19(1)	22(1) 	2(1)	9(1) 	1(1)

C22	30(2) 	29(2)	26(2) 	0(1)	4(1) 	3(1)

C23	41(2) 	28(2)	24(2) 	5(1)	9(1) 	2(1)

C24	31(2) 	26(1)	33(2) 	2(1)	11(1) 	7(1)

C25	26(2) 	29(2)	32(2) 	2(1)	4(1) 	7(1)

C26	28(2) 	26(1)	26(2) 	5(1)	6(1) 	3(1)

C27	24(1) 	21(1)	22(1) 	0(1)	8(1) 	3(1)

C28	36(2) 	25(1)	25(2) 	4(1)	11(1) 	2(1)

N29	26(1) 	19(1)	25(1) 	2(1)	10(1) 	2(1)

Table 6. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O2H2O...O3	0.84	2.44	2.853(3)	111.0

O3H3O...O4A	0.84	2.09	2.602(3)	118.6

O2H2O...O1Bi	0.84	2.06	2.872(3)	162.2

N19H19A...O1Bii	0.91	1.87	2.734(3)	157.6

N19H19B...O1Aiii	0.91	1.89	2.760(3)	160.0

N19H19C...O4Biv	0.91	1.93	2.817(3)	162.8

N29H29A...O1Aiv	0.91	1.94	2.775(3)	151.8

N29H29B...O4Av	0.91	1.81	2.708(3)	168.4

N29H29C...O4Bvi	0.91	1.85	2.741(3)	167.0

Symmetry transformations used to generate equivalent atoms:

(i) x1,y,z    (ii) x+1,y1/2,z+1    (iii) x,y1/2,z+1

(iv)  x,y,z+1    (v) x,y+1/2,z+1    (vi) x+1,y+1/2,z+1