|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0059p21

Empirical formula 	C7H18N2O6

Formula weight 	226.23

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 8.2165(4) Å	 = 90°

b = 7.0534(5) Å	 = 104.266(4)°

c = 10.0677(7) Å	  = 90°

Volume	565.47(6) Å3

Z	2

Density (calculated)	1.329 Mg / m3

Absorption coefficient	0.115 mm1

F(000)	244

Crystal	plate; colourless

Crystal size	0.20  0.11  0.03 mm3

 range for data collection	3.56  23.35°

Index ranges	9  h  9, 7  k  7, 11  l  11

Reflections collected	7091

Independent reflections	738 [Rint = 0.0657]

Completeness to  = 23.35°	82.3 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9966 and 0.9773

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	738 / 7 / 155

Goodness-of-fit on F2	1.063

Final R indices [F2 > 2(F2)]	R1 = 0.0344, wR2 = 0.0761

R indices (all data)	R1 = 0.0462, wR2 = 0.0788

Absolute structure parameter	10(10)

Extinction coefficient	0.058(12)

Largest diff. peak and hole	0.155 and 0.167 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1903(4)	2033(5)	8753(4)	24(1)	1

C2	1488(4)	514(5)	7602(4)	25(1)	1

O1A	3433(3)	2147(3)	9406(3)	28(1)	1

O1B	738(3)	2984(5)	8971(3)	37(1)	1

O2A	2606(3)	619(4)	7512(3)	34(1)	1

O2B	17(3)	605(4)	6823(3)	31(1)	1

C22	6242(5)	1313(5)	6670(4)	28(1)	1

C23	6423(5)	382(5)	7610(4)	29(1)	1

C25	7232(4)	1753(6)	9591(4)	28(1)	1

C26	7068(5)	3418(5)	8649(4)	26(1)	1

C27	7401(5)	4497(5)	6390(4)	35(1)	1

N21	7430(4)	2835(5)	7317(3)	25(1)	1

N24	6108(4)	184(4)	8946(3)	25(1)	1

O1W	1501(4)	1878(4)	4880(3)	37(1)	1

O2W	3555(3)	4172(4)	6752(3)	39(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1B	1.231(5)

C1O1A	1.270(4)

C1C2	1.553(5)

C2O2A	1.238(4)

C2O2B	1.270(5)

C22N21	1.489(5)

C22C23	1.509(6)

C22H22A	0.9900

C22H22B	0.9900

C23N24	1.485(5)

C23H23A	0.9900

C23H23B	0.9900

C25N24	1.485(5)

C25C26	1.495(5)

C25H25A	0.9900

C25H25B	0.9900

C26N21	1.500(4)

C26H26A	0.9900

C26H26B	0.9900

C27N21	1.495(5)

C27H27A	0.9800

C27H27B	0.9800

C27H27C	0.9800

N21H21	0.9300

N24H24A	0.9200

N24H24B	0.9200

O1WH1W	0.85(2)

O1WH2W	0.85(2)

O2WH21W	0.84(2)

O2WH22W	0.86(2)

O1BC1O1A	125.9(3)

O1BC1C2	118.1(3)

O1AC1C2	115.9(3)

O2AC2O2B	126.7(4)

O2AC2C1	118.0(3)

O2BC2C1	115.3(3)

N21C22C23	110.2(3)

N21C22H22A	109.6

C23C22H22A	109.6

N21C22H22B	109.6

C23C22H22B	109.6

H22AC22H22B	108.1

N24C23C22	110.0(3)

N24C23H23A	109.7

C22C23H23A	109.7

N24C23H23B	109.7

C22C23H23B	109.7

H23AC23H23B	108.2

N24C25C26	111.0(3)

N24C25H25A	109.4

C26C25H25A	109.4

N24C25H25B	109.4

C26C25H25B	109.4

H25AC25H25B	108.0

C25C26N21	110.2(3)

C25C26H26A	109.6

N21C26H26A	109.6

C25C26H26B	109.6

N21C26H26B	109.6

H26AC26H26B	108.1

N21C27H27A	109.5

N21C27H27B	109.5

H27AC27H27B	109.5

N21C27H27C	109.5

H27AC27H27C	109.5

H27BC27H27C	109.5

C22N21C27	112.6(3)

C22N21C26	109.6(3)

C27N21C26	111.5(3)

C22N21H21	107.6

C27N21H21	107.6

C26N21H21	107.6

C25N24C23	111.6(3)

C25N24H24A	109.3

C23N24H24A	109.3

C25N24H24B	109.3

C23N24H24B	109.3

H24AN24H24B	108.0

H1WO1WH2W	105(3)

H21WO2WH22W	105(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	20(2) 	28(2)	24(2) 	2(2)	7(2) 	0(2)

C2	21(2) 	26(2)	29(2) 	4(2)	8(2) 	1(2)

O1A	18(1) 	32(2)	31(2) 	7(1)	3(1) 	0(1)

O1B	19(1) 	44(2)	45(2) 	16(2)	5(1) 	2(1)

O2A	24(2) 	34(2)	41(2) 	8(1)	3(1) 	7(1)

O2B	20(1) 	36(2)	35(2) 	6(1)	2(1) 	0(1)

C22	21(2) 	34(2)	27(2) 	3(2)	4(2) 	1(2)

C23	23(2) 	29(2)	38(2) 	5(2)	10(2) 	2(2)

C25	23(2) 	32(2)	29(2) 	2(2)	6(2) 	0(2)

C26	20(2) 	28(2)	30(2) 	4(2)	5(2) 	4(2)

C27	34(2) 	32(2)	39(2) 	11(2)	10(2) 	4(2)

N21	21(2) 	23(2)	31(2) 	5(2)	6(1) 	5(1)

N24	19(2) 	28(2)	29(2) 	4(2)	7(1) 	2(1)

O1W	39(2) 	34(2)	35(2) 	6(2)	4(2) 	1(2)

O2W	28(2) 	35(2)	54(2) 	4(2)	10(1) 	1(2)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N24H24A...O1A	0.92	1.91	2.733(4)	147.1

N24H24A...O2A	0.92	2.24	2.939(4)	132.0

O1WH2W...O2B	0.85(2)	1.88(3)	2.692(4)	159(6)

O2WH21W...O2A	0.84(2)	2.00(2)	2.787(4)	157(4)

N21H21...O2Bi	0.93	1.98	2.786(4)	143.8

N21H21...O1Bi	0.93	2.10	2.819(4)	133.3

N24H24B...O1Aii	0.92	1.76	2.679(4)	178.3

O1WH1W...O2Biii	0.85(2)	2.11(2)	2.934(4)	165(5)

O2WH22W...O1Wiii	0.86(2)	1.99(3)	2.797(4)	156(5)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z    (ii) x+1,y1/2,z+2    (iii) x,y1/2,z+1