|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	04skc0006p21

Empirical formula 	C5H13NO7

Formula weight 	199.16

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 5.2139(17) Å	 = 90°

b = 11.140(7) Å	 = 95.32(3)°

c = 7.489(3) Å	  = 90°

Volume	433.1(4) Å3

Z	2

Density (calculated)	1.527 Mg / m3

Absorption coefficient	0.144 mm1

F(000)	212

Crystal	block; colourless

Crystal size	0.10  0.10  0.04 mm3

 range for data collection	3.29  27.44°

Index ranges	6  h  5, 14  k  12, 9  l  8

Reflections collected	4112

Independent reflections	1040 [Rint = 0.0818]

Completeness to  = 27.44°	99.5 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9942 and 0.9857

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1040 / 4 / 131

Goodness-of-fit on F2	1.041

Final R indices [F2 > 2(F2)]	R1 = 0.0558, wR2 = 0.1035

R indices (all data)	R1 = 0.0826, wR2 = 0.1137

Absolute structure parameter	10(10)

Largest diff. peak and hole	0.252 and 0.297 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	36(7)	6589(3)	3247(4)	20(1)	1

C2	702(6)	6595(3)	1339(4)	19(1)	1

C3	742(7)	7600(3)	284(4)	20(1)	1

C4	356(8)	7721(4)	1516(4)	21(1)	1

O1A	2265(5)	6296(2)	3504(3)	23(1)	1

O1B	1714(5)	6891(3)	4455(3)	25(1)	1

O2	3387(4)	6766(3)	1230(3)	23(1)	1

O3	424(5)	8672(2)	1293(3)	23(1)	1

O4A	24(5)	6746(2)	2482(3)	28(1)	1

O4B	1406(6)	8620(2)	1996(3)	28(1)	1

C21	5974(8)	9039(4)	5175(6)	31(1)	1

N22	3546(7)	9463(3)	4198(5)	27(1)	1

O1W	4930(6)	9815(3)	611(3)	25(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1A	1.239(4)

C1O1B	1.269(4)

C1C2	1.514(5)

C2O2	1.423(4)

C2C3	1.528(5)

C2H2	1.0000

C3O3	1.415(4)

C3C4	1.519(5)

C3H3	1.0000

C4O4B	1.212(5)

C4O4A	1.308(5)

O2H2O	0.8400

O3H3O	0.8400

O4AH4	0.8400

C21N22	1.480(6)

C21H21A	0.9800

C21H21B	0.9800

C21H21C	0.9800

N22H22A	0.9100

N22H22B	0.9100

N22H22C	0.9100

O1WH1W	0.839(19)

O1WH2W	0.82(2)

O1AC1O1B	125.6(3)

O1AC1C2	118.2(3)

O1BC1C2	116.3(3)

O2C2C1	113.1(3)

O2C2C3	108.2(3)

C1C2C3	109.6(3)

O2C2H2	108.6

C1C2H2	108.6

C3C2H2	108.6

O3C3C4	111.3(3)

O3C3C2	108.4(3)

C4C3C2	108.4(3)

O3C3H3	109.6

C4C3H3	109.6

C2C3H3	109.6

O4BC4O4A	124.2(3)

O4BC4C3	123.7(3)

O4AC4C3	112.1(3)

C2O2H2O	109.5

C3O3H3O	109.5

C4O4AH4	109.5

N22C21H21A	109.5

N22C21H21B	109.5

H21AC21H21B	109.5

N22C21H21C	109.5

H21AC21H21C	109.5

H21BC21H21C	109.5

C21N22H22A	109.5

C21N22H22B	109.5

H22AN22H22B	109.5

C21N22H22C	109.5

H22AN22H22C	109.5

H22BN22H22C	109.5

H1WO1WH2W	109(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	21(2) 	16(2)	22(2) 	3(2)	2(2) 	3(2)

C2	18(2) 	22(2)	16(2) 	1(2)	1(1) 	0(2)

C3	21(2) 	17(2)	20(2) 	1(2)	2(2) 	1(2)

C4	19(2) 	22(2)	20(2) 	2(2)	0(2) 	2(2)

O1A	19(2) 	27(2)	23(1) 	2(1)	1(1) 	1(1)

O1B	19(1) 	35(2)	21(1) 	1(1)	1(1) 	4(1)

O2	16(1) 	35(2)	18(1) 	1(1)	1(1) 	2(1)

O3	23(2) 	20(2)	27(1) 	2(1)	1(1) 	5(1)

O4A	38(2) 	26(2)	18(1) 	0(1)	4(1) 	7(1)

O4B	32(2) 	27(2)	23(1) 	1(1)	5(1) 	5(1)

C21	24(2) 	33(3)	35(2) 	7(2)	3(2) 	4(2)

N22	25(2) 	26(2)	30(2) 	5(2)	2(1) 	1(2)

O1W	24(2) 	23(2)	30(1) 	3(1)	1(1) 	1(1)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O2H2O...O1B	0.84	2.18	2.646(3)	114.9

N22H22A...O1B	0.91	2.24	3.032(5)	145.9

N22H22B...O1W	0.91	1.98	2.872(4)	166.6

O1WH2W...O4B	0.82(2)	2.07(3)	2.881(4)	165(5)

O1WH2W...O3	0.82(2)	2.61(4)	3.152(4)	125(4)

O2H2O...O1Ai	0.84	2.06	2.757(3)	140.3

O3H3O...O1Wii	0.84	1.91	2.742(4)	170.5

O4AH4...O1Biii	0.84	1.70	2.537(4)	171.1

O4AH4...O1Aiii	0.84	2.63	3.169(4)	122.8

N22H22C...O1Aiv	0.91	1.90	2.792(4)	165.3

O1WH1W...O2v	0.839(19)	1.93(2)	2.760(4)	171(5)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z    (ii) x1,y,z    (iii) x,y,z1    (iv)  x,y+1/2,z+1

(v) x+1,y+1/2,z