|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	07skc0001pbca

Empirical formula 	C12H28N2O6

Formula weight 	296.36

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 13.3732(16) Å	 = 90°

b = 8.5025(9) Å	 = 90°

c = 27.693(3) Å	  = 90°

Volume	3148.9(6) Å3

Z	8

Density (calculated)	1.250 Mg / m3

Absorption coefficient	0.099 mm1

F(000)	1296

Crystal	plate; colourless

Crystal size	0.11  0.09  0.02 mm3

 range for data collection	2.93  27.48°

Index ranges	15  h  17, 10  k  10, 24  l  35

Reflections collected	13540

Independent reflections	3058 [Rint = 0.0955]

Completeness to  = 25.00°	90.1 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9980 and 0.9892

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3058 / 0 / 187

Goodness-of-fit on F2	1.145

Final R indices [F2 > 2(F2)]	R1 = 0.1244, wR2 = 0.1932

R indices (all data)	R1 = 0.2187, wR2 = 0.2353

Largest diff. peak and hole	0.454 and 0.346 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5053(5)	2372(7)	4324(2)	26(1)	1

C2	5602(4)	971(7)	4088(2)	29(2)	1

C3	5780(4)	361(7)	4445(2)	27(1)	1

C4	6371(5)	1689(7)	4211(2)	28(1)	1

O1A	5434(3)	3710(5)	4280(1)	30(1)	1

O1B	4242(3)	2085(5)	4539(2)	32(1)	1

O2	6503(3)	1437(5)	3859(1)	29(1)	1

O3	6259(3)	257(5)	4866(1)	28(1)	1

O4A	5999(3)	2248(5)	3830(2)	36(1)	1

O4B	7171(3)	2124(5)	4410(2)	33(1)	1

C21	4087(5)	4313(10)	2295(2)	54(2)	1

C22	5184(5)	4261(9)	2416(2)	42(2)	1

C23	5403(5)	4548(8)	2947(2)	35(2)	1

C24	6511(5)	4550(8)	3059(2)	32(2)	1

N25	6694(4)	4925(6)	3567(2)	28(1)	1

C31	7612(6)	1783(10)	6691(2)	56(2)	1

C32	8279(5)	1998(8)	6251(2)	42(2)	1

C33	8076(5)	771(8)	5861(2)	33(2)	1

C34	8620(5)	1141(7)	5397(2)	32(2)	1

N35	8453(4)	124(6)	5028(2)	32(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1A	1.254(7)

C1O1B	1.259(7)

C1C2	1.546(8)

C2O2	1.419(7)

C2C3	1.522(8)

C2H2	1.0000

C3O3	1.430(6)

C3C4	1.523(8)

C3H3	1.0000

C4O4B	1.258(7)

C4O4A	1.259(7)

O2H20	0.8400

O3H3O	0.8400

C21C22	1.506(9)

C21H21A	0.9800

C21H21B	0.9800

C21H21C	0.9800

C22C23	1.519(8)

C22H22A	0.9900

C22H22B	0.9900

C23C24	1.514(8)

C23H23A	0.9900

C23H23B	0.9900

C24N25	1.462(7)

C24H24A	0.9900

C24H24B	0.9900

N25H25A	0.9100

N25H25B	0.9100

N25H25C	0.9100

C31C32	1.520(9)

C31H31A	0.9800

C31H31B	0.9800

C31H31C	0.9800

C32C33	1.527(8)

C32H32A	0.9900

C32H32B	0.9900

C33C34	1.508(8)

C33H33A	0.9900

C33H33B	0.9900

C34N35	1.500(7)

C34H34A	0.9900

C34H34B	0.9900

N35H35A	0.9100

N35H35B	0.9100

N35H35C	0.9100

O1AC1O1B	125.0(6)

O1AC1C2	117.7(5)

O1BC1C2	117.3(5)

O2C2C3	111.4(5)

O2C2C1	112.2(5)

C3C2C1	111.8(5)

O2C2H2	107.0

C3C2H2	107.0

C1C2H2	107.0

O3C3C4	112.7(5)

O3C3C2	109.1(5)

C4C3C2	110.9(5)

O3C3H3	108.0

C4C3H3	108.0

C2C3H3	108.0

O4BC4O4A	126.2(6)

O4BC4C3	118.3(5)

O4AC4C3	115.5(5)

C2O2H20	109.5

C3O3H3O	109.5

C22C21H21A	109.5

C22C21H21B	109.5

H21AC21H21B	109.5

C22C21H21C	109.5

H21AC21H21C	109.5

H21BC21H21C	109.5

C21C22C23	113.5(5)

C21C22H22A	108.9

C23C22H22A	108.9

C21C22H22B	108.9

C23C22H22B	108.9

H22AC22H22B	107.7

C24C23C22	112.9(5)

C24C23H23A	109.0

C22C23H23A	109.0

C24C23H23B	109.0

C22C23H23B	109.0

H23AC23H23B	107.8

N25C24C23	111.3(5)

N25C24H24A	109.4

C23C24H24A	109.4

N25C24H24B	109.4

C23C24H24B	109.4

H24AC24H24B	108.0

C24N25H25A	109.5

C24N25H25B	109.5

H25AN25H25B	109.5

C24N25H25C	109.5

H25AN25H25C	109.5

H25BN25H25C	109.5

C32C31H31A	109.5

C32C31H31B	109.5

H31AC31H31B	109.5

C32C31H31C	109.5

H31AC31H31C	109.5

H31BC31H31C	109.5

C31C32C33	112.4(6)

C31C32H32A	109.1

C33C32H32A	109.1

C31C32H32B	109.1

C33C32H32B	109.1

H32AC32H32B	107.9

C34C33C32	112.0(5)

C34C33H33A	109.2

C32C33H33A	109.2

C34C33H33B	109.2

C32C33H33B	109.2

H33AC33H33B	107.9

N35C34C33	111.0(5)

N35C34H34A	109.4

C33C34H34A	109.4

N35C34H34B	109.4

C33C34H34B	109.4

H34AC34H34B	108.0

C34N35H35A	109.5

C34N35H35B	109.5

H35AN35H35B	109.5

C34N35H35C	109.5

H35AN35H35C	109.5

H35BN35H35C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	32(4) 	28(4)	17(3) 	4(2)	8(3) 	1(3)

C2	31(4) 	33(4)	23(3) 	6(3)	1(3) 	3(3)

C3	25(3) 	32(4)	24(3) 	2(3)	10(3) 	7(3)

C4	35(4) 	23(3)	27(3) 	6(3)	3(3) 	5(3)

O1A	30(2) 	27(3)	33(2) 	0(2)	2(2) 	2(2)

O1B	31(3) 	35(3)	30(2) 	0(2)	6(2) 	0(2)

O2	23(2) 	37(3)	27(2) 	0(2)	2(2) 	1(2)

O3	33(3) 	30(2)	22(2) 	3(2)	3(2) 	2(2)

O4A	39(3) 	34(3)	34(2) 	12(2)	7(2) 	8(2)

O4B	23(2) 	40(3)	36(2) 	1(2)	2(2) 	9(2)

C21	42(5) 	85(6)	34(4) 	4(4)	5(3) 	2(4)

C22	36(4) 	57(5)	33(4) 	2(3)	3(3) 	4(4)

C23	35(4) 	45(4)	25(3) 	1(3)	1(3) 	3(3)

C24	34(4) 	37(4)	24(3) 	2(3)	3(3) 	6(3)

N25	25(3) 	31(3)	28(3) 	2(2)	2(2) 	3(2)

C31	54(5) 	75(6)	39(4) 	10(4)	3(4) 	7(4)

C32	43(4) 	47(4)	35(4) 	5(3)	4(3) 	8(3)

C33	34(4) 	43(4)	24(3) 	2(3)	2(3) 	5(3)

C34	28(4) 	36(4)	31(3) 	1(3)	6(3) 	4(3)

N35	28(3) 	38(3)	31(3) 	6(2)	3(2) 	2(3)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N25H25A...O1A	0.91	1.99	2.793(6)	146.8

N25H25A...O2	0.91	2.35	3.084(6)	137.6

N35H35C...O3	0.91	2.06	2.971(6)	173.5

N35H35C...O4B	0.91	2.60	3.086(6)	114.0

O2H20...O4Bi	0.84	1.82	2.640(6)	163.6

N25H25C...O2i	0.91	2.08	2.848(6)	141.8

O3H3O...O1Bii	0.84	1.87	2.671(6)	159.2

N25H25B...O4Aiii	0.91	1.77	2.679(6)	173.3

N35H35B...O1Biv	0.91	1.96	2.862(6)	171.7

N35H35A...O1Av	0.91	1.95	2.820(6)	160.3

Symmetry transformations used to generate equivalent atoms:

(i) x+3/2,y+1/2,z    (ii) x+1,y,z+1    (iii) x,y+1,z

(iv)  x+1/2,y+1/2,z+1    (v) x+3/2,y1/2,z