|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	04mbh0606

Empirical formula 	C12H25NO13

Formula weight 	391.33

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P1

Unit cell dimensions	a = 4.865(2) Å	 = 98.13(3)°

b = 9.416(3) Å	 = 95.13(7)°

c = 19.127(12) Å	  = 97.98(3)°

Volume	853.7(7) Å3

Z	2

Density (calculated)	1.522 Mg / m3

Absorption coefficient	0.140 mm1

F(000)	416

Crystal	lath; colourless

Crystal size	0.20  0.10  0.02 mm3

 range for data collection	3.63  27.48°

Index ranges	5  h  6, 12  k  12, 24  l  24

Reflections collected	15063

Independent reflections	3899 [Rint = 0.0922]

Completeness to  = 27.48°	99.4 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9972 and 0.9726

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3899 / 3 / 252

Goodness-of-fit on F2	1.021

Final R indices [F2 > 2(F2)]	R1 = 0.0596, wR2 = 0.1102

R indices (all data)	R1 = 0.1343, wR2 = 0.1354

Largest diff. peak and hole	0.319 and 0.397 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	11676(5)	8357(3)	6080(1)	18(1)	1

C2	9378(5)	7751(3)	5480(1)	18(1)	1

C3	10655(5)	7178(3)	4817(1)	17(1)	1

C4	8385(5)	6583(3)	4213(1)	18(1)	1

O1A	12896(4)	7316(2)	6275(1)	25(1)	1

O1B	12198(4)	9639(2)	6320(1)	22(1)	1

O2	7665(3)	8796(2)	5329(1)	22(1)	1

O3	12487(3)	8266(2)	4577(1)	20(1)	1

O4A	6444(4)	5648(2)	4404(1)	21(1)	1

O4B	8407(4)	6919(2)	3623(1)	20(1)	1

C21	6968(7)	289(4)	9208(2)	40(1)	1

C22	8629(6)	289(3)	8647(2)	29(1)	1

C23	6810(6)	822(3)	8086(1)	24(1)	1

C24	8471(5)	1338(3)	7520(1)	23(1)	1

N25	6709(4)	1897(2)	6975(1)	24(1)	1

C31	12116(5)	3659(3)	2867(1)	20(1)	1

C32	10087(5)	3808(3)	2238(1)	19(1)	1

C33	11713(5)	4202(3)	1626(1)	19(1)	1

C34	9693(6)	4463(3)	1025(2)	22(1)	1

O31A	13179(4)	2505(2)	2806(1)	25(1)	1

O31B	12586(4)	4685(2)	3374(1)	21(1)	1

O32	8463(4)	4913(2)	2422(1)	22(1)	1

O33	13673(4)	5484(2)	1832(1)	23(1)	1

O34A	9816(4)	5600(2)	795(1)	25(1)	1

O34B	7820(4)	3309(2)	798(1)	29(1)	1

O1W	4969(4)	3284(2)	9613(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1B	1.213(3)

C1O1A	1.295(3)

C1C2	1.516(4)

C2O2	1.418(3)

C2C3	1.525(4)

C2H2	1.0000

C3O3	1.417(3)

C3C4	1.512(4)

C3H3	1.0000

C4O4B	1.217(3)

C4O4A	1.311(3)

O1AH1	0.8400

O2H2O	0.8400

O3H3O	0.8400

O4AH4	0.8400

C21C22	1.516(4)

C21H21A	0.9800

C21H21B	0.9800

C21H21C	0.9800

C22C23	1.515(4)

C22H22A	0.9900

C22H22B	0.9900

C23C24	1.501(4)

C23H23A	0.9900

C23H23B	0.9900

C24N25	1.491(3)

C24H24A	0.9900

C24H24B	0.9900

N25H25B	0.9100

N25H25C	0.9100

N25H25A	0.9100

C31O31B	1.248(3)

C31O31A	1.262(3)

C31C32	1.522(4)

C32O32	1.416(3)

C32C33	1.530(4)

C32H32	1.0000

C33O33	1.414(3)

C33C34	1.515(4)

C33H33	1.0000

C34O34A	1.209(3)

C34O34B	1.311(3)

O32H32O	0.8400

O33H33O	0.8400

O34BH34	0.8400

O1WH1W	0.822(17)

O1WH2W	0.861(18)

O1BC1O1A	127.6(2)

O1BC1C2	122.4(2)

O1AC1C2	109.9(2)

O2C2C1	112.1(2)

O2C2C3	110.4(2)

C1C2C3	109.7(2)

O2C2H2	108.1

C1C2H2	108.1

C3C2H2	108.1

O3C3C4	107.0(2)

O3C3C2	112.8(2)

C4C3C2	110.2(2)

O3C3H3	108.9

C4C3H3	108.9

C2C3H3	108.9

O4BC4O4A	124.8(2)

O4BC4C3	123.5(2)

O4AC4C3	111.7(2)

C1O1AH1	109.5

C2O2H2O	109.5

C3O3H3O	109.5

C4O4AH4	109.5

C22C21H21A	109.5

C22C21H21B	109.5

H21AC21H21B	109.5

C22C21H21C	109.5

H21AC21H21C	109.5

H21BC21H21C	109.5

C23C22C21	112.3(3)

C23C22H22A	109.1

C21C22H22A	109.1

C23C22H22B	109.1

C21C22H22B	109.1

H22AC22H22B	107.9

C24C23C22	111.6(2)

C24C23H23A	109.3

C22C23H23A	109.3

C24C23H23B	109.3

C22C23H23B	109.3

H23AC23H23B	108.0

N25C24C23	111.9(2)

N25C24H24A	109.2

C23C24H24A	109.2

N25C24H24B	109.2

C23C24H24B	109.2

H24AC24H24B	107.9

C24N25H25B	109.5

C24N25H25C	109.5

H25BN25H25C	109.5

C24N25H25A	109.5

H25BN25H25A	109.5

H25CN25H25A	109.5

O31BC31O31A	127.4(2)

O31BC31C32	117.4(2)

O31AC31C32	115.2(2)

O32C32C31	111.1(2)

O32C32C33	108.3(2)

C31C32C33	109.6(2)

O32C32H32	109.3

C31C32H32	109.3

C33C32H32	109.3

O33C33C34	107.6(2)

O33C33C32	112.0(2)

C34C33C32	109.2(2)

O33C33H33	109.3

C34C33H33	109.3

C32C33H33	109.3

O34AC34O34B	125.3(3)

O34AC34C33	123.5(3)

O34BC34C33	111.2(2)

C32O32H32O	109.5

C33O33H33O	109.5

C34O34BH34	109.5

H1WO1WH2W	107(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	16(1) 	21(2)	17(1) 	4(1)	4(1) 	6(1)

C2	17(1) 	15(1)	21(2) 	3(1)	1(1) 	3(1)

C3	16(1) 	16(1)	20(2) 	5(1)	1(1) 	1(1)

C4	17(1) 	15(1)	22(2) 	2(1)	4(1) 	6(1)

O1A	24(1) 	24(1)	25(1) 	2(1)	9(1) 	5(1)

O1B	21(1) 	20(1)	23(1) 	1(1)	1(1) 	2(1)

O2	18(1) 	19(1)	27(1) 	2(1)	2(1) 	5(1)

O3	14(1) 	24(1)	23(1) 	7(1)	0(1) 	1(1)

O4A	20(1) 	20(1)	20(1) 	1(1)	2(1) 	2(1)

O4B	21(1) 	23(1)	17(1) 	5(1)	2(1) 	2(1)

C21	56(2) 	34(2)	31(2) 	11(2)	6(2) 	8(2)

C22	35(2) 	25(2)	25(2) 	3(1)	0(1) 	1(1)

C23	25(2) 	21(2)	24(2) 	2(1)	4(1) 	1(1)

C24	20(2) 	25(2)	25(2) 	5(1)	2(1) 	3(1)

N25	21(1) 	27(1)	24(1) 	5(1)	4(1) 	0(1)

C31	13(1) 	25(2)	21(2) 	6(1)	1(1) 	0(1)

C32	16(1) 	20(2)	20(2) 	2(1)	1(1) 	4(1)

C33	17(1) 	17(2)	21(2) 	0(1)	1(1) 	3(1)

C34	21(2) 	27(2)	19(2) 	1(1)	4(1) 	4(1)

O31A	25(1) 	23(1)	25(1) 	4(1)	6(1) 	7(1)

O31B	20(1) 	23(1)	19(1) 	1(1)	4(1) 	3(1)

O32	22(1) 	28(1)	18(1) 	0(1)	1(1) 	10(1)

O33	15(1) 	24(1)	29(1) 	4(1)	2(1) 	2(1)

O34A	27(1) 	26(1)	23(1) 	8(1)	0(1) 	4(1)

O34B	28(1) 	31(1)	26(1) 	8(1)	10(1) 	3(1)

O1W	24(1) 	29(1)	26(1) 	7(1)	1(1) 	4(1)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O2H2O...O1B	0.84	2.30	2.725(3)	111.4

O32H32O...O4B	0.84	2.04	2.764(3)	144.7

O32H32O...O31B	0.84	2.15	2.638(3)	116.7

O1AH1...O31Ai	0.84	1.67	2.448(3)	152.2

O2H2O...O3ii	0.84	2.12	2.758(3)	132.6

O3H3O...O2iii	0.84	1.89	2.732(3)	175.4

O33H33O...O32iii	0.84	1.82	2.654(3)	171.6

O4AH4...O31Biv	0.84	1.75	2.567(3)	165.4

N25H25B...O4Bv	0.91	2.10	2.881(3)	143.6

N25H25B...O3v	0.91	2.24	3.014(3)	142.1

N25H25C...O33v	0.91	2.34	3.152(3)	148.5

O1WH2W...O34Av	0.861(18)	2.07(2)	2.828(3)	147(3)

O1WH2W...O33v	0.861(18)	2.50(3)	3.233(3)	143(3)

N25H25A...O1Bvi	0.91	1.99	2.892(3)	171.8

O34BH34...O1Wvii	0.84	1.72	2.543(3)	165.4

O1WH1W...O34Aviii	0.822(17)	1.966(19)	2.779(3)	170(3)

Symmetry transformations used to generate equivalent atoms:

(i) x+3,y+1,z+1    (ii) x+2,y+2,z+1    (iii) x+1,y,z

(iv)  x1,y,z    (v) x+2,y+1,z+1    (vi) x1,y1,z

(vii) x,y,z1    (viii) x+1,y+1,z+1