|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	04skc0005p1

Empirical formula 	C13H28N2O14

Formula weight 	436.37

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P1

Unit cell dimensions	a = 7.4774(6) Å	 = 88.321(8)°

b = 7.7071(7) Å	 = 86.355(6)°

c = 16.2943(16) Å	  = 89.778(6)°

Volume	936.72(15) Å3

Z	2

Density (calculated)	1.547 Mg / m3

Absorption coefficient	0.141 mm1

F(000)	464

Crystal	lath; colourless

Crystal size	0.10  0.08  0.04 mm3

 range for data collection	2.93  27.47°

Index ranges	9  h  9, 10  k  10, 21  l  21

Reflections collected	20348

Independent reflections	4268 [Rint = 0.0500]

Completeness to  = 27.47°	99.8 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9944 and 0.9860

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4268 / 15 / 569

Goodness-of-fit on F2	1.040

Final R indices [F2 > 2(F2)]	R1 = 0.0377, wR2 = 0.0747

R indices (all data)	R1 = 0.0511, wR2 = 0.0800

Absolute structure parameter	10(10)

Largest diff. peak and hole	0.214 and 0.242 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	4457(4)	2516(4)	3198(2)	16(1)	1

C2	2398(4)	2633(4)	3175(2)	15(1)	1

C3	1793(4)	2686(4)	2300(2)	16(1)	1

C4	240(4)	2952(4)	2316(2)	18(1)	1

O1A	5285(3)	1493(3)	2731(1)	19(1)	1

O1B	5179(3)	3435(2)	3713(1)	18(1)	1

O2	1721(3)	4133(3)	3566(1)	18(1)	1

O3	2663(3)	4023(3)	1825(1)	20(1)	1

O4B	1140(3)	1650(3)	2683(1)	21(1)	1

O4A	914(3)	4237(3)	2022(2)	28(1)	1

C22	5964(4)	2541(4)	3275(2)	19(1)	1

C23	4070(4)	2422(4)	3654(2)	18(1)	1

C25	5159(4)	3143(4)	5013(2)	18(1)	1

C26	7028(4)	3275(4)	4632(2)	20(1)	1

C27	9152(4)	2194(4)	3527(2)	29(1)	1

N21	7288(3)	2097(3)	3887(2)	18(1)	1

N24	3845(3)	3590(3)	4401(1)	16(1)	1

C31	8379(4)	272(4)	904(2)	20(1)	1

C32	6470(4)	274(4)	745(2)	17(1)	1

C33	5596(4)	1205(4)	323(2)	17(1)	1

C34	3767(4)	583(3)	96(2)	16(1)	1

O31A	9612(3)	659(3)	498(2)	29(1)	1

O31B	8640(3)	1507(3)	1361(1)	26(1)	1

O32	6401(3)	1771(3)	222(1)	20(1)	1

O33	6680(3)	1736(3)	369(1)	26(1)	1

O34A	2706(3)	259(3)	726(1)	20(1)	1

O34B	3395(3)	401(3)	624(1)	20(1)	1

C42	1591(4)	3147(4)	9028(2)	19(1)	1

C43	339(4)	2431(4)	8434(2)	22(1)	1

C45	2037(4)	4340(4)	8971(2)	22(1)	1

C46	830(4)	4984(4)	9601(2)	20(1)	1

C47	2272(4)	5539(4)	9909(2)	25(1)	1

N41	1081(3)	4939(3)	9276(2)	17(1)	1

N44	1558(3)	2521(3)	8773(2)	20(1)	1

C51	1681(4)	539(4)	5613(2)	16(1)	1

C52	1822(4)	2358(3)	5933(2)	16(1)	1

C53	118(4)	3391(4)	5789(2)	15(1)	1

C54	411(4)	5223(4)	6088(2)	16(1)	1

O51A	2459(3)	63(3)	4983(1)	29(1)	1

O51B	609(3)	445(2)	6089(1)	24(1)	1

O52	3261(3)	3292(3)	5541(1)	20(1)	1

O53	268(3)	3420(2)	4943(1)	17(1)	1

O54A	655(3)	6461(2)	5562(1)	18(1)	1

O54B	425(3)	5327(3)	6843(1)	27(1)	1

C61	6292(3)	1216(4)	6908(2)	15(1)	1

C62	6566(4)	649(3)	7218(2)	14(1)	1

C63	4744(4)	1569(3)	7245(2)	14(1)	1

C64	4927(4)	3472(3)	7503(2)	15(1)	1

O61A	5845(3)	1377(3)	6181(1)	19(1)	1

O61B	6534(3)	2440(2)	7380(1)	20(1)	1

O62	7215(3)	693(2)	8018(1)	16(1)	1

O63	3467(2)	700(2)	7762(1)	16(1)	1

O64A	4216(3)	4107(3)	8127(1)	21(1)	1

O64B	5961(3)	4320(2)	6962(1)	21(1)	1

O1W	7103(3)	1135(3)	4592(1)	18(1)	1

O2W	305(3)	7527(3)	8021(1)	17(1)	1

O3W	5997(3)	4562(3)	1125(1)	23(1)	1

O4W	1821(3)	7393(3)	1993(1)	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1A	1.247(4)

C1O1B	1.263(3)

C1C2	1.544(4)

C2O2	1.413(3)

C2C3	1.523(4)

C2H2	1.0000

C3O3	1.406(3)

C3C4	1.532(4)

C3H3	1.0000

C4O4A	1.209(4)

C4O4B	1.318(3)

O2H2O	0.8400

O3H3O	0.8400

O4BH4	0.8400

C22N21	1.497(4)

C22C23	1.512(4)

C22H22A	0.9900

C22H22B	0.9900

C23N24	1.495(4)

C23H23A	0.9900

C23H23B	0.9900

C25N24	1.491(4)

C25C26	1.497(4)

C25H25A	0.9900

C25H25B	0.9900

C26N21	1.497(4)

C26H26A	0.9900

C26H26B	0.9900

C27N21	1.480(4)

C27H27A	0.9800

C27H27B	0.9800

C27H27C	0.9800

N21H21	0.9300

N24H24A	0.9200

N24H24B	0.9200

C31O31B	1.214(4)

C31O31A	1.304(4)

C31C32	1.522(4)

C32O32	1.417(3)

C32C33	1.519(4)

C32H32	1.0000

C33O33	1.415(3)

C33C34	1.512(4)

C33H33	1.0000

C34O34B	1.227(3)

C34O34A	1.286(3)

O31AH31	0.8400

O32H32O	0.8400

O33H33O	0.8400

C42N41	1.492(4)

C42C43	1.506(4)

C42H42A	0.9900

C42H42B	0.9900

C43N44	1.491(4)

C43H43A	0.9900

C43H43B	0.9900

C45N44	1.485(4)

C45C46	1.505(4)

C45H45A	0.9900

C45H45B	0.9900

C46N41	1.493(4)

C46H46A	0.9900

C46H46B	0.9900

C47N41	1.490(4)

C47H47A	0.9800

C47H47B	0.9800

C47H47C	0.9800

N41H41	0.9300

N44H44A	0.9200

N44H44B	0.9200

C51O51A	1.214(4)

C51O51B	1.307(4)

C51C52	1.517(4)

C52O52	1.405(3)

C52C53	1.527(4)

C52H52	1.0000

C53O53	1.426(3)

C53C54	1.529(4)

C53H53	1.0000

C54O54B	1.236(4)

C54O54A	1.270(3)

O51BH51	0.8400

O52H52O	0.8400

O53H53O	0.8400

C61O61A	1.253(3)

C61O61B	1.255(3)

C61C62	1.527(4)

C62O62	1.418(3)

C62C63	1.536(4)

C62H62	1.0000

C63O63	1.413(3)

C63C64	1.522(4)

C63H63	1.0000

C64O64A	1.208(3)

C64O64B	1.321(3)

O62H62O	0.8400

O63H63O	0.8400

O64BH64	0.8400

O1WH1W	0.851(18)

O1WH2W	0.842(18)

O2WH21W	0.844(19)

O2WH22W	0.863(18)

O3WH31W	0.831(18)

O3WH32W	0.834(19)

O4WH41W	0.836(19)

O4WH42W	0.838(19)

O1AC1O1B	124.5(3)

O1AC1C2	118.5(2)

O1BC1C2	116.9(2)

O2C2C3	107.7(2)

O2C2C1	111.3(2)

C3C2C1	112.2(2)

O2C2H2	108.5

C3C2H2	108.5

C1C2H2	108.5

O3C3C2	111.0(2)

O3C3C4	109.9(2)

C2C3C4	109.7(2)

O3C3H3	108.7

C2C3H3	108.7

C4C3H3	108.7

O4AC4O4B	124.8(3)

O4AC4C3	122.4(3)

O4BC4C3	112.8(2)

C2O2H2O	109.5

C3O3H3O	109.5

C4O4BH4	109.5

N21C22C23	110.6(2)

N21C22H22A	109.5

C23C22H22A	109.5

N21C22H22B	109.5

C23C22H22B	109.5

H22AC22H22B	108.1

N24C23C22	110.3(2)

N24C23H23A	109.6

C22C23H23A	109.6

N24C23H23B	109.6

C22C23H23B	109.6

H23AC23H23B	108.1

N24C25C26	110.0(2)

N24C25H25A	109.7

C26C25H25A	109.7

N24C25H25B	109.7

C26C25H25B	109.7

H25AC25H25B	108.2

N21C26C25	111.2(2)

N21C26H26A	109.4

C25C26H26A	109.4

N21C26H26B	109.4

C25C26H26B	109.4

H26AC26H26B	108.0

N21C27H27A	109.5

N21C27H27B	109.5

H27AC27H27B	109.5

N21C27H27C	109.5

H27AC27H27C	109.5

H27BC27H27C	109.5

C27N21C26	110.9(2)

C27N21C22	111.6(2)

C26N21C22	109.7(2)

C27N21H21	108.2

C26N21H21	108.2

C22N21H21	108.2

C25N24C23	110.6(2)

C25N24H24A	109.5

C23N24H24A	109.5

C25N24H24B	109.5

C23N24H24B	109.5

H24AN24H24B	108.1

O31BC31O31A	125.9(3)

O31BC31C32	119.9(3)

O31AC31C32	114.2(2)

O32C32C33	107.7(2)

O32C32C31	112.7(2)

C33C32C31	107.9(2)

O32C32H32	109.5

C33C32H32	109.5

C31C32H32	109.5

O33C33C34	112.4(2)

O33C33C32	110.9(2)

C34C33C32	107.3(2)

O33C33H33	108.7

C34C33H33	108.7

C32C33H33	108.7

O34BC34O34A	125.3(3)

O34BC34C33	121.6(3)

O34AC34C33	113.1(2)

C31O31AH31	109.5

C32O32H32O	109.5

C33O33H33O	109.5

N41C42C43	112.1(2)

N41C42H42A	109.2

C43C42H42A	109.2

N41C42H42B	109.2

C43C42H42B	109.2

H42AC42H42B	107.9

N44C43C42	110.9(2)

N44C43H43A	109.5

C42C43H43A	109.5

N44C43H43B	109.5

C42C43H43B	109.5

H43AC43H43B	108.0

N44C45C46	109.6(2)

N44C45H45A	109.7

C46C45H45A	109.7

N44C45H45B	109.7

C46C45H45B	109.7

H45AC45H45B	108.2

N41C46C45	110.5(2)

N41C46H46A	109.6

C45C46H46A	109.6

N41C46H46B	109.6

C45C46H46B	109.6

H46AC46H46B	108.1

N41C47H47A	109.5

N41C47H47B	109.5

H47AC47H47B	109.5

N41C47H47C	109.5

H47AC47H47C	109.5

H47BC47H47C	109.5

C47N41C42	110.1(2)

C47N41C46	110.2(2)

C42N41C46	110.3(2)

C47N41H41	108.7

C42N41H41	108.7

C46N41H41	108.7

C45N44C43	110.0(2)

C45N44H44A	109.7

C43N44H44A	109.7

C45N44H44B	109.7

C43N44H44B	109.7

H44AN44H44B	108.2

O51AC51O51B	124.1(3)

O51AC51C52	123.7(2)

O51BC51C52	112.3(2)

O52C52C51	112.4(2)

O52C52C53	107.2(2)

C51C52C53	110.5(2)

O52C52H52	108.9

C51C52H52	108.9

C53C52H52	108.9

O53C53C52	111.3(2)

O53C53C54	111.3(2)

C52C53C54	107.0(2)

O53C53H53	109.1

C52C53H53	109.1

C54C53H53	109.1

O54BC54O54A	126.4(3)

O54BC54C53	114.5(2)

O54AC54C53	119.1(2)

C51O51BH51	109.5

C52O52H52O	109.5

C53O53H53O	109.5

O61AC61O61B	125.6(3)

O61AC61C62	115.3(2)

O61BC61C62	119.1(2)

O62C62C61	111.2(2)

O62C62C63	109.4(2)

C61C62C63	107.7(2)

O62C62H62	109.5

C61C62H62	109.5

C63C62H62	109.5

O63C63C64	111.8(2)

O63C63C62	110.7(2)

C64C63C62	110.9(2)

O63C63H63	107.8

C64C63H63	107.8

C62C63H63	107.8

O64AC64O64B	124.9(3)

O64AC64C63	123.7(3)

O64BC64C63	111.3(2)

C62O62H62O	109.5

C63O63H63O	109.5

C64O64BH64	109.5

H1WO1WH2W	106(3)

H21WO2WH22W	104(3)

H31WO3WH32W	110(3)

H41WO4WH42W	109(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	17(1) 	15(1)	16(1) 	4(1)	2(1) 	2(1)

C2	15(1) 	13(1)	18(1) 	0(1)	0(1) 	1(1)

C3	14(1) 	17(1)	16(1) 	1(1)	0(1) 	1(1)

C4	16(1) 	19(2)	19(2) 	3(1)	4(1) 	0(1)

O1A	14(1) 	21(1)	22(1) 	6(1)	0(1) 	3(1)

O1B	17(1) 	17(1)	20(1) 	1(1)	4(1) 	0(1)

O2	16(1) 	21(1)	17(1) 	3(1)	2(1) 	4(1)

O3	17(1) 	23(1)	19(1) 	2(1)	1(1) 	3(1)

O4B	15(1) 	20(1)	29(1) 	2(1)	2(1) 	1(1)

O4A	18(1) 	24(1)	41(1) 	8(1)	9(1) 	3(1)

C22	24(2) 	20(2)	13(1) 	2(1)	0(1) 	1(1)

C23	19(2) 	19(1)	16(2) 	2(1)	5(1) 	2(1)

C25	21(2) 	17(1)	15(1) 	1(1)	5(1) 	4(1)

C26	17(2) 	20(2)	22(2) 	5(1)	4(1) 	0(1)

C27	20(2) 	24(2)	43(2) 	1(2)	11(2) 	4(1)

N21	17(1) 	13(1)	24(1) 	1(1)	1(1) 	1(1)

N24	16(1) 	17(1)	16(1) 	2(1)	0(1) 	0(1)

C31	20(2) 	20(2)	19(2) 	0(1)	1(1) 	1(1)

C32	15(1) 	16(1)	20(2) 	5(1)	1(1) 	2(1)

C33	16(1) 	20(2)	13(1) 	1(1)	2(1) 	5(1)

C34	17(1) 	12(1)	21(2) 	1(1)	1(1) 	0(1)

O31A	12(1) 	33(1)	41(1) 	16(1)	2(1) 	2(1)

O31B	19(1) 	29(1)	28(1) 	12(1)	5(1) 	1(1)

O32	19(1) 	16(1)	27(1) 	6(1)	3(1) 	1(1)

O33	24(1) 	38(1)	15(1) 	1(1)	0(1) 	21(1)

O34A	16(1) 	25(1)	18(1) 	0(1)	2(1) 	2(1)

O34B	23(1) 	22(1)	16(1) 	2(1)	6(1) 	6(1)

C42	18(2) 	15(1)	25(2) 	0(1)	3(1) 	2(1)

C43	22(2) 	21(2)	22(2) 	4(1)	5(1) 	1(1)

C45	16(2) 	22(2)	27(2) 	2(1)	3(1) 	3(1)

C46	20(2) 	17(1)	22(2) 	4(1)	0(1) 	1(1)

C47	25(2) 	30(2)	22(2) 	1(1)	7(1) 	12(1)

N41	18(1) 	16(1)	17(1) 	1(1)	2(1) 	4(1)

N44	21(1) 	19(1)	20(1) 	1(1)	2(1) 	5(1)

C51	15(1) 	18(1)	17(2) 	4(1)	2(1) 	4(1)

C52	19(2) 	12(1)	16(1) 	1(1)	2(1) 	2(1)

C53	14(1) 	15(1)	16(1) 	1(1)	2(1) 	0(1)

C54	13(1) 	14(1)	21(2) 	1(1)	2(1) 	2(1)

O51A	40(1) 	19(1)	25(1) 	5(1)	11(1) 	3(1)

O51B	30(1) 	12(1)	27(1) 	4(1)	7(1) 	4(1)

O52	14(1) 	16(1)	29(1) 	5(1)	0(1) 	0(1)

O53	18(1) 	16(1)	16(1) 	1(1)	3(1) 	4(1)

O54A	19(1) 	13(1)	23(1) 	1(1)	1(1) 	0(1)

O54B	41(1) 	19(1)	20(1) 	4(1)	2(1) 	2(1)

C61	8(1) 	17(1)	19(2) 	2(1)	1(1) 	0(1)

C62	16(1) 	15(1)	12(1) 	2(1)	0(1) 	1(1)

C63	16(1) 	14(1)	14(1) 	1(1)	3(1) 	2(1)

C64	14(1) 	14(1)	18(2) 	2(1)	5(1) 	1(1)

O61A	21(1) 	21(1)	17(1) 	3(1)	2(1) 	3(1)

O61B	26(1) 	12(1)	22(1) 	1(1)	3(1) 	1(1)

O62	15(1) 	16(1)	17(1) 	2(1)	3(1) 	3(1)

O63	14(1) 	19(1)	15(1) 	2(1)	0(1) 	1(1)

O64A	23(1) 	20(1)	21(1) 	4(1)	2(1) 	1(1)

O64B	28(1) 	12(1)	22(1) 	0(1)	5(1) 	4(1)

O1W	20(1) 	17(1)	18(1) 	0(1)	4(1) 	2(1)

O2W	14(1) 	18(1)	19(1) 	2(1)	0(1) 	2(1)

O3W	17(1) 	24(1)	26(1) 	2(1)	1(1) 	1(1)

O4W	18(1) 	26(1)	23(1) 	7(1)	2(1) 	0(1)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N21H21...O1W	0.93	1.87	2.772(3)	163.5

N41H41...O2W	0.93	2.04	2.897(3)	152.7

O32H32O...O3W	0.84	1.81	2.648(3)	179.8

O2H2O...O53	0.84	1.83	2.657(3)	166.8

O3H3O...O4W	0.84	1.88	2.687(3)	160.6

O52H52O...O61A	0.84	1.87	2.673(3)	159.9

O1WH1W...O1B	0.851(18)	1.862(19)	2.712(3)	177(3)

O1WH2W...O61A	0.842(18)	1.88(2)	2.710(3)	169(4)

O2WH21W...O54B	0.844(19)	1.76(2)	2.596(3)	172(5)

O3WH31W...O3	0.831(18)	1.890(19)	2.702(3)	165(4)

N44H44A...O61Bi	0.92	1.92	2.760(3)	150.1

N44H44A...O62i	0.92	2.31	2.973(3)	128.9

O4BH4...O1Ai	0.84	1.86	2.673(3)	161.9

O53H53O...O1Wi	0.84	1.93	2.742(3)	163.0

N44H44B...O32ii	0.92	2.07	2.775(3)	132.8

N44H44B...O31Aii	0.92	2.47	3.285(3)	147.4

N41H41...O64Aiii	0.93	2.45	2.986(3)	116.9

O2WH22W...O63iii	0.863(18)	1.877(19)	2.739(3)	177(4)

O4WH42W...O34Aiii	0.838(19)	2.01(3)	2.756(3)	149(3)

N24H24A...O54Aiv	0.92	2.08	2.949(3)	157.4

N24H24B...O1Biv	0.92	1.87	2.739(3)	155.5

N24H24B...O2iv	0.92	2.30	2.809(3)	114.8

O51BH51...O54Aiv	0.84	1.72	2.557(3)	177.0

O64BH64...O61Biv	0.84	1.78	2.610(3)	169.1

O31AH31...O34Av	0.84	1.63	2.463(3)	171.8

O3WH32W...O4Av	0.834(19)	2.00(2)	2.817(3)	166(4)

O33H33O...O62vi	0.84	2.05	2.732(3)	138.5

O62H62O...O2Wvii	0.84	1.85	2.683(3)	170.6

O63H63O...O34Bviii	0.84	1.88	2.643(3)	150.6

O4WH41W...O31Bix	0.836(19)	1.98(3)	2.771(3)	159(4)

Symmetry transformations used to generate equivalent atoms:

(i) x1,y,z    (ii) x1,y,z+1    (iii) x,y+1,z    (iv)  x,y1,z

(v) x+1,y,z    (vi) x,y,z1    (vii) x+1,y1,z    (viii) x,y,z+1

(xi) x1,y+1,z