|  | # Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2008src0992  (SEH95)

Empirical formula 	C5H3MoNdO8S

Formula weight 	463.31

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P1

Unit cell dimensions	a = 7.2720(15) Å	 = 86.13(3)°

b = 7.4040(15) Å	 = 78.47(3)°

c = 18.131(4) Å	  = 89.29(3)°

Volume	954.3(3) Å3

Z	4

Density (calculated)	3.225 Mg / m3

Absorption coefficient	6.937 mm1

F(000)	860

Crystal	needle; purple

Crystal size	0.14  0.02  0.01 mm3

 range for data collection	3.06  27.48°

Index ranges	9  h  9, 9  k  9, 23  l  23

Reflections collected	16689

Independent reflections	4360 [Rint = 0.0885]

Completeness to  = 27.48°	99.3 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9339 and 0.4434

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4360 / 148 / 277

Goodness-of-fit on F2	1.070

Final R indices [F2 > 2(F2)]	R1 = 0.0728, wR2 = 0.1527

R indices (all data)	R1 = 0.1004, wR2 = 0.1692

Largest diff. peak and hole	4.769 and 2.255 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

Additional symmetry along the b axis was investigated and found to be only pseudo.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2090(20)	4390(20)	8763(9)	18(3)	1

C2	180(20)	4160(20)	9050(8)	16(3)	1

C3	600(20)	4650(20)	9772(9)	19(3)	1

C5	2480(30)	4320(30)	10105(11)	32(4)	1

C6	3250(20)	5234(19)	9185(10)	23(3)	1

C21	900(20)	8990(20)	8820(8)	16(3)	1

C22	2580(30)	8950(20)	9389(10)	28(3)	1

C23	2550(20)	9460(20)	10095(10)	24(3)	1

C24	810(20)	10050(20)	10263(8)	17(3)	1

C26	750(20)	9440(20)	9007(9)	18(3)	1

O1	4568(15)	2337(14)	8020(6)	19(2)	1

O2	1701(14)	2913(15)	7548(6)	18(2)	1

O3	4043(16)	5279(14)	7461(6)	20(2)	1

O21	2574(15)	7244(14)	8003(6)	19(2)	1

O22	725(14)	7699(15)	7573(6)	16(2)	1

O23	1373(15)	205(14)	7509(6)	19(2)	1

O30	4442(14)	8894(14)	7484(6)	16(2)	1

O31	1945(14)	3777(14)	7520(6)	17(2)	1

O32	2924(14)	2235(14)	6247(6)	16(1)	1

O33	323(14)	5653(14)	6234(6)	16(2)	1

O34	4013(15)	4455(14)	5938(6)	17(2)	1

O35	752(14)	2843(14)	5157(5)	14(2)	1

O36	3399(14)	748(14)	6236(5)	14(2)	1

O37	4037(15)	7951(14)	5154(6)	19(2)	1

O38	6678(14)	7364(14)	6220(6)	16(1)	1

O39	126(14)	657(14)	5982(6)	16(1)	1

S1	3164(5)	3674(5)	7885(2)	14(1)	1

S2	1034(5)	8482(5)	7907(2)	14(1)	1

Mo1	5152(2)	2380(2)	5807(1)	12(1)	1

Mo2	946(2)	7372(2)	5802(1)	12(1)	1

Nd1	184(1)	2361(1)	6494(1)	13(1)	1

Nd2	3299(1)	7438(1)	6469(1)	13(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1C2	1.39(2)

C1C6	1.42(2)

C1S1	1.741(16)

C2C3	1.39(2)

C2H2	0.9500

C3C5	1.40(2)

C3C3i	1.44(3)

C5C6i	1.36(3)

C5H5	0.9500

C6C5i	1.36(3)

C6H6	0.9500

C21C26	1.36(2)

C21C22	1.43(2)

C21S2	1.745(15)

C22C23	1.36(2)

C22H22	0.9500

C23C24	1.44(2)

C23H23	0.9500

C24C24ii	1.36(3)

C24C26ii	1.41(2)

C26C24ii	1.41(2)

C26H26	0.9500

O1S1	1.459(11)

O2S1	1.463(11)

O2Nd1	2.450(10)

O3S1	1.452(11)

O3Nd2	2.462(11)

O21S2	1.432(11)

O22S2	1.435(11)

O22Nd2	2.469(10)

O23S2iii	1.466(11)

O23Nd1	2.456(11)

O30Nd2	2.478(10)

O31Nd1	2.456(10)

O32Mo1iv	1.743(10)

O32Nd1	2.394(10)

O33Mo2	1.791(11)

O33Nd1	2.451(10)

O33Nd2	2.670(10)

O34Mo1	1.744(10)

O34Nd2	2.476(10)

O35Mo2v	1.734(10)

O35Nd1	2.379(10)

O36Mo1	1.790(10)

O36Nd2iii	2.458(10)

O36Nd1	2.584(10)

O37Mo1vi	1.757(10)

O37Nd2	2.342(10)

O38Mo2vii	1.742(10)

O38Nd2	2.409(10)

O39Mo2iii	1.743(10)

O39Nd1	2.480(10)

O39Nd2iii	2.943(11)

S2O23viii	1.466(11)

Mo1O32vii	1.743(10)

Mo1O37vi	1.757(10)

Mo1Nd1	3.5779(17)

Mo2O35v	1.734(10)

Mo2O38iv	1.742(10)

Mo2O39viii	1.743(10)

Mo2Nd2	3.5350(16)

Nd2O36viii	2.458(11)

Nd2O39viii	2.943(11)

C2C1C6	120.4(15)

C2C1S1	122.2(12)

C6C1S1	117.4(12)

C1C2C3	120.6(13)

C1C2H2	119.7

C3C2H2	119.7

C2C3C5	122.5(15)

C2C3C3i	118.8(18)

C5C3C3i	118.3(19)

C6iC5C3	122.8(18)

C6iC5H5	118.6

C3C5H5	118.6

C5iC6C1	118.6(17)

C5iC6H6	120.7

C1C6H6	120.7

C26C21C22	119.1(14)

C26C21S2	121.9(12)

C22C21S2	119.1(12)

C23C22C21	120.6(16)

C23C22H22	119.7

C21C22H22	119.7

C22C23C24	119.2(15)

C22C23H23	120.4

C24C23H23	120.4

C24iiC24C26ii	120.0(19)

C24iiC24C23	119.8(19)

C26iiC24C23	119.9(14)

C21C26C24ii	121.0(14)

C21C26H26	119.5

C24iiC26H26	119.5

S1O2Nd1	153.7(7)

S1O3Nd2	135.9(6)

S2O22Nd2	149.4(7)

S2iiiO23Nd1	140.8(7)

Mo1ivO32Nd1	163.2(6)

Mo2O33Nd1	137.8(5)

Mo2O33Nd2	103.1(4)

Nd1O33Nd2	118.7(4)

Mo1O34Nd2	156.8(6)

Mo2vO35Nd1	165.2(6)

Mo1O36Nd2iii	135.5(5)

Mo1O36Nd1	108.4(5)

Nd2iiiO36Nd1	115.5(4)

Mo1viO37Nd2	161.6(6)

Mo2viiO38Nd2	165.4(6)

Mo2iiiO39Nd1	154.7(6)

Mo2iiiO39Nd2iii	94.5(4)

Nd1O39Nd2iii	103.4(3)

O3S1O1	111.0(7)

O3S1O2	113.1(6)

O1S1O2	112.5(6)

O3S1C1	105.6(7)

O1S1C1	106.5(7)

O2S1C1	107.6(7)

O21S2O22	113.0(6)

O21S2O23viii	113.1(7)

O22S2O23viii	111.6(7)

O21S2C21	104.7(7)

O22S2C21	107.7(7)

O23viiiS2C21	106.0(7)

O32viiMo1O34	111.0(5)

O32viiMo1O37vi	107.8(5)

O34Mo1O37vi	111.7(5)

O32viiMo1O36	110.8(5)

O34Mo1O36	104.0(5)

O37viMo1O36	111.5(5)

O32viiMo1Nd1	133.5(3)

O34Mo1Nd1	61.8(3)

O37viMo1Nd1	117.5(4)

O36Mo1Nd1	43.3(3)

O35vMo2O38iv	108.2(5)

O35vMo2O39viii	111.9(5)

O38ivMo2O39viii	110.4(5)

O35vMo2O33	112.5(5)

O38ivMo2O33	111.9(5)

O39viiiMo2O33	102.0(5)

O35vMo2Nd2	116.5(3)

O38ivMo2Nd2	135.2(3)

O39viiiMo2Nd2	56.1(3)

O33Mo2Nd2	47.4(3)

O35Nd1O32	78.2(3)

O35Nd1O2	139.4(3)

O32Nd1O2	138.4(3)

O35Nd1O33	74.4(3)

O32Nd1O33	91.8(3)

O2Nd1O33	85.4(4)

O35Nd1O31	133.2(4)

O32Nd1O31	72.2(3)

O2Nd1O31	67.6(3)

O33Nd1O31	71.3(3)

O35Nd1O23	140.5(3)

O32Nd1O23	77.9(4)

O2Nd1O23	76.4(4)

O33Nd1O23	137.1(3)

O31Nd1O23	65.9(4)

O35Nd1O39	73.2(3)

O32Nd1O39	77.6(3)

O2Nd1O39	122.9(4)

O33Nd1O39	147.3(3)

O31Nd1O39	131.5(3)

O23Nd1O39	71.3(3)

O35Nd1O36	83.6(3)

O32Nd1O36	142.3(3)

O2Nd1O36	73.3(3)

O33Nd1O36	114.8(3)

O31Nd1O36	139.9(3)

O23Nd1O36	96.9(3)

O39Nd1O36	65.5(3)

O35Nd1Mo1	71.9(2)

O32Nd1Mo1	149.3(2)

O2Nd1Mo1	72.0(2)

O33Nd1Mo1	86.6(2)

O31Nd1Mo1	134.9(2)

O23Nd1Mo1	122.5(3)

O39Nd1Mo1	87.4(2)

O36Nd1Mo1	28.3(2)

O37Nd2O38	78.1(4)

O37Nd2O36viii	74.8(3)

O38Nd2O36viii	89.8(3)

O37Nd2O3	139.3(4)

O38Nd2O3	76.0(4)

O36viiiNd2O3	135.3(3)

O37Nd2O22	142.4(4)

O38Nd2O22	137.3(3)

O36viiiNd2O22	90.5(3)

O3Nd2O22	74.1(4)

O37Nd2O34	73.0(4)

O38Nd2O34	77.3(3)

O36viiiNd2O34	147.1(3)

O3Nd2O34	71.1(4)

O22Nd2O34	119.5(4)

O37Nd2O30	131.5(4)

O38Nd2O30	70.7(3)

O36viiiNd2O30	69.0(3)

O3Nd2O30	66.2(4)

O22Nd2O30	69.6(3)

O34Nd2O30	131.3(4)

O37Nd2O33	85.2(3)

O38Nd2O33	142.0(3)

O36viiiNd2O33	118.6(3)

O3Nd2O33	96.4(3)

O22Nd2O33	71.6(3)

O34Nd2O33	65.1(3)

O30Nd2O33	140.6(3)

O37Nd2O39viii	71.8(3)

O38Nd2O39viii	141.8(3)

O36viiiNd2O39viii	60.2(3)

O3Nd2O39viii	141.8(3)

O22Nd2O39viii	70.9(3)

O34Nd2O39viii	114.3(3)

O30Nd2O39viii	113.6(3)

O33Nd2O39viii	58.3(3)

O37Nd2Mo2	72.3(3)

O38Nd2Mo2	149.6(2)

O36viiiNd2Mo2	89.2(2)

O3Nd2Mo2	123.6(3)

O22Nd2Mo2	73.1(2)

O34Nd2Mo2	87.3(2)

O30Nd2Mo2	136.1(2)

O33Nd2Mo2	29.6(2)

O39viiiNd2Mo2	29.5(2)

Symmetry transformations used to generate equivalent atoms:

(i) x,y+1,z+2    (ii) x,y+2,z+2    (iii) x,y1,z

(iv)  x1,y,z    (v) x,y+1,z+1    (vi) x+1,y+1,z+1

(vii) x+1,y,z    (viii) x,y+1,z

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	23(6) 	14(7)	18(6) 	1(5)	4(5) 	4(5)

C2	25(6) 	18(7)	9(6) 	1(5)	11(4) 	4(6)

C3	22(7) 	17(7)	17(7) 	5(6)	5(5) 	4(6)

C5	23(8) 	34(10)	38(10) 	2(8)	6(6) 	8(7)

C6	33(8) 	7(7)	30(8) 	7(6)	5(7) 	1(6)

C21	24(7) 	19(7)	6(5) 	7(5)	5(4) 	1(5)

C22	29(7) 	26(8)	27(7) 	5(7)	1(6) 	10(7)

C23	11(7) 	33(9)	29(7) 	16(7)	0(6) 	5(6)

C24	16(7) 	24(8)	10(7) 	1(6)	3(5) 	9(6)

C26	19(6) 	22(7)	13(7) 	7(6)	0(5) 	6(6)

O1	21(5) 	16(5)	20(6) 	1(4)	7(4) 	1(4)

O2	12(4) 	32(6)	11(4) 	0(4)	2(3) 	1(4)

O3	25(5) 	19(4)	17(5) 	4(4)	7(4) 	5(4)

O21	20(5) 	15(5)	20(6) 	3(4)	1(4) 	4(4)

O22	12(4) 	30(6)	6(4) 	5(4)	3(3) 	2(4)

O23	21(5) 	19(5)	15(5) 	1(4)	2(4) 	0(4)

O30	12(4) 	20(5)	16(5) 	4(4)	3(4) 	3(4)

O31	11(4) 	21(5)	16(5) 	4(4)	2(3) 	2(4)

O32	15(2) 	21(3)	10(3) 	0(2)	2(2) 	2(2)

O33	15(4) 	20(4)	11(5) 	1(3)	1(3) 	2(3)

O34	18(4) 	20(4)	12(5) 	4(3)	0(4) 	1(3)

O35	17(5) 	22(5)	5(4) 	1(3)	6(3) 	5(4)

O36	16(4) 	24(5)	2(4) 	2(3)	2(3) 	0(3)

O37	24(5) 	22(5)	8(4) 	0(4)	0(4) 	5(4)

O38	15(2) 	21(3)	10(3) 	0(2)	2(2) 	2(2)

O39	15(2) 	21(3)	10(3) 	0(2)	2(2) 	2(2)

S1	14(2) 	18(2)	11(2) 	1(1)	2(1) 	2(1)

S2	15(2) 	14(2)	10(2) 	1(1)	0(1) 	1(1)

Mo1	12(1) 	15(1)	9(1) 	1(1)	2(1) 	0(1)

Mo2	12(1) 	15(1)	10(1) 	1(1)	2(1) 	0(1)

Nd1	14(1) 	14(1)	10(1) 	2(1)	3(1) 	1(1)

Nd2	13(1) 	15(1)	10(1) 	2(1)	1(1) 	0(1)