Table 1.  Crystal data and structure refinement for 2008src0895r.

Identification code 	2008src0895r

Empirical formula 	C34 H36 Mn3 N3 O19 S2

Formula weight 	1019.60

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 12.183 Å	a= 96.11º.

b = 12.325 Å	b= 106.87º.

c = 16.518 Å	g = 114.86º.

Volume	2077.8 Å3

Z	2

Density (calculated)	1.630 Mg/m3

Absorption coefficient	1.079 mm-1

F(000)	1040

Crystal size	0.20 x 0.14 x 0.06 mm3

Theta range for data collection	3.09 to 27.50º.

Index ranges	-15<=h<=15, -15<=k<=16, -21<=l<=21

Reflections collected	48531

Independent reflections	9473 [R(int) = 0.0498]

Completeness to theta = 27.50º	99.4 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9381 and 0.8131

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9473 / 21 / 601

Goodness-of-fit on F2	1.054

Final R indices [I>2sigma(I)]	R1 = 0.0426, wR2 = 0.1118

R indices (all data)	R1 = 0.0568, wR2 = 0.1201

Largest diff. peak and hole	1.435 and -0.771 e.Å-3

Table 2.  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2x 103)

for 2008src0895r.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

C(1)	4169(3)	9169(3)	3106(2)	22(1)

C(2)	4787(3)	10465(3)	3223(2)	26(1)

C(3)	4073(3)	11090(3)	3027(2)	31(1)

C(4)	2719(4)	10450(3)	2703(2)	33(1)

C(5)	2091(3)	9176(3)	2588(2)	28(1)

C(6)	2790(3)	8520(3)	2783(2)	21(1)

C(7)	2049(3)	7191(3)	2642(2)	20(1)

C(8)	-19(3)	2009(2)	3149(2)	19(1)

C(9)	-1392(3)	1360(3)	2844(2)	26(1)

C(10)	-2008(3)	322(3)	3115(2)	30(1)

C(11)	-1308(3)	-115(3)	3680(2)	36(1)

C(12)	29(3)	489(3)	3972(2)	32(1)

C(13)	693(3)	1560(2)	3718(2)	20(1)

C(14)	2098(3)	2209(2)	4117(2)	19(1)

C(15)	7493(3)	4678(3)	4207(2)	20(1)

C(16)	8037(3)	3877(3)	4302(2)	26(1)

C(17)	9051(3)	4040(3)	4021(2)	33(1)

C(18)	9534(3)	4979(3)	3631(2)	36(1)

C(19)	9023(3)	5782(3)	3535(2)	34(1)

C(20)	7991(3)	5649(3)	3816(2)	25(1)

C(21)	7541(3)	6555(3)	3722(2)	25(1)

C(22)	3556(3)	3348(2)	2126(2)	18(1)

C(23)	3605(3)	2740(3)	1335(2)	21(1)

C(24)	2656(3)	2050(3)	526(2)	23(1)

C(25)	700(3)	1361(4)	-648(2)	43(1)

C(26)	979(3)	414(4)	-1035(2)	44(1)

C(27)	3130(3)	1601(3)	-48(2)	24(1)

C(28)	4436(3)	1949(3)	313(2)	25(1)

C(29)	5238(3)	1662(3)	-84(2)	26(1)

C(30)	6574(3)	2125(3)	280(2)	30(1)

C(31)	8717(3)	3477(3)	1237(2)	39(1)

C(32)	9023(3)	2473(4)	951(2)	40(1)

C(33)	7065(3)	1594(3)	-238(2)	31(1)

C(34)	6117(3)	750(3)	-985(2)	33(1)

O(1)	4922(2)	8631(2)	3297(1)	23(1)

O(2)	1683(2)	5241(2)	2651(1)	19(1)

O(3)	545(2)	3029(2)	2901(1)	22(1)

O(4)	4131(2)	3751(2)	4514(1)	15(1)

O(5)	6553(2)	4520(2)	4521(1)	18(1)

O(6)	6275(2)	7450(2)	3827(1)	20(1)

O(7)	3979(2)	5473(2)	3674(1)	15(1)

O(8)	2498(2)	3360(2)	2076(1)	21(1)

O(9)	4577(2)	3798(2)	2804(1)	19(1)

O(10)	1384(2)	1803(2)	290(1)	29(1)

O(11)	2351(2)	895(2)	-900(1)	32(1)

O(12)	8364(2)	1927(2)	12(2)	39(1)

O(13)	7337(2)	2974(2)	1076(2)	38(1)

O(14)	3311(4)	18(4)	4869(2)	80(1)

O(15)	2124(3)	4678(3)	627(2)	58(1)

O(16)	6732(3)	7125(3)	1820(2)	57(1)

O(17)	6362(8)	5233(4)	440(4)	60(2)

O(18)	4396(2)	6336(2)	2083(2)	35(1)

O(19)	9677(7)	4075(6)	-532(5)	66(2)

O(20)	4368(2)	7699(2)	4733(1)	24(1)

S(1)	5089(1)	2830(1)	1389(1)	23(1)

S(2)	4612(1)	579(1)	-1068(1)	33(1)

N(1)	2555(2)	6483(2)	2850(1)	17(1)

N(2)	2815(2)	3246(2)	3997(1)	15(1)

N(3)	6511(2)	6455(2)	3852(1)	17(1)

Mn(1)	5261(1)	4979(1)	4080(1)	13(1)

Mn(2)	2283(1)	4180(1)	3176(1)	14(1)

Mn(3)	4462(1)	7010(1)	3402(1)	16(1)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [º] for 2008src0895r.

_____________________________________________________

C(1)-O(1) 	1.330(3)

C(1)-C(2) 	1.412(4)

C(1)-C(6) 	1.416(4)

C(2)-C(3) 	1.381(4)

C(3)-C(4) 	1.391(5)

C(4)-C(5) 	1.389(4)

C(5)-C(6) 	1.400(4)

C(6)-C(7) 	1.450(4)

C(7)-N(1) 	1.286(4)

C(8)-O(3) 	1.330(3)

C(8)-C(13) 	1.408(4)

C(8)-C(9) 	1.412(4)

C(9)-C(10) 	1.381(4)

C(10)-C(11) 	1.385(5)

C(11)-C(12) 	1.374(5)

C(12)-C(13) 	1.411(4)

C(13)-C(14) 	1.444(4)

C(14)-N(2) 	1.285(3)

C(15)-O(5) 	1.341(3)

C(15)-C(16) 	1.399(4)

C(15)-C(20) 	1.414(4)

C(16)-C(17) 	1.388(4)

C(17)-C(18) 	1.380(5)

C(18)-C(19) 	1.374(5)

C(19)-C(20) 	1.414(4)

C(20)-C(21) 	1.441(4)

C(21)-N(3) 	1.292(4)

C(22)-O(9) 	1.260(3)

C(22)-O(8) 	1.274(3)

C(22)-C(23) 	1.464(4)

C(23)-C(24) 	1.372(4)

C(23)-S(1) 	1.740(3)

C(24)-O(10) 	1.369(3)

C(24)-C(27) 	1.417(4)

C(25)-O(10) 	1.443(4)

C(25)-C(26) 	1.479(5)

C(26)-O(11) 	1.456(4)

C(27)-C(28) 	1.376(4)

C(27)-O(11) 	1.382(3)

C(28)-C(29) 	1.458(4)

C(28)-S(1) 	1.735(3)

C(29)-C(30) 	1.383(4)

C(29)-S(2) 	1.722(3)

C(30)-O(13) 	1.367(4)

C(30)-C(33) 	1.423(4)

C(31)-O(13) 	1.452(4)

C(31)-C(32) 	1.503(5)

C(32)-O(12) 	1.451(4)

C(33)-C(34) 	1.353(5)

C(33)-O(12) 	1.371(4)

C(34)-S(2) 	1.717(3)

O(1)-Mn(3) 	1.8771(19)

O(2)-N(1) 	1.380(3)

O(2)-Mn(2) 	1.9162(19)

O(3)-Mn(2) 	1.8660(19)

O(4)-N(2) 	1.393(3)

O(4)-Mn(1) 	1.9380(18)

O(4)-Mn(1)#1 	2.3756(18)

O(5)-Mn(1) 	1.8717(18)

O(6)-N(3) 	1.375(3)

O(6)-Mn(3) 	1.9167(19)

O(7)-Mn(2) 	1.8571(17)

O(7)-Mn(3) 	1.8801(18)

O(7)-Mn(1) 	1.8815(18)

O(8)-Mn(2) 	2.1201(19)

O(9)-Mn(1) 	2.1357(18)

O(18)-Mn(3) 	2.214(2)

O(20)-Mn(3) 	2.324(2)

N(1)-Mn(3) 	2.007(2)

N(2)-Mn(2) 	2.009(2)

N(3)-Mn(1) 	1.979(2)

Mn(1)-O(4)#1 	2.3756(18)

Mn(1)-Mn(2) 	3.1462(5)

Mn(1)-Mn(3) 	3.2374(5)

O(1)-C(1)-C(2)	117.7(3)

O(1)-C(1)-C(6)	124.0(2)

C(2)-C(1)-C(6)	118.3(3)

C(3)-C(2)-C(1)	121.3(3)

C(2)-C(3)-C(4)	120.4(3)

C(5)-C(4)-C(3)	119.3(3)

C(4)-C(5)-C(6)	121.5(3)

C(5)-C(6)-C(1)	119.3(3)

C(5)-C(6)-C(7)	117.5(3)

C(1)-C(6)-C(7)	123.3(2)

N(1)-C(7)-C(6)	124.4(3)

O(3)-C(8)-C(13)	122.9(2)

O(3)-C(8)-C(9)	118.6(3)

C(13)-C(8)-C(9)	118.4(3)

C(10)-C(9)-C(8)	120.0(3)

C(9)-C(10)-C(11)	121.5(3)

C(12)-C(11)-C(10)	119.4(3)

C(11)-C(12)-C(13)	120.7(3)

C(8)-C(13)-C(12)	119.8(3)

C(8)-C(13)-C(14)	122.5(2)

C(12)-C(13)-C(14)	117.5(3)

N(2)-C(14)-C(13)	123.8(3)

O(5)-C(15)-C(16)	118.5(3)

O(5)-C(15)-C(20)	122.7(2)

C(16)-C(15)-C(20)	118.8(3)

C(17)-C(16)-C(15)	120.5(3)

C(18)-C(17)-C(16)	121.0(3)

C(19)-C(18)-C(17)	119.6(3)

C(18)-C(19)-C(20)	121.0(3)

C(15)-C(20)-C(19)	119.0(3)

C(15)-C(20)-C(21)	123.2(2)

C(19)-C(20)-C(21)	117.7(3)

N(3)-C(21)-C(20)	123.5(3)

O(9)-C(22)-O(8)	125.9(2)

O(9)-C(22)-C(23)	116.0(2)

O(8)-C(22)-C(23)	118.1(2)

C(24)-C(23)-C(22)	131.6(3)

C(24)-C(23)-S(1)	110.8(2)

C(22)-C(23)-S(1)	117.6(2)

O(10)-C(24)-C(23)	124.3(3)

O(10)-C(24)-C(27)	123.0(2)

C(23)-C(24)-C(27)	112.7(3)

O(10)-C(25)-C(26)	111.4(3)

O(11)-C(26)-C(25)	112.6(3)

C(28)-C(27)-O(11)	122.9(3)

C(28)-C(27)-C(24)	114.2(2)

O(11)-C(27)-C(24)	122.9(3)

C(27)-C(28)-C(29)	128.9(3)

C(27)-C(28)-S(1)	109.9(2)

C(29)-C(28)-S(1)	121.2(2)

C(30)-C(29)-C(28)	126.6(3)

C(30)-C(29)-S(2)	109.6(2)

C(28)-C(29)-S(2)	123.6(2)

O(13)-C(30)-C(29)	123.1(3)

O(13)-C(30)-C(33)	123.4(3)

C(29)-C(30)-C(33)	113.5(3)

O(13)-C(31)-C(32)	110.9(3)

O(12)-C(32)-C(31)	110.8(3)

C(34)-C(33)-O(12)	125.1(3)

C(34)-C(33)-C(30)	112.5(3)

O(12)-C(33)-C(30)	122.4(3)

C(33)-C(34)-S(2)	111.6(2)

C(1)-O(1)-Mn(3)	128.81(18)

N(1)-O(2)-Mn(2)	118.45(15)

C(8)-O(3)-Mn(2)	132.84(18)

N(2)-O(4)-Mn(1)	113.04(14)

N(2)-O(4)-Mn(1)#1	113.88(13)

Mn(1)-O(4)-Mn(1)#1	98.55(7)

C(15)-O(5)-Mn(1)	124.09(17)

N(3)-O(6)-Mn(3)	114.14(15)

Mn(2)-O(7)-Mn(3)	122.28(10)

Mn(2)-O(7)-Mn(1)	114.61(9)

Mn(3)-O(7)-Mn(1)	118.78(9)

C(22)-O(8)-Mn(2)	122.04(17)

C(22)-O(9)-Mn(1)	135.47(17)

C(24)-O(10)-C(25)	111.9(2)

C(27)-O(11)-C(26)	110.8(2)

C(33)-O(12)-C(32)	110.4(2)

C(30)-O(13)-C(31)	112.2(2)

C(28)-S(1)-C(23)	92.50(14)

C(34)-S(2)-C(29)	92.79(15)

C(7)-N(1)-O(2)	115.5(2)

C(7)-N(1)-Mn(3)	126.37(19)

O(2)-N(1)-Mn(3)	118.08(16)

C(14)-N(2)-O(4)	113.3(2)

C(14)-N(2)-Mn(2)	128.72(18)

O(4)-N(2)-Mn(2)	117.97(15)

C(21)-N(3)-O(6)	117.1(2)

C(21)-N(3)-Mn(1)	124.7(2)

O(6)-N(3)-Mn(1)	118.20(15)

O(5)-Mn(1)-O(7)	178.08(8)

O(5)-Mn(1)-O(4)	89.84(8)

O(7)-Mn(1)-O(4)	89.84(8)

O(5)-Mn(1)-N(3)	90.94(9)

O(7)-Mn(1)-N(3)	89.01(8)

O(4)-Mn(1)-N(3)	168.97(8)

O(5)-Mn(1)-O(9)	91.91(8)

O(7)-Mn(1)-O(9)	90.01(7)

O(4)-Mn(1)-O(9)	96.00(8)

N(3)-Mn(1)-O(9)	94.97(8)

O(5)-Mn(1)-O(4)#1	91.09(7)

O(7)-Mn(1)-O(4)#1	86.99(7)

O(4)-Mn(1)-O(4)#1	81.45(7)

N(3)-Mn(1)-O(4)#1	87.54(8)

O(9)-Mn(1)-O(4)#1	176.06(7)

O(5)-Mn(1)-Mn(2)	148.47(6)

O(7)-Mn(1)-Mn(2)	32.46(5)

O(4)-Mn(1)-Mn(2)	65.50(5)

N(3)-Mn(1)-Mn(2)	117.10(6)

O(9)-Mn(1)-Mn(2)	72.64(5)

O(4)#1-Mn(1)-Mn(2)	103.51(4)

O(5)-Mn(1)-Mn(3)	149.10(6)

O(7)-Mn(1)-Mn(3)	30.60(5)

O(4)-Mn(1)-Mn(3)	118.97(5)

N(3)-Mn(1)-Mn(3)	58.60(6)

O(9)-Mn(1)-Mn(3)	95.57(5)

O(4)#1-Mn(1)-Mn(3)	83.12(4)

Mn(2)-Mn(1)-Mn(3)	61.673(12)

O(7)-Mn(2)-O(3)	167.13(9)

O(7)-Mn(2)-O(2)	90.95(8)

O(3)-Mn(2)-O(2)	88.13(8)

O(7)-Mn(2)-N(2)	88.63(8)

O(3)-Mn(2)-N(2)	88.83(8)

O(2)-Mn(2)-N(2)	164.47(9)

O(7)-Mn(2)-O(8)	96.41(8)

O(3)-Mn(2)-O(8)	96.44(8)

O(2)-Mn(2)-O(8)	97.84(8)

N(2)-Mn(2)-O(8)	97.63(8)

O(7)-Mn(2)-Mn(1)	32.94(5)

O(3)-Mn(2)-Mn(1)	149.26(6)

O(2)-Mn(2)-Mn(1)	122.49(6)

N(2)-Mn(2)-Mn(1)	61.01(6)

O(8)-Mn(2)-Mn(1)	82.89(5)

O(1)-Mn(3)-O(7)	170.89(9)

O(1)-Mn(3)-O(6)	88.84(8)

O(7)-Mn(3)-O(6)	92.73(8)

O(1)-Mn(3)-N(1)	91.87(9)

O(7)-Mn(3)-N(1)	87.38(8)

O(6)-Mn(3)-N(1)	174.81(9)

O(1)-Mn(3)-O(18)	93.67(9)

O(7)-Mn(3)-O(18)	95.38(9)

O(6)-Mn(3)-O(18)	86.90(9)

N(1)-Mn(3)-O(18)	87.92(9)

O(1)-Mn(3)-O(20)	85.65(8)

O(7)-Mn(3)-O(20)	85.25(8)

O(6)-Mn(3)-O(20)	97.56(8)

N(1)-Mn(3)-O(20)	87.62(8)

O(18)-Mn(3)-O(20)	175.47(9)

O(1)-Mn(3)-Mn(1)	150.62(6)

O(7)-Mn(3)-Mn(1)	30.62(5)

O(6)-Mn(3)-Mn(1)	62.28(6)

N(1)-Mn(3)-Mn(1)	117.39(6)

O(18)-Mn(3)-Mn(1)	90.20(7)

O(20)-Mn(3)-Mn(1)	92.59(5)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y+1,-z+1

Table 4.   Anisotropic displacement parameters (Å2x 103)for 2008src0895r.  The anisotropic

displacement factor exponent takes the form: -2p2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

C(1)	32(2) 	17(1)	19(1) 	7(1)	11(1) 	14(1)

C(2)	35(2) 	19(1)	22(1) 	6(1)	8(1) 	11(1)

C(3)	50(2) 	17(1)	24(2) 	5(1)	11(1) 	17(1)

C(4)	53(2) 	29(2)	29(2) 	11(1)	14(2) 	30(2)

C(5)	37(2) 	29(2)	27(2) 	8(1)	10(1) 	22(1)

C(6)	28(2) 	19(1)	20(1) 	7(1)	9(1) 	14(1)

C(7)	19(1) 	21(1)	23(1) 	7(1)	9(1) 	11(1)

C(8)	16(1) 	16(1)	23(1) 	2(1)	9(1) 	4(1)

C(9)	17(1) 	23(1)	31(2) 	2(1)	8(1) 	6(1)

C(10)	18(1) 	25(2)	37(2) 	2(1)	12(1) 	-1(1)

C(11)	26(2) 	23(2)	46(2) 	15(1)	15(2) 	-2(1)

C(12)	23(2) 	25(2)	36(2) 	13(1)	8(1) 	4(1)

C(13)	16(1) 	14(1)	23(1) 	3(1)	7(1) 	2(1)

C(14)	19(1) 	16(1)	19(1) 	3(1)	6(1) 	7(1)

C(15)	14(1) 	23(1)	19(1) 	-1(1)	4(1) 	9(1)

C(16)	24(2) 	23(1)	32(2) 	2(1)	9(1) 	13(1)

C(17)	26(2) 	36(2)	38(2) 	-3(1)	9(1) 	19(1)

C(18)	28(2) 	50(2)	41(2) 	7(2)	21(2) 	23(2)

C(19)	28(2) 	48(2)	38(2) 	16(2)	20(1) 	22(2)

C(20)	18(1) 	32(2)	28(2) 	7(1)	11(1) 	14(1)

C(21)	19(1) 	27(2)	32(2) 	13(1)	15(1) 	9(1)

C(22)	20(1) 	16(1)	17(1) 	4(1)	7(1) 	9(1)

C(23)	18(1) 	23(1)	20(1) 	3(1)	6(1) 	10(1)

C(24)	20(1) 	25(1)	20(1) 	2(1)	7(1) 	9(1)

C(25)	27(2) 	63(2)	24(2) 	-6(2)	1(1) 	18(2)

C(26)	30(2) 	52(2)	33(2) 	-11(2)	3(1) 	14(2)

C(27)	26(2) 	24(1)	17(1) 	0(1)	7(1) 	10(1)

C(28)	25(2) 	29(2)	17(1) 	0(1)	8(1) 	11(1)

C(29)	24(2) 	28(2)	27(2) 	2(1)	12(1) 	13(1)

C(30)	29(2) 	35(2)	23(2) 	3(1)	9(1) 	15(1)

C(31)	24(2) 	46(2)	36(2) 	2(2)	6(1) 	11(2)

C(32)	31(2) 	51(2)	33(2) 	6(2)	8(1) 	18(2)

C(33)	27(2) 	40(2)	28(2) 	9(1)	12(1) 	17(1)

C(34)	37(2) 	41(2)	25(2) 	5(1)	15(1) 	21(2)

O(1)	20(1) 	16(1)	33(1) 	11(1)	10(1) 	8(1)

O(2)	12(1) 	13(1)	29(1) 	6(1)	6(1) 	4(1)

O(3)	13(1) 	18(1)	33(1) 	9(1)	6(1) 	6(1)

O(4)	10(1) 	14(1)	18(1) 	3(1)	4(1) 	5(1)

O(5)	16(1) 	21(1)	22(1) 	6(1)	9(1) 	11(1)

O(6)	17(1) 	15(1)	30(1) 	10(1)	11(1) 	7(1)

O(7)	12(1) 	11(1)	20(1) 	4(1)	6(1) 	4(1)

O(8)	19(1) 	24(1)	20(1) 	0(1)	7(1) 	10(1)

O(9)	20(1) 	19(1)	18(1) 	1(1)	6(1) 	10(1)

O(10)	20(1) 	40(1)	21(1) 	-3(1)	4(1) 	12(1)

O(11)	26(1) 	38(1)	19(1) 	-7(1)	4(1) 	11(1)

O(12)	29(1) 	54(2)	33(1) 	7(1)	13(1) 	20(1)

O(13)	25(1) 	45(1)	33(1) 	-6(1)	6(1) 	12(1)

O(14)	59(2) 	91(3)	35(2) 	2(2)	13(2) 	-6(2)

O(15)	56(2) 	49(2)	47(2) 	20(1)	14(1) 	8(2)

O(16)	62(2) 	60(2)	51(2) 	21(2)	32(2) 	22(2)

O(17)	121(5) 	18(2)	43(3) 	8(2)	63(4) 	13(3)

O(18)	28(1) 	45(1)	27(1) 	3(1)	14(1) 	11(1)

O(19)	52(4) 	60(4)	67(4) 	30(3)	21(3) 	8(3)

O(20)	28(1) 	20(1)	23(1) 	5(1)	10(1) 	11(1)

S(1)	20(1) 	27(1)	19(1) 	0(1)	7(1) 	11(1)

S(2)	29(1) 	40(1)	24(1) 	-2(1)	7(1) 	16(1)

N(1)	17(1) 	14(1)	21(1) 	5(1)	9(1) 	7(1)

N(2)	11(1) 	15(1)	16(1) 	1(1)	5(1) 	4(1)

N(3)	15(1) 	18(1)	20(1) 	6(1)	8(1) 	8(1)

Mn(1)	11(1) 	13(1)	17(1) 	4(1)	6(1) 	5(1)

Mn(2)	10(1) 	12(1)	20(1) 	4(1)	6(1) 	5(1)

Mn(3)	13(1) 	12(1)	21(1) 	6(1)	7(1) 	5(1)

______________________________________________________________________________