|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	s92

Empirical formula 	C20H30Cl2FeN6O8

Formula weight 	609.25

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	?

Space group 	?

Unit cell dimensions	a = 19.0961(8) Å	 = 90°

b = 8.5356(5) Å	 = 115.869(4)°

c = 16.7145(7) Å	  = 90°

Volume	2451.4(2) Å3

Z	4

Density (calculated)	1.651 Mg / m3

Absorption coefficient	0.893 mm1

F(000)	1264

Crystal	?; ?

Crystal size	0.15  0.10  0.02 mm3

 range for data collection	3.22  25.02°

Index ranges	22  h  22, 10  k  10, 19  l  19

Reflections collected	12542

Independent reflections	2106 [Rint = 0.0620]

Completeness to  = 25.02°	97.0 %

Max. and min. transmission	0.9824 and 0.8777

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2106 / 0 / 169

Goodness-of-fit on F2	1.047

Final R indices [F2 > 2(F2)]	R1 = 0.0468, wR2 = 0.1104

R indices (all data)	R1 = 0.0600, wR2 = 0.1170

Extinction coefficient	0.0004(3)

Largest diff. peak and hole	0.705 and 0.599 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

O1	5509(2)	2946(4)	881(2)	54(1)	1

O2	6685(2)	2657(3)	2122(2)	41(1)	1

O3	6479(2)	4831(5)	1219(4)	113(2)	1

O4	5790(2)	4547(4)	2103(2)	71(1)	1

Cl1	6129(1)	3790(1)	1577(1)	35(1)	1

C1	3772(2)	252(4)	651(2)	20(1)	1

C2	3291(2)	882(4)	176(2)	24(1)	1

C3	2878(2)	97(4)	884(2)	26(1)	1

C4	2948(2)	1715(5)	773(2)	30(1)	1

C5	3426(2)	2343(4)	44(3)	29(1)	1

C6	3836(2)	1359(4)	758(2)	23(1)	1

C7	3700(2)	2075(4)	1727(2)	23(1)	1

C8	4743(2)	2333(4)	1234(2)	23(1)	1

C9	5397(2)	1404(4)	1182(2)	25(1)	1

C10	6500(2)	997(4)	2691(2)	25(1)	1

N1	4347(2)	1949(4)	1618(2)	34(1)	1

N2	4226(2)	1247(3)	1422(2)	19(1)	1

N3	5781(2)	351(3)	1964(2)	21(1)	1

Fe1	5000	251(1)	2500	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

O1Cl1	1.439(3)

O2Cl1	1.432(3)

O3Cl1	1.394(4)

O4Cl1	1.451(4)

C1C6	1.385(5)

C1C2	1.391(5)

C1N2	1.469(4)

C2C3	1.380(5)

C3C4	1.393(5)

C4C5	1.378(5)

C5C6	1.388(5)

C6N1	1.432(4)

C7N2	1.488(4)

C7C10i	1.504(5)

C8N2	1.484(4)

C8C9	1.513(5)

C9N3	1.489(4)

C10N3	1.486(4)

C10C7i	1.504(5)

N1Fe1	2.055(3)

N2Fe1	2.178(3)

N3Fe1	2.112(3)

Fe1N1i	2.055(3)

Fe1N3i	2.112(3)

Fe1N2i	2.178(3)

O3Cl1O2	109.9(2)

O3Cl1O1	110.6(3)

O2Cl1O1	107.28(19)

O3Cl1O4	113.6(3)

O2Cl1O4	108.6(2)

O1Cl1O4	106.6(2)

C6C1C2	119.6(3)

C6C1N2	118.4(3)

C2C1N2	121.9(3)

C3C2C1	120.1(3)

C2C3C4	120.0(3)

C5C4C3	120.1(3)

C4C5C6	119.8(3)

C1C6C5	120.4(3)

C1C6N1	117.5(3)

C5C6N1	122.1(3)

N2C7C10i	109.3(3)

N2C8C9	109.0(3)

N3C9C8	111.7(3)

N3C10C7i	110.6(3)

C6N1Fe1	114.0(2)

C1N2C8	111.6(2)

C1N2C7	110.3(2)

C8N2C7	112.7(2)

C1N2Fe1	108.30(19)

C8N2Fe1	105.52(18)

C7N2Fe1	108.11(19)

C10N3C9	114.8(3)

C10N3Fe1	108.3(2)

C9N3Fe1	110.50(19)

N1iFe1N1	90.32(17)

N1iFe1N3i	100.81(11)

N1Fe1N3i	98.95(11)

N1iFe1N3	98.95(11)

N1Fe1N3	100.81(11)

N3iFe1N3	151.84(16)

N1iFe1N2	171.04(11)

N1Fe1N2	80.80(11)

N3iFe1N2	81.86(10)

N3Fe1N2	81.72(10)

N1iFe1N2i	80.80(11)

N1Fe1N2i	171.04(11)

N3iFe1N2i	81.72(10)

N3Fe1N2i	81.86(10)

N2Fe1N2i	108.10(14)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z+1/2

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

O1	32(2) 	92(3)	28(2) 	8(2)	5(1) 	5(2)

O2	34(2) 	32(2)	45(2) 	7(1)	5(1) 	1(1)

O3	63(3) 	98(3)	167(5) 	90(3)	41(3) 	10(2)

O4	99(3) 	41(2)	65(2) 	16(2)	27(2) 	22(2)

Cl1	32(1) 	31(1)	34(1) 	9(1)	8(1) 	2(1)

C1	17(2) 	24(2)	21(2) 	3(1)	11(1) 	1(1)

C2	20(2) 	27(2)	25(2) 	1(1)	9(1) 	4(1)

C3	17(2) 	35(2)	26(2) 	2(2)	8(1) 	2(2)

C4	23(2) 	40(2)	32(2) 	13(2)	17(2) 	9(2)

C5	34(2) 	23(2)	41(2) 	7(2)	27(2) 	6(2)

C6	22(2) 	25(2)	28(2) 	2(1)	17(2) 	3(1)

C7	21(2) 	24(2)	21(2) 	2(1)	7(1) 	7(1)

C8	25(2) 	18(2)	23(2) 	4(1)	7(1) 	3(1)

C9	24(2) 	29(2)	22(2) 	1(1)	11(2) 	5(2)

C10	16(2) 	29(2)	29(2) 	4(2)	9(2) 	3(2)

N1	38(2) 	41(2)	30(2) 	13(1)	22(2) 	17(2)

N2	20(1) 	17(1)	22(2) 	1(1)	11(1) 	1(1)

N3	19(1) 	22(2)	23(2) 	3(1)	9(1) 	1(1)

Fe1	13(1) 	22(1)	18(1) 	0	7(1) 	0

Table 5. Hydrogen coordinates [ 104] and isotropic displacement parameters [Å2  103].

Atom 	x	y	z	Ueq	S.o.f.

H5	3246	1986	253	29	1

H4	2545	335	1447	32	1

H3	2666	2387	1262	36	1

H2	3475	3447	119	35	1

H7A	3961	3026	2064	27	1

H7B	3219	2401	1207	27	1

H8A	4443	2884	664	28	1

H8B	4960	3128	1712	28	1

H9A	5787	2135	1153	30	1

H9B	5186	769	631	30	1

H77A	6828	127	3054	30	1

H77B	6801	1579	2434	30	1

H2A	4055	2462	1853	41	1

H2B	4677	2670	1556	41	1

H3A	5916	567	1766	26	1

Table 6. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N1H2A...O4i	0.92	2.42	3.169(5)	138.7

N1H2B...O1	0.92	2.33	3.092(4)	140.4

N1H2B...O4	0.92	2.49	3.350(5)	154.9

N1H2B...Cl1	0.92	2.92	3.776(3)	156.0

N3H3A...O2	0.93	2.22	3.041(4)	146.6

N3H3A...O1	0.93	2.43	3.263(5)	148.8

N3H3A...Cl1	0.93	2.82	3.705(3)	159.7

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z+1/2