|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	00src186

Empirical formula 	C13H10OS4

Formula weight 	310.45

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbcn

Unit cell dimensions	a = 14.5002(3) Å	 = 90°

b = 13.4816(3) Å	 = 90°

c = 7.00910(10) Å	  = 90°

Volume	1370.18(5) Å3

Z	4

Density (calculated)	1.505 Mg / m3

Absorption coefficient	0.676 mm1

F(000)	640

Crystal	Block; colourless

Crystal size	0.20  0.20  0.15 mm3

 range for data collection	3.02  25.99°

Index ranges	15  h  17, 16  k  15, 8  l  8

Reflections collected	5309

Independent reflections	1343 [Rint = 0.0298]

Completeness to  = 25.99°	99.3 %

Max. and min. transmission	0.9054 and 0.8766

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1343 / 0 / 93

Goodness-of-fit on F2	1.081

Final R indices [F2 > 2(F2)]	R1 = 0.0380, wR2 = 0.1020

R indices (all data)	R1 = 0.0426, wR2 = 0.1049

Extinction coefficient	0.0000(19)

Largest diff. peak and hole	0.672 and 0.600 e Å3

Diffractometer: Enraf Nonius KappaCCD area detector ( scans and  scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426 Program used to solve structure: DIRDIF-96 (P. T. Beurskens, G. Beurskens, W. P. Bosman, R. de Gelder, S. Garcia-Granda, R. O. Gould, R. Israël & J. M. M. Smits (1996). Crystallography Laboratory, University of Nijmegen, The Netherlands.  Program used to refine structure: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

S1	991(1)	566(1)	2117(1)	29(1)	1

S2	1918(1)	4213(1)	2888(1)	33(1)	1

O1	0	1068(2)	2500	48(1)	1

C1	586(2)	3455(2)	5353(3)	36(1)	1

C2	1109(1)	3339(2)	3530(3)	25(1)	1

C3	1075(1)	2588(2)	2217(3)	23(1)	1

C4	2226(2)	3557(2)	893(4)	40(1)	1

C5	1730(2)	2721(2)	705(3)	35(1)	1

C6	458(2)	1725(1)	2340(3)	22(1)	1

C10	0	172(2)	2500	32(1)	1

Table 3. Bond lengths [Å] and angles [°].

S1C6	1.751(2)

S1C10	1.7688(18)

S2C4	1.714(3)

S2C2	1.722(2)

O1C10	1.207(4)

C1C2	1.494(3)

C2C3	1.369(3)

C3C5	1.434(3)

C3C6	1.470(3)

C4C5	1.344(3)

C6C6i	1.347(4)

C10S1i	1.7688(18)

C6S1C10	97.45(11)

C4S2C2	92.15(11)

C3C2C1	129.32(18)

C3C2S2	110.79(15)

C1C2S2	119.85(16)

C2C3C5	112.36(19)

C2C3C6	124.59(18)

C5C3C6	123.03(19)

C5C4S2	111.92(17)

C4C5C3	112.8(2)

C6iC6C3	127.58(11)

C6iC6S1	116.78(7)

C3C6S1	115.62(15)

O1C10S1	124.24(8)

O1C10S1i	124.24(8)

S1C10S1i	111.53(17)

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z+1/2

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

S1	35(1) 	21(1)	31(1) 	2(1)	9(1) 	8(1)

S2	27(1) 	24(1)	48(1) 	7(1)	5(1) 	5(1)

O1	74(2) 	17(1)	54(2) 	0	28(1) 	0

C1	43(1) 	35(1)	30(1) 	10(1)	5(1) 	16(1)

C2	22(1) 	23(1)	29(1) 	4(1)	2(1) 	3(1)

C3	21(1) 	22(1)	25(1) 	4(1)	2(1) 	4(1)

C4	35(1) 	36(1)	50(1) 	11(1)	21(1) 	3(1)

C5	36(1) 	32(1)	38(1) 	3(1)	14(1) 	9(1)

C6	29(1) 	18(1)	18(1) 	1(1)	2(1) 	5(1)

C10	47(2) 	20(2)	29(2) 	0	17(1) 	0

Table 5. Hydrogen coordinates [ 104] and isotropic displacement parameters [Å2  103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	766	4077	5974	50(20)	0.45(7)

H1B	724	2896	6200	80(30)	0.45(7)

H1C	77	3468	5080	80(30)	0.45(7)

H1D	176	2884	5528	24(15)	0.55(7)

H1E	218	4065	5302	70(20)	0.55(7)

H1F	1019	3493	6422	42(17)	0.55(7)

H4	2692	3760	24	47(7)	1

H5	1805	2267	320	38(7)	1