|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src277 (301-365/2)

Empirical formula 	C12H16ClF8N4O4P3

Formula weight 	560.65

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Cmc21

Unit cell dimensions	a = 20.1599(10) Å	 = 90°

b = 11.7656(6) Å	 = 90°

c = 8.7964(5) Å	  = 90°

Volume	2086.45(19) Å3

Z	4

Density (calculated)	1.785 Mg / m3

Absorption coefficient	0.513 mm1

F(000)	1128

Crystal	plate; colourless

Crystal size	0.12  0.10  0.03 mm3

 range for data collection	3.06  27.44°

Index ranges	25  h  21, 15  k  13, 11  l  10

Reflections collected	6431

Independent reflections	2027 [Rint = 0.0488]

Completeness to  = 27.44°	99.2 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9848 and 0.9410

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2027 / 7 / 152

Goodness-of-fit on F2	1.010

Final R indices [F2 > 2(F2)]	R1 = 0.0413, wR2 = 0.0967

R indices (all data)	R1 = 0.0568, wR2 = 0.1053

Absolute structure parameter	0.31(12)

Extinction coefficient	0.0014(5)

Largest diff. peak and hole	0.405 and 0.394 e Å3

Diffractometer: Enraf Nonius KappaCCD area detector ( scans and  scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

P1-P1' = 2.743, P1-P2 = 2.75, max deviation from mean plane = 0.007(P2).

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	3231(2)	3044(3)	739(5)	35(1)	1

C2	2880(2)	2399(4)	492(5)	38(1)	1

C3	2924(2)	1094(4)	412(5)	39(1)	1

C4	3617(2)	597(4)	248(5)	40(1)	1

C5	4400(2)	3824(4)	5967(5)	51(1)	1

C6	4646(3)	4525(8)	7218(10)	120(3)	1

N1	5000	1850(4)	591(6)	33(1)	1

N2	4324(2)	2200(3)	3215(4)	34(1)	1

N3	5000	3500(4)	5101(5)	36(1)	1

F1	3126(1)	2711(2)	1881(3)	50(1)	1

F2	2230(1)	2698(2)	499(3)	49(1)	1

F3	2537(1)	764(2)	765(3)	48(1)	1

F4	2648(1)	653(2)	1695(3)	58(1)	1

P1	4320(1)	1969(1)	1456(1)	29(1)	1

P2	5000	2334(1)	4121(2)	29(1)	1

Cl1	5000	1072(1)	5732(2)	45(1)	1

O1	3932(1)	2930(2)	549(3)	35(1)	1

O2	3854(1)	882(2)	1241(3)	34(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1	1.429(4)

C1C2	1.500(6)

C1H1A	0.9900

C1H1B	0.9900

C2F2	1.357(4)

C2F1	1.368(5)

C2C3	1.540(6)

C3F3	1.353(5)

C3F4	1.360(5)

C3C4	1.522(6)

C4O2	1.434(5)

C4H4A	0.9900

C4H4B	0.9900

C5C6	1.462(8)

C5N3	1.479(5)

C5H5A	0.9900

C5H5B	0.9900

C6C6i	1.426(13)

C6H6A	0.9900

C6H6B	0.9900

N1P1	1.575(3)

N1P1i	1.575(3)

N2P1	1.571(4)

N2P2	1.588(3)

N3C5i	1.479(5)

N3P2	1.620(5)

P1O1	1.589(3)

P1O2	1.597(3)

P2N2i	1.588(3)

P2Cl1	2.052(2)

O1C1C2	109.6(3)

O1C1H1A	109.8

C2C1H1A	109.8

O1C1H1B	109.8

C2C1H1B	109.8

H1AC1H1B	108.2

F2C2F1	106.1(3)

F2C2C1	109.2(3)

F1C2C1	109.7(3)

F2C2C3	108.3(3)

F1C2C3	106.7(3)

C1C2C3	116.4(3)

F3C3F4	106.8(3)

F3C3C4	110.3(3)

F4C3C4	107.9(3)

F3C3C2	106.8(3)

F4C3C2	108.6(3)

C4C3C2	116.1(3)

O2C4C3	107.6(3)

O2C4H4A	110.2

C3C4H4A	110.2

O2C4H4B	110.2

C3C4H4B	110.2

H4AC4H4B	108.5

C6C5N3	104.9(4)

C6C5H5A	110.8

N3C5H5A	110.8

C6C5H5B	110.8

N3C5H5B	110.8

H5AC5H5B	108.9

C6iC6C5	109.8(3)

C6iC6H6A	109.7

C5C6H6A	109.7

C6iC6H6B	109.7

C5C6H6B	109.7

H6AC6H6B	108.2

P1N1P1i	121.2(3)

P1N2P2	121.1(2)

C5iN3C5	109.6(5)

C5iN3P2	119.5(3)

C5N3P2	119.5(3)

N2P1N1	119.1(2)

N2P1O1	111.94(17)

N1P1O1	104.4(2)

N2P1O2	104.97(17)

N1P1O2	112.53(18)

O1P1O2	102.79(14)

N2P2N2i	118.4(3)

N2P2N3	110.55(14)

N2iP2N3	110.55(14)

N2P2Cl1	105.96(14)

N2iP2Cl1	105.96(14)

N3P2Cl1	104.21(19)

C1O1P1	119.6(3)

C4O2P1	119.4(3)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	26(2) 	38(2)	41(2) 	1(2)	2(2) 	10(2)

C2	28(2) 	52(3)	35(2) 	4(2)	1(2) 	9(2)

C3	33(2) 	50(2)	33(2) 	3(2)	8(2) 	2(2)

C4	36(2) 	39(2)	44(3) 	11(2)	9(2) 	4(2)

C5	64(3) 	50(3)	40(3) 	4(2)	15(2) 	11(2)

C6	115(5) 	150(7)	93(5) 	80(6)	26(4) 	46(5)

N1	21(2) 	43(3)	35(3) 	12(2)	0 	0

N2	23(2) 	46(2)	33(2) 	11(2)	1(2) 	1(1)

N3	43(3) 	31(3)	33(3) 	5(2)	0 	0

F1	49(2) 	66(2)	37(1) 	9(1)	1(1) 	9(1)

F2	29(1) 	63(2)	56(2) 	2(1)	7(1) 	13(1)

F3	34(1) 	50(1)	60(2) 	12(1)	4(1) 	8(1)

F4	53(2) 	66(2)	55(2) 	17(1)	24(1) 	7(1)

P1	21(1) 	31(1)	34(1) 	3(1)	1(1) 	1(1)

P2	28(1) 	29(1)	31(1) 	3(1)	0 	0

Cl1	48(1) 	31(1)	56(1) 	11(1)	0 	0

O1	26(1) 	39(2)	40(2) 	3(1)	3(1) 	2(1)

O2	25(1) 	36(2)	41(2) 	2(1)	7(1) 	0(1)

Table 5. Torsion angles [°].

O1C1C2F2	167.4(3)

O1C1C2F1	51.6(4)

O1C1C2C3	69.7(5)

F2C2C3F3	51.2(4)

F1C2C3F3	165.0(3)

C1C2C3F3	72.1(4)

F2C2C3F4	63.6(4)

F1C2C3F4	50.2(4)

C1C2C3F4	173.0(3)

F2C2C3C4	174.6(3)

F1C2C3C4	71.6(4)

C1C2C3C4	51.3(5)

F3C3C4O2	52.5(4)

F4C3C4O2	168.8(3)

C2C3C4O2	69.1(5)

N3C5C6C6i	6.1(5)

C6C5N3C5i	10.0(8)

C6C5N3P2	153.4(5)

P2N2P1N1	1.0(4)

P2N2P1O1	121.2(2)

P2N2P1O2	128.1(2)

P1iN1P1N2	0.5(4)

P1iN1P1O1	125.3(3)

P1iN1P1O2	124.0(3)

P1N2P2N2i	1.4(4)

P1N2P2N3	127.6(3)

P1N2P2Cl1	120.1(2)

C5iN3P2N2	176.6(4)

C5N3P2N2	43.5(4)

C5iN3P2N2i	43.5(4)

C5N3P2N2i	176.6(4)

C5iN3P2Cl1	69.9(4)

C5N3P2Cl1	69.9(4)

C2C1O1P1	94.9(4)

N2P1O1C1	67.3(3)

N1P1O1C1	162.5(3)

O2P1O1C1	44.9(3)

C3C4O2P1	96.5(3)

N2P1O2C4	165.5(3)

N1P1O2C4	63.5(3)

O1P1O2C4	48.3(3)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z