|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src177

Empirical formula 	C17H10Br2O2S5

Formula weight 	566.37

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	Cc

Unit cell dimensions	a = 20.9579(5) Å	 = 90°

b = 13.8067(4) Å	 = 116.4930(10)°

c = 15.1219(5) Å	  = 90°

Volume	3916.2(2) Å3

Z	8

Density (calculated)	1.921 Mg / m3

Absorption coefficient	4.684 mm1

F(000)	2224

Crystal	block; yellow

Crystal size	0.40  0.28  0.18 mm3

 range for data collection	2.95  27.50°

Index ranges	26  h  27, 17  k  17, 18  l  19

Reflections collected	8839

Independent reflections	5227 [Rint = 0.0675]

Completeness to  = 27.50°	74.8 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.4861 and 0.2559

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5227 / 2 / 471

Goodness-of-fit on F2	1.020

Final R indices [F2 > 2(F2)]	R1 = 0.0570, wR2 = 0.1449

R indices (all data)	R1 = 0.0665, wR2 = 0.1557

Absolute structure parameter	0.502(13)

Extinction coefficient	0.0015(2)

Largest diff. peak and hole	1.313 and 1.543 e Å3

Diffractometer: Enraf Nonius KappaCCD area detector ( scans and  scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Two molecules present

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C11	7071(6)	5048(8)	9927(9)	25(3)	1

C12	7818(6)	4887(8)	10661(9)	27(3)	1

C13	8093(7)	3948(9)	10873(11)	34(3)	1

C14	8774(7)	3811(9)	11598(12)	43(4)	1

C15	9204(7)	4566(9)	12075(10)	34(3)	1

C16	8955(6)	5519(9)	11863(10)	30(3)	1

C17	8261(6)	5675(8)	11141(11)	28(3)	1

C18	1348(6)	6553(7)	2205(9)	22(3)	1

C19	935(6)	6482(7)	337(8)	19(2)	1

C20	350(6)	6268(7)	498(10)	23(3)	1

C21	674(5)	4894(8)	318(9)	23(3)	1

C22	1373(6)	4525(8)	1047(10)	27(3)	1

C23	1457(7)	3523(9)	1124(13)	43(4)	1

C24	2113(9)	3161(10)	1822(13)	55(5)	1

C25	2661(8)	3754(11)	2394(12)	43(4)	1

C26	2571(7)	4740(10)	2302(10)	35(3)	1

C27	1938(7)	5154(8)	1630(10)	27(3)	1

C28	1685(6)	6082(7)	694(10)	24(3)	1

C29	1749(6)	6010(8)	1645(10)	23(3)	1

C30	2380(6)	5599(7)	1586(10)	25(3)	1

C31	2468(6)	5510(8)	2432(10)	28(3)	1

C32	1933(6)	5830(8)	3333(10)	28(3)	1

C33	1312(7)	6231(9)	3382(11)	31(3)	1

C34	1208(6)	6317(8)	2556(9)	23(3)	1

O2	6685(5)	4450(6)	9384(8)	42(3)	1

O3	227(5)	4407(6)	320(8)	43(3)	1

O4	2125(5)	5809(6)	92(7)	32(2)	1

C1	4890(6)	6348(7)	7208(9)	23(3)	1

C2	5904(6)	6213(7)	8954(10)	24(3)	1

C3	5326(6)	6360(8)	9086(9)	25(3)	1

C4	4569(6)	6169(8)	10174(10)	24(3)	1

C5	4525(6)	6195(7)	11103(9)	21(3)	1

C6	5106(6)	6216(8)	12020(10)	27(3)	1

C7	5023(7)	6192(7)	12876(10)	29(3)	1

C8	4341(6)	6139(7)	12828(10)	25(3)	1

C9	3740(6)	6122(7)	11903(10)	25(3)	1

C10	3852(6)	6145(8)	11086(8)	22(3)	1

O1	4090(4)	5917(6)	9386(7)	33(2)	1

S1	4376(2)	6358(2)	5934(2)	24(1)	1

S2	4521(2)	6450(2)	8005(2)	23(1)	1

S3	5785(1)	6165(2)	7736(2)	24(1)	1

S4	5393(2)	6629(2)	10249(2)	27(1)	1

S5	6783(2)	6295(2)	9885(2)	26(1)	1

S6	1860(1)	6662(2)	3484(2)	21(1)	1

S7	1706(1)	6721(2)	1408(2)	22(1)	1

S8	480(1)	6256(2)	1701(2)	23(1)	1

S9	523(2)	6171(2)	452(2)	25(1)	1

S10	878(2)	6679(2)	830(2)	26(1)	1

Br1	3269(1)	6570(1)	6010(1)	29(1)	1

Br2	5448(1)	6101(1)	5597(1)	28(1)	1

Br3	2937(1)	7108(1)	3395(1)	29(1)	1

Br4	837(1)	6210(1)	3858(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

C11O2	1.190(14)

C11C12	1.477(16)

C11S5	1.816(12)

C12C13	1.397(16)

C12C17	1.405(18)

C13C14	1.371(19)

C13H13	0.9500

C14C15	1.356(19)

C14H14	0.9500

C15C16	1.399(17)

C15H15	0.9500

C16C17	1.391(18)

C16H16	0.9500

C17H17	0.9500

C18S8	1.681(11)

C18S7	1.696(14)

C18S6	1.750(12)

C19C20	1.384(17)

C19S7	1.735(11)

C19S10	1.736(12)

C20S8	1.716(14)

C20S9	1.756(11)

C21O3	1.206(14)

C21C22	1.476(15)

C21S9	1.818(11)

C22C23	1.392(17)

C22C27	1.415(17)

C23C24	1.40(2)

C23H23	0.9500

C24C25	1.36(2)

C24H24	0.9500

C25C26	1.372(19)

C25H25	0.9500

C26C27	1.384(17)

C26H26	0.9500

C27H27	0.9500

C28O4	1.194(16)

C28C29	1.506(19)

C28S10	1.810(12)

C29C34	1.403(17)

C29C30	1.405(16)

C30C31	1.377(19)

C30H30	0.9500

C31C32	1.395(18)

C31H31	0.9500

C32C33	1.386(19)

C32H32	0.9500

C33C34	1.37(2)

C33H33	0.9500

C34H34	0.9500

C1S3	1.697(11)

C1S2	1.704(14)

C1S1	1.738(12)

C2C3	1.327(18)

C2S5	1.754(12)

C2S3	1.747(15)

C3S4	1.741(14)

C3S2	1.753(11)

C4O1	1.218(15)

C4C5	1.449(19)

C4S4	1.794(12)

C5C6	1.379(17)

C5C10	1.400(17)

C6C7	1.38(2)

C6H6	0.9500

C7C8	1.400(19)

C7H7	0.9500

C8C9	1.405(18)

C8H8	0.9500

C9C10	1.357(19)

C9H9	0.9500

C10H10	0.9500

S1Br1	2.391(3)

S1Br2	2.540(4)

S6Br3	2.401(3)

S6Br4	2.528(3)

O2C11C12	125.4(11)

O2C11S5	121.4(9)

C12C11S5	113.1(8)

C13C12C17	119.4(11)

C13C12C11	120.2(11)

C17C12C11	120.5(10)

C14C13C12	119.2(12)

C14C13H13	120.4

C12C13H13	120.4

C15C14C13	121.8(11)

C15C14H14	119.1

C13C14H14	119.1

C14C15C16	120.7(11)

C14C15H15	119.7

C16C15H15	119.7

C17C16C15	118.6(12)

C17C16H16	120.7

C15C16H16	120.7

C16C17C12	120.3(11)

C16C17H17	119.9

C12C17H17	119.9

S8C18S7	116.4(7)

S8C18S6	121.9(8)

S7C18S6	121.7(7)

C20C19S7	114.0(9)

C20C19S10	123.2(9)

S7C19S10	122.2(7)

C19C20S8	117.0(9)

C19C20S9	123.6(10)

S8C20S9	118.8(8)

O3C21C22	124.3(10)

O3C21S9	121.2(8)

C22C21S9	114.6(8)

C23C22C27	121.2(11)

C23C22C21	116.8(11)

C27C22C21	122.0(10)

C22C23C24	117.6(13)

C22C23H23	121.2

C24C23H23	121.2

C25C24C23	122.0(12)

C25C24H24	119.0

C23C24H24	119.0

C24C25C26	119.6(12)

C24C25H25	120.2

C26C25H25	120.2

C25C26C27	121.8(13)

C25C26H26	119.1

C27C26H26	119.1

C26C27C22	117.8(11)

C26C27H27	121.1

C22C27H27	121.1

O4C28C29	124.9(11)

O4C28S10	121.6(11)

C29C28S10	113.5(8)

C34C29C30	120.6(12)

C34C29C28	122.7(10)

C30C29C28	116.6(10)

C31C30C29	119.3(11)

C31C30H30	120.3

C29C30H30	120.3

C30C31C32	119.8(11)

C30C31H31	120.1

C32C31H31	120.1

C33C32C31	120.3(13)

C33C32H32	119.8

C31C32H32	119.8

C34C33C32	121.0(13)

C34C33H33	119.5

C32C33H33	119.5

C33C34C29	118.9(11)

C33C34H34	120.6

C29C34H34	120.6

S3C1S2	115.7(7)

S3C1S1	122.0(8)

S2C1S1	122.1(7)

C3C2S5	124.8(11)

C3C2S3	117.0(9)

S5C2S3	117.0(8)

C2C3S4	121.2(9)

C2C3S2	115.7(10)

S4C3S2	122.4(8)

O1C4C5	125.0(11)

O1C4S4	120.9(11)

C5C4S4	114.0(8)

C6C5C10	116.7(12)

C6C5C4	124.5(11)

C10C5C4	118.7(10)

C7C6C5	121.3(12)

C7C6H6	119.4

C5C6H6	119.4

C6C7C8	120.3(12)

C6C7H7	119.8

C8C7H7	119.8

C7C8C9	119.6(13)

C7C8H8	120.2

C9C8H8	120.2

C10C9C8	117.6(10)

C10C9H9	121.2

C8C9H9	121.2

C9C10C5	124.5(11)

C9C10H10	117.7

C5C10H10	117.7

C1S1Br1	94.7(4)

C1S1Br2	93.2(4)

Br1S1Br2	172.06(14)

C1S2C3	95.9(6)

C1S3C2	95.7(6)

C3S4C4	102.7(6)

C2S5C11	100.4(5)

C18S6Br3	95.1(4)

C18S6Br4	93.6(4)

Br3S6Br4	171.29(14)

C18S7C19	96.6(5)

C18S8C20	96.1(6)

C20S9C21	98.8(5)

C19S10C28	100.1(6)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C11	26(5) 	20(6)	27(6) 	2(5)	11(5) 	6(4)

C12	31(6) 	25(6)	26(7) 	5(5)	14(5) 	9(5)

C13	38(7) 	20(6)	51(9) 	3(5)	25(7) 	1(4)

C14	34(7) 	26(7)	55(10) 	3(6)	8(7) 	13(5)

C15	35(7) 	34(7)	28(7) 	8(5)	9(6) 	17(5)

C16	33(6) 	29(6)	27(7) 	7(5)	13(5) 	1(5)

C17	29(6) 	24(6)	38(7) 	13(5)	21(5) 	5(5)

C18	31(6) 	9(5)	21(6) 	3(4)	7(5) 	3(4)

C19	29(6) 	17(5)	15(6) 	3(4)	13(5) 	4(4)

C20	25(6) 	19(5)	21(7) 	2(4)	7(5) 	3(4)

C21	16(5) 	22(6)	26(6) 	5(5)	5(5) 	3(4)

C22	29(6) 	18(6)	38(8) 	5(5)	19(6) 	1(4)

C23	44(7) 	16(6)	67(11) 	9(6)	24(7) 	11(5)

C24	68(10) 	18(7)	65(11) 	4(6)	19(9) 	19(7)

C25	37(8) 	56(9)	40(9) 	21(7)	20(7) 	28(6)

C26	27(6) 	42(8)	37(8) 	11(6)	15(6) 	12(5)

C27	41(7) 	24(6)	22(6) 	8(5)	20(5) 	9(5)

C28	24(6) 	11(5)	36(8) 	5(5)	14(6) 	6(4)

C29	22(5) 	18(5)	27(7) 	2(4)	8(5) 	6(4)

C30	29(5) 	13(5)	33(7) 	5(4)	15(5) 	7(4)

C31	22(5) 	24(6)	35(7) 	2(5)	12(5) 	2(4)

C32	39(7) 	19(6)	32(7) 	5(5)	21(6) 	12(5)

C33	34(7) 	29(7)	32(8) 	2(5)	18(6) 	7(5)

C34	28(6) 	28(6)	20(7) 	0(5)	17(5) 	2(4)

O2	26(4) 	25(5)	58(7) 	3(4)	4(4) 	4(3)

O3	43(5) 	19(5)	48(6) 	1(4)	3(5) 	1(4)

O4	29(4) 	43(5)	25(5) 	7(4)	14(4) 	15(4)

C1	24(5) 	8(5)	30(7) 	3(4)	4(5) 	5(4)

C2	31(6) 	10(5)	27(7) 	2(4)	9(5) 	0(4)

C3	30(6) 	23(6)	20(7) 	1(5)	8(5) 	6(4)

C4	20(6) 	16(6)	32(8) 	4(5)	7(5) 	6(4)

C5	27(6) 	9(5)	26(7) 	1(4)	11(5) 	4(4)

C6	25(6) 	21(6)	34(8) 	1(5)	11(6) 	1(4)

C7	36(7) 	16(6)	25(8) 	2(5)	5(6) 	6(4)

C8	35(7) 	15(6)	27(7) 	1(4)	15(6) 	2(4)

C9	26(6) 	18(6)	39(8) 	4(5)	21(5) 	2(4)

C10	27(6) 	28(6)	10(6) 	5(4)	7(5) 	4(4)

O1	29(4) 	40(5)	27(5) 	0(4)	9(4) 	5(4)

S1	29(1) 	17(1)	24(2) 	1(1)	9(1) 	4(1)

S2	26(1) 	22(1)	22(2) 	1(1)	10(1) 	2(1)

S3	24(1) 	19(1)	25(2) 	1(1)	9(1) 	0(1)

S4	31(2) 	30(2)	23(2) 	4(1)	13(1) 	9(1)

S5	25(1) 	20(1)	27(2) 	1(1)	7(1) 	2(1)

S6	24(1) 	17(1)	21(2) 	4(1)	10(1) 	0(1)

S7	20(1) 	23(1)	22(2) 	1(1)	9(1) 	1(1)

S8	22(1) 	23(1)	23(2) 	2(1)	11(1) 	2(1)

S9	25(1) 	18(1)	26(2) 	1(1)	6(1) 	2(1)

S10	28(2) 	26(2)	22(2) 	5(1)	10(1) 	7(1)

Br1	26(1) 	29(1)	29(1) 	4(1)	8(1) 	1(1)

Br2	34(1) 	24(1)	27(1) 	2(1)	16(1) 	4(1)

Br3	26(1) 	27(1)	30(1) 	5(1)	9(1) 	6(1)

Br4	29(1) 	23(1)	26(1) 	1(1)	14(1) 	1(1)

Molecule 1.

Molecule 2.