|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0197

Empirical formula 	C44H46Cl4Co2N16O21

Formula weight 	1394.63

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pna21

Unit cell dimensions	a = 25.808(5) Å	a = 90°

b = 11.9889(8) Å	b = 90°

c = 17.384(3) Å	g  = 90°

Volume	5378.8(15) Å3

Z	4

Density (calculated)	1.722 Mg / m3

Absorption coefficient	0.912 mm-1

F(000)	2848

Crystal	Block; Red

Crystal size	0.36 ´ 0.24 ´ 0.16 mm3

q range for data collection	3.00 - 27.48°

Index ranges	-32 £ h £ 33, -15 £ k £ 15, -22 £ l £ 22

Reflections collected	72712

Independent reflections	12146 [Rint = 0.0606]

Completeness to q = 27.48°	99.8 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.8678 and 0.7349

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	12146 / 71 / 786

Goodness-of-fit on F2	1.022

Final R indices [F2 > 2s(F2)]	R1 = 0.0568, wR2 = 0.1381

R indices (all data)	R1 = 0.0827, wR2 = 0.1512

Absolute structure parameter	0.48(2)

Largest diff. peak and hole	1.414 and -1.270 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33-37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421-426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

It was not possible to locate the hydrogen atoms on the solvent water molecules.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	3525(3)	3911(6)	1450(4)	31(2)	1

C2	3903(2)	4709(5)	1516(4)	29(2)	1

C3	4049(3)	5287(6)	882(4)	32(2)	1

C4	3803(3)	5055(5)	187(4)	29(2)	1

C5	3433(2)	4260(5)	157(4)	21(1)	1

C6	3144(2)	3951(5)	-542(3)	20(1)	1

C7	3253(2)	4393(5)	-1265(4)	25(1)	1

C8	2946(3)	4052(5)	-1870(4)	28(1)	1

C9	2549(2)	3300(5)	-1759(4)	24(1)	1

C10	2462(2)	2921(5)	-1012(3)	20(1)	1

C11	2044(2)	2174(5)	-776(3)	19(1)	1

C12	1674(2)	413(4)	590(4)	21(1)	1

C13	1215(2)	123(5)	1043(4)	19(1)	1

C14	1074(2)	-922(5)	1283(4)	26(1)	1

C15	620(2)	-1011(6)	1713(4)	26(1)	1

C16	354(2)	-88(5)	1914(4)	25(1)	1

C17	504(2)	944(5)	1654(3)	21(1)	1

C18	250(2)	2028(6)	1796(4)	26(1)	1

C19	-164(2)	2143(6)	2270(4)	28(1)	1

C20	-348(2)	3199(6)	2402(4)	28(1)	1

C21	-119(2)	4078(6)	2055(4)	29(2)	1

C22	285(3)	3896(6)	1567(4)	29(2)	1

C31	3478(2)	961(5)	-306(4)	27(1)	1

C32	3890(2)	229(5)	-381(4)	27(1)	1

C33	4086(3)	-235(5)	259(4)	31(2)	1

C34	3879(3)	30(5)	960(4)	31(2)	1

C35	3458(2)	740(5)	990(4)	20(1)	1

C36	3186(2)	988(5)	1713(4)	21(1)	1

C37	3298(3)	584(5)	2437(4)	28(1)	1

C38	3014(2)	934(5)	3040(4)	29(1)	1

C39	2598(2)	1650(5)	2936(4)	25(1)	1

C40	2502(2)	2011(4)	2211(4)	19(1)	1

C41	2063(2)	2722(5)	1957(3)	17(1)	1

C42	1679(2)	4476(4)	611(4)	17(1)	1

C43	1218(2)	4744(5)	121(4)	19(1)	1

C44	1088(3)	5782(5)	-132(4)	26(1)	1

C45	647(3)	5881(6)	-572(4)	33(2)	1

C46	357(2)	4945(5)	-748(4)	30(2)	1

C47	515(2)	3948(5)	-455(4)	23(1)	1

C48	254(2)	2884(5)	-601(3)	21(1)	1

C49	-165(3)	2742(6)	-1084(4)	28(1)	1

C50	-358(3)	1685(6)	-1198(4)	35(2)	1

C51	-137(3)	783(6)	-859(4)	34(2)	1

C52	278(2)	979(5)	-377(4)	26(1)	1

N1	3283(2)	3669(4)	794(3)	25(1)	1

N2	2764(2)	3249(4)	-445(3)	20(1)	1

N3	1639(2)	2053(4)	-1235(3)	25(1)	1

N4	2098(2)	1759(4)	-95(3)	18(1)	1

N5	1637(2)	1360(4)	217(3)	21(1)	1

N6	2086(2)	-234(3)	591(3)	22(1)	1

N7	936(2)	1022(4)	1222(3)	21(1)	1

N8	462(2)	2883(4)	1422(3)	23(1)	1

N31	3275(2)	1202(4)	366(3)	22(1)	1

N32	2792(2)	1697(4)	1604(3)	18(1)	1

N33	1667(2)	2893(4)	2422(3)	28(1)	1

N34	2104(2)	3112(4)	1271(3)	18(1)	1

N35	1636(2)	3532(4)	971(3)	19(1)	1

N36	2086(2)	5131(4)	592(4)	24(1)	1

N37	933(2)	3860(4)	-32(3)	16(1)	1

N38	472(2)	1992(4)	-240(3)	21(1)	1

Co1	2697(1)	2457(1)	582(1)	17(1)	1

Co2	1041(1)	2443(1)	594(1)	17(1)	1

O1	4343(2)	6713(4)	2656(3)	33(1)	1

O2	4245(2)	8643(4)	2712(3)	32(1)	1

O3	4455(2)	7793(5)	1553(3)	46(1)	1

O4	3638(2)	7589(4)	2076(4)	42(2)	1

Cl1	4185(1)	7678(1)	2250(1)	28(1)	1

O11	774(2)	1350(4)	3423(3)	34(1)	1

O12	652(2)	3283(4)	3447(3)	40(1)	1

O13	1370(2)	2453(4)	4036(4)	41(2)	1

O14	558(2)	2238(5)	4574(3)	52(2)	1

Cl11	819(1)	2330(1)	3871(1)	29(1)	1

O21	3098(2)	3980(5)	3886(3)	58(1)	1

O22	3867(2)	3524(5)	4516(3)	64(2)	1

O23	3867(2)	4820(4)	3542(4)	68(2)	1

O24	3744(2)	2975(5)	3251(3)	52(1)	1

Cl21	3640(1)	3821(1)	3789(1)	36(1)	1

O31	1317(2)	7040(4)	2836(4)	59(2)	1

O32	1224(3)	6395(5)	1614(3)	77(2)	1

O33	1401(3)	5163(4)	2573(4)	82(2)	1

O34	600(2)	6006(6)	2517(4)	91(2)	1

Cl31	1152(1)	6146(1)	2380(1)	46(1)	1

O51	2696(2)	2041(4)	4720(3)	42(1)	1

O52	2427(2)	5398(5)	3106(4)	74(2)	1

O53	2804(2)	6016(4)	1724(3)	55(1)	1

O54	2171(2)	7813(5)	1513(3)	54(2)	1

O55	3167(2)	7918(5)	466(3)	70(2)	1

Table 3. Bond lengths [Å] and angles [°].

C1-N1	1.333(8)

C1-C2	1.371(9)

C1-H1	0.9500

C2-C3	1.354(9)

C2-H2	0.9500

C3-C4	1.393(9)

C3-H3	0.9500

C4-C5	1.351(9)

C4-H4	0.9500

C5-N1	1.369(8)

C5-C6	1.473(9)

C6-N2	1.304(7)

C6-C7	1.393(8)

C7-C8	1.379(9)

C7-H7	0.9500

C8-C9	1.379(9)

C8-H8	0.9500

C9-C10	1.394(8)

C9-H9	0.9500

C10-N2	1.317(8)

C10-C11	1.461(9)

C11-N4	1.292(7)

C11-N3	1.321(8)

C12-N5	1.311(7)

C12-N6	1.317(7)

C12-C13	1.463(8)

C13-N7	1.332(7)

C13-C14	1.370(8)

C14-C15	1.394(9)

C14-H14	0.9500

C15-C16	1.349(9)

C15-H15	0.9500

C16-C17	1.374(8)

C16-H16	0.9500

C17-N7	1.348(8)

C17-C18	1.476(9)

C18-N8	1.330(9)

C18-C19	1.358(9)

C19-C20	1.371(9)

C19-H19	0.9500

C20-C21	1.349(9)

C20-H20	0.9500

C21-C22	1.362(9)

C21-H21	0.9500

C22-N8	1.321(8)

C22-H22	0.9500

C31-N31	1.312(8)

C31-C32	1.386(9)

C31-H31	0.9500

C32-C33	1.342(9)

C32-H32	0.9500

C33-C34	1.368(10)

C33-H33	0.9500

C34-C35	1.381(9)

C34-H34	0.9500

C35-N31	1.306(8)

C35-C36	1.470(9)

C36-N32	1.339(7)

C36-C37	1.379(9)

C37-C38	1.346(10)

C37-H37	0.9500

C38-C39	1.387(9)

C38-H38	0.9500

C39-C40	1.354(9)

C39-H39	0.9500

C40-N32	1.348(8)

C40-C41	1.486(8)

C41-N34	1.285(7)

C41-N33	1.319(8)

C42-N35	1.298(7)

C42-N36	1.312(6)

C42-C43	1.498(8)

C43-N37	1.316(7)

C43-C44	1.361(8)

C44-C45	1.376(9)

C44-H44	0.9500

C45-C46	1.383(10)

C45-H45	0.9500

C46-C47	1.362(9)

C46-H46	0.9500

C47-N37	1.312(8)

C47-C48	1.464(9)

C48-N38	1.361(8)

C48-C49	1.380(9)

C49-C50	1.376(10)

C49-H49	0.9500

C50-C51	1.357(10)

C50-H50	0.9500

C51-C52	1.380(9)

C51-H51	0.9500

C52-N38	1.335(8)

C52-H52	0.9500

N1-Co1	2.129(5)

N2-Co1	2.029(5)

N3-H3A	0.8800

N3-H3B	0.8800

N4-N5	1.393(7)

N4-Co1	2.116(5)

N5-Co2	2.117(5)

N6-H6A	0.8800

N6-H6B	0.8800

N7-Co2	2.041(5)

N8-Co2	2.141(5)

N31-Co1	2.152(5)

N32-Co1	2.012(5)

N33-H33A	0.8800

N33-H33B	0.8800

N34-N35	1.407(6)

N34-Co1	2.097(5)

N35-Co2	2.120(5)

N36-H36A	0.8800

N36-H36B	0.8800

N37-Co2	2.037(5)

N38-Co2	2.133(5)

O1-Cl1	1.415(4)

O2-Cl1	1.416(4)

O3-Cl1	1.404(5)

O4-Cl1	1.448(5)

O11-Cl11	1.414(5)

O12-Cl11	1.426(5)

O13-Cl11	1.460(5)

O14-Cl11	1.400(5)

O21-Cl21	1.422(5)

O22-Cl21	1.438(5)

O23-Cl21	1.401(5)

O24-Cl21	1.406(5)

O31-Cl31	1.399(5)

O32-Cl31	1.377(6)

O33-Cl31	1.383(5)

O34-Cl31	1.454(5)

N1-C1-C2	123.8(7)

N1-C1-H1	118.1

C2-C1-H1	118.1

C3-C2-C1	119.1(7)

C3-C2-H2	120.4

C1-C2-H2	120.4

C2-C3-C4	118.5(6)

C2-C3-H3	120.7

C4-C3-H3	120.7

C5-C4-C3	119.7(6)

C5-C4-H4	120.2

C3-C4-H4	120.2

C4-C5-N1	122.3(6)

C4-C5-C6	124.5(6)

N1-C5-C6	113.2(5)

N2-C6-C7	120.9(6)

N2-C6-C5	115.9(5)

C7-C6-C5	123.2(5)

C8-C7-C6	117.4(5)

C8-C7-H7	121.3

C6-C7-H7	121.3

C9-C8-C7	120.9(6)

C9-C8-H8	119.6

C7-C8-H8	119.6

C8-C9-C10	117.7(6)

C8-C9-H9	121.2

C10-C9-H9	121.2

N2-C10-C9	120.2(6)

N2-C10-C11	114.2(5)

C9-C10-C11	125.5(6)

N4-C11-N3	126.6(6)

N4-C11-C10	114.4(5)

N3-C11-C10	118.8(5)

N5-C12-N6	124.7(6)

N5-C12-C13	114.4(5)

N6-C12-C13	120.9(5)

N7-C13-C14	121.7(6)

N7-C13-C12	111.8(5)

C14-C13-C12	126.6(5)

C13-C14-C15	117.1(6)

C13-C14-H14	121.4

C15-C14-H14	121.4

C16-C15-C14	120.3(6)

C16-C15-H15	119.8

C14-C15-H15	119.8

C15-C16-C17	120.7(6)

C15-C16-H16	119.7

C17-C16-H16	119.7

N7-C17-C16	118.6(6)

N7-C17-C18	113.6(5)

C16-C17-C18	127.8(5)

N8-C18-C19	122.8(7)

N8-C18-C17	114.5(6)

C19-C18-C17	122.7(6)

C18-C19-C20	117.9(7)

C18-C19-H19	121.1

C20-C19-H19	121.1

C21-C20-C19	119.7(6)

C21-C20-H20	120.2

C19-C20-H20	120.2

C20-C21-C22	119.2(6)

C20-C21-H21	120.4

C22-C21-H21	120.4

N8-C22-C21	122.1(6)

N8-C22-H22	119.0

C21-C22-H22	119.0

N31-C31-C32	121.9(6)

N31-C31-H31	119.0

C32-C31-H31	119.0

C33-C32-C31	118.3(6)

C33-C32-H32	120.9

C31-C32-H32	120.9

C32-C33-C34	119.7(6)

C32-C33-H33	120.2

C34-C33-H33	120.2

C33-C34-C35	119.0(6)

C33-C34-H34	120.5

C35-C34-H34	120.5

N31-C35-C34	120.9(6)

N31-C35-C36	116.9(5)

C34-C35-C36	122.2(6)

N32-C36-C37	120.8(6)

N32-C36-C35	111.7(5)

C37-C36-C35	127.5(5)

C38-C37-C36	119.1(6)

C38-C37-H37	120.4

C36-C37-H37	120.4

C37-C38-C39	120.9(6)

C37-C38-H38	119.6

C39-C38-H38	119.6

C40-C39-C38	117.4(6)

C40-C39-H39	121.3

C38-C39-H39	121.3

N32-C40-C39	122.6(5)

N32-C40-C41	110.5(5)

C39-C40-C41	126.8(6)

N34-C41-N33	125.1(5)

N34-C41-C40	115.0(5)

N33-C41-C40	119.8(5)

N35-C42-N36	127.0(5)

N35-C42-C43	113.2(4)

N36-C42-C43	119.6(5)

N37-C43-C44	122.2(6)

N37-C43-C42	112.7(5)

C44-C43-C42	125.1(5)

C43-C44-C45	117.5(6)

C43-C44-H44	121.2

C45-C44-H44	121.2

C44-C45-C46	120.1(6)

C44-C45-H45	120.0

C46-C45-H45	120.0

C47-C46-C45	117.9(6)

C47-C46-H46	121.1

C45-C46-H46	121.1

N37-C47-C46	121.7(6)

N37-C47-C48	113.9(5)

C46-C47-C48	124.3(6)

N38-C48-C49	120.5(6)

N38-C48-C47	114.5(6)

C49-C48-C47	124.9(6)

C50-C49-C48	119.0(7)

C50-C49-H49	120.5

C48-C49-H49	120.5

C51-C50-C49	121.2(7)

C51-C50-H50	119.4

C49-C50-H50	119.4

C50-C51-C52	117.1(6)

C50-C51-H51	121.5

C52-C51-H51	121.5

N38-C52-C51	123.6(6)

N38-C52-H52	118.2

C51-C52-H52	118.2

C1-N1-C5	116.5(5)

C1-N1-Co1	129.0(4)

C5-N1-Co1	114.5(4)

C6-N2-C10	122.8(5)

C6-N2-Co1	118.6(4)

C10-N2-Co1	118.0(4)

C11-N3-H3A	120.0

C11-N3-H3B	120.0

H3A-N3-H3B	120.0

C11-N4-N5	113.3(5)

C11-N4-Co1	115.9(4)

N5-N4-Co1	123.0(4)

C12-N5-N4	115.3(5)

C12-N5-Co2	115.5(4)

N4-N5-Co2	122.0(3)

C12-N6-H6A	120.0

C12-N6-H6B	120.0

H6A-N6-H6B	120.0

C13-N7-C17	121.5(5)

C13-N7-Co2	118.6(4)

C17-N7-Co2	117.7(4)

C22-N8-C18	118.2(6)

C22-N8-Co2	126.6(5)

C18-N8-Co2	115.1(4)

C35-N31-C31	120.2(5)

C35-N31-Co1	113.7(4)

C31-N31-Co1	125.8(4)

C36-N32-C40	119.1(5)

C36-N32-Co1	120.4(4)

C40-N32-Co1	119.9(4)

C41-N33-H33A	120.0

C41-N33-H33B	120.0

H33A-N33-H33B	120.0

C41-N34-N35	113.9(5)

C41-N34-Co1	117.0(4)

N35-N34-Co1	123.3(3)

C42-N35-N34	114.8(4)

C42-N35-Co2	116.7(4)

N34-N35-Co2	121.0(3)

C42-N36-H36A	120.0

C42-N36-H36B	120.0

H36A-N36-H36B	120.0

C47-N37-C43	120.6(5)

C47-N37-Co2	118.6(4)

C43-N37-Co2	119.2(4)

C52-N38-C48	118.5(6)

C52-N38-Co2	127.6(4)

C48-N38-Co2	113.5(4)

N32-Co1-N2	168.14(14)

N32-Co1-N34	75.74(19)

N2-Co1-N34	112.90(18)

N32-Co1-N4	113.64(18)

N2-Co1-N4	75.97(19)

N34-Co1-N4	86.07(13)

N32-Co1-N1	94.01(19)

N2-Co1-N1	76.87(19)

N34-Co1-N1	99.47(19)

N4-Co1-N1	152.27(19)

N32-Co1-N31	75.71(18)

N2-Co1-N31	96.62(18)

N34-Co1-N31	150.19(19)

N4-Co1-N31	97.64(18)

N1-Co1-N31	90.89(15)

N37-Co2-N7	164.55(14)

N37-Co2-N5	116.46(19)

N7-Co2-N5	75.51(19)

N37-Co2-N35	75.52(18)

N7-Co2-N35	116.40(19)

N5-Co2-N35	86.97(13)

N37-Co2-N38	75.78(19)

N7-Co2-N38	93.5(2)

N5-Co2-N38	97.72(19)

N35-Co2-N38	149.87(19)

N37-Co2-N8	93.31(19)

N7-Co2-N8	75.8(2)

N5-Co2-N8	150.1(2)

N35-Co2-N8	98.43(19)

N38-Co2-N8	92.19(14)

O3-Cl1-O1	111.6(3)

O3-Cl1-O2	110.8(4)

O1-Cl1-O2	110.7(3)

O3-Cl1-O4	108.1(4)

O1-Cl1-O4	108.9(3)

O2-Cl1-O4	106.6(3)

O14-Cl11-O11	112.1(4)

O14-Cl11-O12	111.6(3)

O11-Cl11-O12	110.9(3)

O14-Cl11-O13	107.8(4)

O11-Cl11-O13	105.8(3)

O12-Cl11-O13	108.3(3)

O23-Cl21-O24	109.5(4)

O23-Cl21-O21	109.4(4)

O24-Cl21-O21	111.4(3)

O23-Cl21-O22	108.0(4)

O24-Cl21-O22	109.1(4)

O21-Cl21-O22	109.3(4)

O32-Cl31-O33	110.9(4)

O32-Cl31-O31	109.9(4)

O33-Cl31-O31	111.9(4)

O32-Cl31-O34	108.4(5)

O33-Cl31-O34	108.5(5)

O31-Cl31-O34	107.1(4)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	37(4) 	33(3)	24(3) 	1(3)	-11(3) 	-4(3)

C2	26(3) 	27(3)	34(4) 	-1(3)	-2(3) 	-3(3)

C3	21(3) 	30(3)	46(4) 	-1(3)	-4(3) 	-9(3)

C4	30(3) 	29(3)	29(4) 	-4(3)	4(3) 	-7(3)

C5	20(3) 	19(3)	25(3) 	0(2)	7(2) 	3(2)

C6	20(3) 	17(3)	22(3) 	2(2)	0(2) 	2(2)

C7	24(3) 	27(3)	25(3) 	10(3)	8(3) 	-1(2)

C8	40(4) 	33(3)	10(3) 	2(2)	2(2) 	-6(3)

C9	28(3) 	26(3)	19(3) 	5(2)	3(2) 	-2(2)

C10	25(3) 	25(3)	10(3) 	0(2)	4(2) 	3(2)

C11	22(3) 	15(2)	21(3) 	-5(2)	3(2) 	4(3)

C12	25(3) 	21(2)	16(3) 	0(3)	-4(3) 	-1(2)

C13	19(3) 	23(3)	16(3) 	-1(2)	-1(2) 	0(2)

C14	27(3) 	17(3)	34(4) 	4(2)	2(3) 	1(2)

C15	30(3) 	25(3)	25(4) 	14(3)	4(3) 	1(2)

C16	28(3) 	28(3)	18(3) 	8(2)	2(2) 	-9(3)

C17	16(3) 	31(3)	16(3) 	10(2)	0(2) 	-3(2)

C18	16(3) 	39(4)	22(3) 	2(3)	0(2) 	-4(3)

C19	25(4) 	37(3)	22(3) 	-3(3)	-2(3) 	-2(3)

C20	20(3) 	46(4)	19(3) 	-3(3)	2(3) 	4(3)

C21	28(3) 	34(3)	25(4) 	-6(3)	1(3) 	8(3)

C22	31(4) 	26(3)	28(4) 	-5(3)	0(3) 	2(3)

C31	23(3) 	27(3)	32(4) 	9(3)	2(3) 	5(2)

C32	22(3) 	25(3)	33(4) 	-4(3)	5(3) 	-1(2)

C33	28(4) 	22(3)	44(4) 	-5(3)	-1(3) 	6(3)

C34	27(3) 	30(3)	36(4) 	4(3)	-5(3) 	11(3)

C35	15(3) 	21(3)	23(3) 	0(2)	0(2) 	-2(2)

C36	16(3) 	15(3)	32(4) 	0(2)	-8(2) 	1(2)

C37	31(3) 	24(3)	29(4) 	-2(3)	-9(3) 	6(2)

C38	23(3) 	27(3)	36(4) 	6(3)	-11(3) 	-1(2)

C39	30(3) 	27(3)	19(3) 	1(2)	-10(2) 	-1(3)

C40	16(3) 	15(3)	27(3) 	1(2)	-5(2) 	-3(2)

C41	16(3) 	17(2)	17(3) 	4(2)	-3(2) 	1(2)

C42	17(2) 	14(2)	19(3) 	-4(3)	0(3) 	-1(2)

C43	18(3) 	18(3)	22(3) 	3(2)	5(2) 	0(2)

C44	32(4) 	23(3)	22(3) 	6(2)	-3(3) 	0(2)

C45	35(4) 	33(4)	31(4) 	6(3)	0(3) 	19(3)

C46	20(3) 	40(4)	31(4) 	10(3)	-4(3) 	0(3)

C47	23(3) 	29(3)	18(3) 	-1(2)	2(2) 	4(3)

C48	20(3) 	28(3)	15(3) 	-1(2)	4(2) 	2(2)

C49	20(3) 	41(3)	23(4) 	2(3)	-5(3) 	2(3)

C50	23(3) 	55(4)	26(3) 	-9(3)	-3(3) 	-4(3)

C51	24(3) 	44(4)	34(4) 	-7(3)	1(3) 	-7(3)

C52	22(3) 	26(3)	30(4) 	-4(3)	0(3) 	-3(2)

N1	18(2) 	29(3)	27(3) 	4(2)	-8(2) 	-4(2)

N2	21(3) 	16(2)	22(3) 	3(2)	7(2) 	3(2)

N3	23(3) 	34(3)	17(3) 	2(2)	-4(2) 	-4(2)

N4	19(2) 	15(2)	20(3) 	2(2)	3(2) 	-1(2)

N5	23(3) 	18(2)	21(3) 	-2(2)	6(2) 	-1(2)

N6	25(2) 	19(2)	23(3) 	4(2)	-2(3) 	2(2)

N7	23(3) 	19(2)	22(3) 	1(2)	-4(2) 	-5(2)

N8	19(3) 	21(2)	29(3) 	-3(2)	0(2) 	8(2)

N31	28(3) 	15(2)	24(3) 	4(2)	-3(2) 	4(2)

N32	13(2) 	21(2)	19(3) 	-3(2)	3(2) 	-2(2)

N33	22(3) 	34(3)	28(3) 	7(2)	1(2) 	8(2)

N34	10(2) 	20(2)	23(3) 	0(2)	-4(2) 	-1(2)

N35	11(2) 	28(2)	18(3) 	8(2)	1(2) 	1(2)

N36	18(2) 	22(2)	33(3) 	3(3)	-7(3) 	1(2)

N37	9(2) 	25(2)	15(2) 	3(2)	1(2) 	2(2)

N38	18(3) 	28(3)	15(2) 	2(2)	-5(2) 	5(2)

Co1	15(1) 	18(1)	18(1) 	3(1)	-1(1) 	-1(1)

Co2	15(1) 	18(1)	18(1) 	1(1)	-1(1) 	-1(1)

O1	31(3) 	28(3)	40(3) 	8(2)	-6(2) 	-1(2)

O2	39(3) 	26(3)	32(3) 	-9(2)	-11(2) 	-2(2)

O3	48(3) 	51(3)	40(4) 	-4(3)	12(3) 	2(3)

O4	34(3) 	45(3)	47(4) 	-1(2)	-18(3) 	-5(2)

Cl1	27(1) 	23(1)	32(1) 	-2(1)	1(1) 	-1(1)

O11	42(3) 	29(3)	30(3) 	4(2)	4(2) 	9(2)

O12	57(3) 	19(2)	45(3) 	-1(2)	-22(2) 	3(2)

O13	20(3) 	59(4)	43(4) 	0(2)	0(3) 	-2(2)

O14	65(4) 	59(3)	32(3) 	6(3)	18(3) 	26(3)

Cl11	38(1) 	26(1)	24(1) 	1(1)	-2(1) 	-1(1)

O21	36(3) 	73(4)	63(3) 	-2(3)	8(2) 	11(2)

O22	89(4) 	65(4)	36(3) 	8(3)	0(3) 	24(3)

O23	89(4) 	25(3)	91(5) 	7(3)	9(4) 	-7(3)

O24	57(3) 	55(3)	43(3) 	-24(3)	7(3) 	13(3)

Cl21	63(1) 	23(1)	22(1) 	-2(1)	8(1) 	-3(1)

O31	64(4) 	30(3)	83(5) 	-20(3)	-26(3) 	1(3)

O32	139(6) 	52(4)	41(4) 	13(3)	27(4) 	18(4)

O33	104(5) 	38(3)	105(5) 	-3(3)	-46(4) 	17(3)

O34	36(3) 	125(6)	111(5) 	-69(5)	30(3) 	-16(3)

Cl31	81(1) 	26(1)	31(1) 	-1(1)	6(1) 	1(1)

O51	67(3) 	34(3)	25(2) 	2(2)	0(2) 	14(2)

O52	69(4) 	68(4)	85(4) 	24(4)	-16(3) 	4(3)

O53	43(3) 	54(3)	66(3) 	-9(3)	-5(2) 	2(2)

O54	75(4) 	48(3)	38(3) 	7(2)	-2(3) 	22(3)

O55	62(3) 	91(4)	56(4) 	-19(3)	22(3) 	-32(3)

Table 5. Hydrogen coordinates [´ 104] and isotropic displacement parameters [Å2 ´ 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	3429	3508	1899	37	1

H2	4061	4853	1999	35	1

H3	4312	5840	912	39	1

H4	3896	5454	-265	35	1

H7	3528	4909	-1338	30	1

H8	3009	4340	-2371	33	1

H9	2343	3049	-2177	29	1

H14	1277	-1559	1161	31	1

H15	498	-1725	1865	32	1

H16	59	-153	2239	30	1

H19	-322	1512	2503	34	1

H20	-635	3312	2735	34	1

H21	-239	4815	2150	35	1

H22	445	4516	1324	34	1

H31	3338	1299	-755	33	1

H32	4031	60	-872	32	1

H33	4367	-745	225	38	1

H34	4022	-270	1419	37	1

H37	3571	65	2510	34	1

H38	3099	687	3544	34	1

H39	2388	1879	3356	31	1

H44	1294	6414	-8	31	1

H45	543	6592	-756	40	1

H46	57	4997	-1063	37	1

H49	-318	3365	-1334	33	1

H50	-652	1584	-1520	42	1

H51	-262	50	-950	40	1

H52	434	358	-128	31	1

H3A	1371	1656	-1083	30	1

H3B	1638	2369	-1692	30	1

H6A	2363	-40	327	27	1

H6B	2085	-860	855	27	1

H33A	1403	3302	2268	34	1

H33B	1666	2599	2885	34	1

H36A	2369	4943	842	29	1

H36B	2076	5758	329	29	1